|  |
| --- |
| **Acid dyeing of polyamide-6,6 fabric with carbon black nano particle** |
| **for camouflage textiles in Vis-NIR Spectrums** |
| Md. Anowar Hossain |
| School of Fashion and Textiles, RMIT University, 25 Dawson Street, Brunswick, Melbourne, VIC 3056, Australia |

[(e](mailto:engr.anowar@yahoo.com)ngr.ano[war@yahoo.co](mailto:engr.anowar@yahoo.com)m)

|  |
| --- |
| **NIR-K-M reflection of undyed PA-6,6 fabric and CBNP dyed PA-6,6 fabric with** |
| **Formulation-1, PH:0; Formulation-2, PH:1; Formulation-3, PH:2; Formulation-4, PH:3** |
| **Formulation-5, PH:4; Formulation-6, PH:5; Formulation-7, PH:6** |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Wavelength (nm)** | **Untreated PA-6,6 fabric** | **Formulation-1** | **Formulation-2** | **Formulation-3** | **Formulation-4** | **Formulation-5** | **Formulation-6** | **Formulation-7** |
| 1000 | 0.30 | 2.29 | 2.07 | 2.35 | 3.22 | 5.95 | 2.02 | 1.68 |
| 1000.5 | 0.30 | 2.3 | 2.08 | 2.34 | 3.21 | 5.91 | 2.02 | 1.68 |
| 1001 | 0.29 | 2.31 | 2.08 | 2.34 | 3.22 | 5.9 | 2.01 | 1.67 |
| 1001.5 | 0.29 | 2.32 | 2.06 | 2.35 | 3.23 | 5.9 | 2 | 1.67 |
| 1002 | 0.30 | 2.32 | 2.05 | 2.35 | 3.25 | 5.88 | 2 | 1.67 |
| 1002.5 | 0.30 | 2.33 | 2.04 | 2.36 | 3.25 | 5.88 | 2.01 | 1.68 |
| 1003 | 0.30 | 2.33 | 2.04 | 2.36 | 3.23 | 5.88 | 2.02 | 1.68 |
| 1003.5 | 0.30 | 2.32 | 2.04 | 2.35 | 3.21 | 5.87 | 2.02 | 1.69 |
| 1004 | 0.30 | 2.32 | 2.05 | 2.34 | 3.2 | 5.87 | 2.02 | 1.68 |
| 1004.5 | 0.30 | 2.32 | 2.05 | 2.33 | 3.22 | 5.87 | 2.01 | 1.66 |
| 1005 | 0.29 | 2.33 | 2.05 | 2.33 | 3.23 | 5.87 | 2.02 | 1.65 |
| 1005.5 | 0.29 | 2.33 | 2.04 | 2.33 | 3.22 | 5.85 | 2.03 | 1.65 |
| 1006 | 0.29 | 2.32 | 2.03 | 2.34 | 3.21 | 5.82 | 2.02 | 1.66 |
| 1006.5 | 0.30 | 2.32 | 2.02 | 2.35 | 3.21 | 5.8 | 2 | 1.66 |
| 1007 | 0.30 | 2.32 | 2.03 | 2.35 | 3.22 | 5.78 | 1.99 | 1.66 |
| 1007.5 | 0.30 | 2.33 | 2.03 | 2.35 | 3.22 | 5.77 | 2 | 1.66 |
| 1008 | 0.30 | 2.32 | 2.03 | 2.33 | 3.2 | 5.79 | 2.01 | 1.67 |
| 1008.5 | 0.30 | 2.31 | 2.04 | 2.33 | 3.18 | 5.81 | 2.01 | 1.67 |
| 1009 | 0.30 | 2.3 | 2.04 | 2.34 | 3.16 | 5.81 | 2.01 | 1.67 |
| 1009.5 | 0.30 | 2.3 | 2.03 | 2.34 | 3.16 | 5.78 | 2.01 | 1.67 |
| 1010 | 0.30 | 2.31 | 2.03 | 2.34 | 3.16 | 5.74 | 2 | 1.67 |
| 1010.5 | 0.30 | 2.31 | 2.04 | 2.34 | 3.17 | 5.71 | 2 | 1.66 |
| 1011 | 0.30 | 2.31 | 2.04 | 2.35 | 3.18 | 5.71 | 1.99 | 1.65 |
| 1011.5 | 0.30 | 2.3 | 2.03 | 2.35 | 3.18 | 5.74 | 1.99 | 1.65 |
| 1012 | 0.30 | 2.29 | 2.01 | 2.35 | 3.19 | 5.77 | 1.99 | 1.66 |
| 1012.5 | 0.30 | 2.28 | 2.01 | 2.35 | 3.2 | 5.79 | 1.99 | 1.66 |
| 1013 | 0.30 | 2.28 | 2.01 | 2.34 | 3.2 | 5.78 | 1.99 | 1.66 |
| 1013.5 | 0.30 | 2.29 | 2.01 | 2.33 | 3.19 | 5.75 | 1.99 | 1.66 |
| 1014 | 0.30 | 2.3 | 2.01 | 2.32 | 3.18 | 5.74 | 1.99 | 1.65 |
| 1014.5 | 0.30 | 2.3 | 2.02 | 2.31 | 3.18 | 5.76 | 1.99 | 1.65 |
| 1015 | 0.30 | 2.3 | 2.03 | 2.3 | 3.17 | 5.78 | 1.99 | 1.65 |
| 1015.5 | 0.30 | 2.3 | 2.03 | 2.3 | 3.17 | 5.79 | 1.99 | 1.66 |
| 1016 | 0.30 | 2.29 | 2.02 | 2.3 | 3.17 | 5.78 | 1.99 | 1.66 |
| 1016.5 | 0.30 | 2.29 | 2.01 | 2.31 | 3.18 | 5.8 | 1.98 | 1.66 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1017 | 0.30 | 2.3 | 2.01 | 2.31 | 3.19 | 5.84 | 1.97 | 1.65 |
| 1017.5 | 0.30 | 2.3 | 2.01 | 2.3 | 3.2 | 5.87 | 1.97 | 1.65 |
| 1018 | 0.30 | 2.29 | 2.01 | 2.3 | 3.19 | 5.87 | 1.97 | 1.65 |
| 1018.5 | 0.30 | 2.28 | 2.02 | 2.31 | 3.19 | 5.84 | 1.98 | 1.65 |
| 1019 | 0.30 | 2.28 | 2.03 | 2.32 | 3.19 | 5.81 | 1.98 | 1.65 |
| 1019.5 | 0.30 | 2.28 | 2.03 | 2.34 | 3.2 | 5.78 | 1.98 | 1.66 |
| 1020 | 0.30 | 2.28 | 2.03 | 2.35 | 3.2 | 5.76 | 1.98 | 1.66 |
| 1020.5 | 0.30 | 2.28 | 2.02 | 2.35 | 3.19 | 5.77 | 1.99 | 1.67 |
| 1021 | 0.30 | 2.29 | 2.03 | 2.34 | 3.19 | 5.79 | 1.99 | 1.66 |
| 1021.5 | 0.30 | 2.29 | 2.03 | 2.33 | 3.18 | 5.8 | 2 | 1.65 |
| 1022 | 0.30 | 2.29 | 2.02 | 2.32 | 3.18 | 5.79 | 2 | 1.65 |
| 1022.5 | 0.30 | 2.3 | 2.01 | 2.31 | 3.2 | 5.79 | 2 | 1.64 |
| 1023 | 0.30 | 2.3 | 2.01 | 2.3 | 3.21 | 5.8 | 2 | 1.65 |
| 1023.5 | 0.30 | 2.29 | 2.02 | 2.3 | 3.21 | 5.78 | 2 | 1.65 |
| 1024 | 0.30 | 2.27 | 2.03 | 2.31 | 3.2 | 5.75 | 1.99 | 1.65 |
| 1024.5 | 0.30 | 2.27 | 2.03 | 2.31 | 3.18 | 5.72 | 1.98 | 1.65 |
| 1025 | 0.30 | 2.28 | 2.03 | 2.3 | 3.16 | 5.71 | 1.98 | 1.65 |
| 1025.5 | 0.30 | 2.29 | 2.03 | 2.29 | 3.14 | 5.72 | 1.98 | 1.65 |
| 1026 | 0.30 | 2.29 | 2.01 | 2.29 | 3.13 | 5.75 | 1.98 | 1.65 |
| 1026.5 | 0.30 | 2.28 | 2 | 2.29 | 3.14 | 5.77 | 1.98 | 1.66 |
| 1027 | 0.30 | 2.28 | 2 | 2.3 | 3.17 | 5.77 | 1.98 | 1.67 |
| 1027.5 | 0.30 | 2.27 | 2 | 2.31 | 3.18 | 5.74 | 1.98 | 1.67 |
| 1028 | 0.30 | 2.27 | 2.01 | 2.31 | 3.19 | 5.72 | 1.98 | 1.67 |
| 1028.5 | 0.30 | 2.27 | 2.01 | 2.31 | 3.18 | 5.73 | 1.99 | 1.67 |
| 1029 | 0.30 | 2.27 | 2.01 | 2.3 | 3.18 | 5.77 | 1.99 | 1.67 |
| 1029.5 | 0.30 | 2.28 | 2.01 | 2.3 | 3.19 | 5.81 | 1.99 | 1.67 |
| 1030 | 0.30 | 2.29 | 2.01 | 2.3 | 3.18 | 5.81 | 1.98 | 1.67 |
| 1030.5 | 0.30 | 2.3 | 2.01 | 2.29 | 3.15 | 5.79 | 1.98 | 1.67 |
| 1031 | 0.30 | 2.3 | 2.01 | 2.28 | 3.11 | 5.78 | 1.97 | 1.66 |
| 1031.5 | 0.30 | 2.29 | 2.01 | 2.28 | 3.09 | 5.78 | 1.98 | 1.66 |
| 1032 | 0.30 | 2.29 | 2.01 | 2.29 | 3.1 | 5.78 | 1.98 | 1.65 |
| 1032.5 | 0.30 | 2.29 | 2.02 | 2.3 | 3.14 | 5.78 | 1.99 | 1.65 |
| 1033 | 0.30 | 2.3 | 2.02 | 2.31 | 3.17 | 5.8 | 1.98 | 1.66 |
| 1033.5 | 0.30 | 2.3 | 2.02 | 2.31 | 3.19 | 5.83 | 1.98 | 1.66 |
| 1034 | 0.30 | 2.29 | 2.01 | 2.32 | 3.18 | 5.84 | 1.98 | 1.66 |
| 1034.5 | 0.30 | 2.28 | 2 | 2.32 | 3.16 | 5.85 | 1.98 | 1.65 |
| 1035 | 0.30 | 2.27 | 1.99 | 2.31 | 3.14 | 5.85 | 1.97 | 1.65 |
| 1035.5 | 0.30 | 2.27 | 1.99 | 2.31 | 3.13 | 5.83 | 1.97 | 1.64 |
| 1036 | 0.30 | 2.27 | 1.99 | 2.3 | 3.13 | 5.77 | 1.96 | 1.64 |
| 1036.5 | 0.30 | 2.27 | 1.99 | 2.3 | 3.14 | 5.73 | 1.96 | 1.65 |
| 1037 | 0.30 | 2.27 | 2 | 2.31 | 3.13 | 5.74 | 1.96 | 1.65 |
| 1037.5 | 0.30 | 2.27 | 2 | 2.32 | 3.13 | 5.8 | 1.97 | 1.65 |
| 1038 | 0.30 | 2.27 | 2.01 | 2.32 | 3.12 | 5.84 | 1.97 | 1.64 |
| 1038.5 | 0.30 | 2.27 | 2 | 2.31 | 3.12 | 5.84 | 1.98 | 1.63 |
| 1039 | 0.30 | 2.27 | 2 | 2.29 | 3.11 | 5.82 | 1.97 | 1.63 |
| 1039.5 | 0.30 | 2.26 | 2 | 2.28 | 3.1 | 5.79 | 1.97 | 1.63 |
| 1040 | 0.30 | 2.25 | 2 | 2.27 | 3.11 | 5.75 | 1.97 | 1.63 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1040.5 | 0.30 | 2.24 | 1.99 | 2.27 | 3.13 | 5.71 | 1.97 | 1.63 |
| 1041 | 0.30 | 2.24 | 1.99 | 2.28 | 3.16 | 5.69 | 1.98 | 1.64 |
| 1041.5 | 0.30 | 2.25 | 1.99 | 2.29 | 3.18 | 5.7 | 1.98 | 1.64 |
| 1042 | 0.30 | 2.26 | 1.98 | 2.29 | 3.17 | 5.69 | 1.98 | 1.65 |
| 1042.5 | 0.30 | 2.27 | 1.99 | 2.29 | 3.16 | 5.67 | 1.97 | 1.64 |
| 1043 | 0.30 | 2.27 | 1.99 | 2.29 | 3.16 | 5.66 | 1.97 | 1.64 |
| 1043.5 | 0.30 | 2.27 | 2 | 2.28 | 3.16 | 5.7 | 1.96 | 1.64 |
| 1044 | 0.30 | 2.26 | 2 | 2.28 | 3.16 | 5.75 | 1.96 | 1.64 |
| 1044.5 | 0.30 | 2.25 | 1.99 | 2.27 | 3.15 | 5.78 | 1.97 | 1.63 |
| 1045 | 0.30 | 2.25 | 1.99 | 2.26 | 3.15 | 5.78 | 1.97 | 1.62 |
| 1045.5 | 0.30 | 2.25 | 1.98 | 2.25 | 3.16 | 5.76 | 1.98 | 1.63 |
| 1046 | 0.30 | 2.26 | 1.98 | 2.24 | 3.15 | 5.74 | 1.97 | 1.63 |
| 1046.5 | 0.30 | 2.28 | 1.98 | 2.25 | 3.13 | 5.73 | 1.97 | 1.65 |
| 1047 | 0.30 | 2.29 | 1.98 | 2.26 | 3.12 | 5.73 | 1.96 | 1.66 |
| 1047.5 | 0.30 | 2.29 | 1.98 | 2.27 | 3.11 | 5.73 | 1.94 | 1.66 |
| 1048 | 0.30 | 2.28 | 1.98 | 2.28 | 3.1 | 5.7 | 1.93 | 1.66 |
| 1048.5 | 0.30 | 2.26 | 1.98 | 2.28 | 3.1 | 5.65 | 1.93 | 1.66 |
| 1049 | 0.30 | 2.25 | 1.99 | 2.28 | 3.1 | 5.63 | 1.93 | 1.65 |
| 1049.5 | 0.30 | 2.24 | 1.98 | 2.28 | 3.1 | 5.63 | 1.94 | 1.64 |
| 1050 | 0.30 | 2.23 | 1.98 | 2.29 | 3.1 | 5.65 | 1.95 | 1.63 |
| 1050.5 | 0.30 | 2.24 | 1.98 | 2.29 | 3.11 | 5.7 | 1.95 | 1.63 |
| 1051 | 0.30 | 2.25 | 1.99 | 2.3 | 3.11 | 5.74 | 1.96 | 1.64 |
| 1051.5 | 0.30 | 2.27 | 1.99 | 2.29 | 3.13 | 5.76 | 1.96 | 1.65 |
| 1052 | 0.30 | 2.27 | 1.99 | 2.28 | 3.14 | 5.75 | 1.97 | 1.65 |
| 1052.5 | 0.30 | 2.27 | 1.99 | 2.27 | 3.15 | 5.74 | 1.97 | 1.65 |
| 1053 | 0.30 | 2.27 | 1.99 | 2.27 | 3.14 | 5.75 | 1.97 | 1.65 |
| 1053.5 | 0.30 | 2.26 | 1.98 | 2.28 | 3.11 | 5.77 | 1.96 | 1.65 |
| 1054 | 0.30 | 2.26 | 1.99 | 2.28 | 3.09 | 5.78 | 1.96 | 1.64 |
| 1054.5 | 0.30 | 2.26 | 1.99 | 2.28 | 3.07 | 5.77 | 1.96 | 1.63 |
| 1055 | 0.30 | 2.27 | 1.98 | 2.28 | 3.07 | 5.73 | 1.95 | 1.62 |
| 1055.5 | 0.30 | 2.27 | 1.98 | 2.27 | 3.08 | 5.69 | 1.95 | 1.63 |
| 1056 | 0.30 | 2.27 | 1.98 | 2.26 | 3.09 | 5.67 | 1.95 | 1.64 |
| 1056.5 | 0.30 | 2.26 | 1.98 | 2.26 | 3.1 | 5.67 | 1.95 | 1.64 |
| 1057 | 0.30 | 2.25 | 1.98 | 2.25 | 3.11 | 5.67 | 1.94 | 1.65 |
| 1057.5 | 0.30 | 2.24 | 1.98 | 2.25 | 3.11 | 5.66 | 1.94 | 1.65 |
| 1058 | 0.30 | 2.24 | 1.98 | 2.25 | 3.11 | 5.65 | 1.93 | 1.64 |
| 1058.5 | 0.30 | 2.23 | 1.97 | 2.25 | 3.1 | 5.65 | 1.94 | 1.65 |
| 1059 | 0.30 | 2.23 | 1.96 | 2.25 | 3.1 | 5.65 | 1.94 | 1.65 |
| 1059.5 | 0.30 | 2.23 | 1.96 | 2.25 | 3.1 | 5.67 | 1.93 | 1.64 |
| 1060 | 0.30 | 2.24 | 1.96 | 2.25 | 3.1 | 5.69 | 1.93 | 1.64 |
| 1060.5 | 0.30 | 2.25 | 1.97 | 2.25 | 3.09 | 5.72 | 1.92 | 1.64 |
| 1061 | 0.30 | 2.26 | 1.98 | 2.24 | 3.09 | 5.72 | 1.92 | 1.64 |
| 1061.5 | 0.30 | 2.25 | 1.98 | 2.24 | 3.1 | 5.71 | 1.92 | 1.64 |
| 1062 | 0.30 | 2.25 | 1.97 | 2.23 | 3.11 | 5.68 | 1.92 | 1.64 |
| 1062.5 | 0.30 | 2.24 | 1.97 | 2.23 | 3.11 | 5.64 | 1.92 | 1.64 |
| 1063 | 0.30 | 2.23 | 1.97 | 2.24 | 3.1 | 5.61 | 1.92 | 1.63 |
| 1063.5 | 0.30 | 2.22 | 1.98 | 2.24 | 3.08 | 5.61 | 1.92 | 1.63 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1064 | 0.30 | 2.21 | 1.99 | 2.24 | 3.07 | 5.62 | 1.91 | 1.63 |
| 1064.5 | 0.30 | 2.22 | 1.99 | 2.24 | 3.06 | 5.63 | 1.92 | 1.63 |
| 1065 | 0.30 | 2.23 | 1.99 | 2.23 | 3.06 | 5.63 | 1.92 | 1.63 |
| 1065.5 | 0.30 | 2.24 | 1.98 | 2.23 | 3.06 | 5.62 | 1.92 | 1.63 |
| 1066 | 0.30 | 2.24 | 1.98 | 2.23 | 3.07 | 5.63 | 1.93 | 1.63 |
| 1066.5 | 0.30 | 2.24 | 1.98 | 2.24 | 3.08 | 5.65 | 1.93 | 1.63 |
| 1067 | 0.30 | 2.24 | 1.98 | 2.24 | 3.08 | 5.66 | 1.93 | 1.64 |
| 1067.5 | 0.30 | 2.24 | 1.98 | 2.24 | 3.08 | 5.64 | 1.93 | 1.64 |
| 1068 | 0.30 | 2.23 | 1.97 | 2.25 | 3.08 | 5.61 | 1.93 | 1.64 |
| 1068.5 | 0.30 | 2.22 | 1.96 | 2.24 | 3.07 | 5.61 | 1.93 | 1.63 |
| 1069 | 0.30 | 2.21 | 1.96 | 2.24 | 3.07 | 5.63 | 1.94 | 1.63 |
| 1069.5 | 0.30 | 2.21 | 1.96 | 2.23 | 3.06 | 5.65 | 1.94 | 1.63 |
| 1070 | 0.30 | 2.21 | 1.96 | 2.23 | 3.06 | 5.65 | 1.94 | 1.63 |
| 1070.5 | 0.30 | 2.22 | 1.96 | 2.24 | 3.07 | 5.65 | 1.93 | 1.63 |
| 1071 | 0.30 | 2.22 | 1.96 | 2.24 | 3.08 | 5.66 | 1.92 | 1.62 |
| 1071.5 | 0.30 | 2.21 | 1.96 | 2.24 | 3.08 | 5.67 | 1.91 | 1.62 |
| 1072 | 0.30 | 2.21 | 1.96 | 2.24 | 3.08 | 5.66 | 1.91 | 1.61 |
| 1072.5 | 0.30 | 2.21 | 1.95 | 2.24 | 3.07 | 5.63 | 1.9 | 1.61 |
| 1073 | 0.30 | 2.21 | 1.95 | 2.24 | 3.07 | 5.61 | 1.9 | 1.62 |
| 1073.5 | 0.30 | 2.22 | 1.96 | 2.24 | 3.08 | 5.62 | 1.9 | 1.63 |
| 1074 | 0.30 | 2.22 | 1.96 | 2.24 | 3.08 | 5.64 | 1.91 | 1.64 |
| 1074.5 | 0.30 | 2.22 | 1.96 | 2.24 | 3.08 | 5.66 | 1.92 | 1.64 |
| 1075 | 0.30 | 2.22 | 1.96 | 2.24 | 3.07 | 5.66 | 1.92 | 1.63 |
| 1075.5 | 0.30 | 2.23 | 1.95 | 2.24 | 3.06 | 5.65 | 1.93 | 1.62 |
| 1076 | 0.30 | 2.23 | 1.95 | 2.24 | 3.05 | 5.63 | 1.93 | 1.62 |
| 1076.5 | 0.30 | 2.23 | 1.94 | 2.25 | 3.05 | 5.61 | 1.92 | 1.62 |
| 1077 | 0.30 | 2.23 | 1.94 | 2.25 | 3.04 | 5.59 | 1.92 | 1.62 |
| 1077.5 | 0.30 | 2.22 | 1.94 | 2.25 | 3.02 | 5.57 | 1.91 | 1.62 |
| 1078 | 0.30 | 2.22 | 1.94 | 2.24 | 3.01 | 5.57 | 1.9 | 1.62 |
| 1078.5 | 0.30 | 2.22 | 1.94 | 2.24 | 3.01 | 5.58 | 1.9 | 1.61 |
| 1079 | 0.30 | 2.22 | 1.94 | 2.23 | 3.03 | 5.57 | 1.9 | 1.61 |
| 1079.5 | 0.30 | 2.22 | 1.94 | 2.22 | 3.04 | 5.55 | 1.91 | 1.61 |
| 1080 | 0.30 | 2.22 | 1.94 | 2.21 | 3.04 | 5.55 | 1.91 | 1.61 |
| 1080.5 | 0.30 | 2.21 | 1.94 | 2.19 | 3.05 | 5.56 | 1.91 | 1.62 |
| 1081 | 0.30 | 2.2 | 1.95 | 2.19 | 3.05 | 5.59 | 1.91 | 1.62 |
| 1081.5 | 0.30 | 2.2 | 1.95 | 2.2 | 3.05 | 5.6 | 1.91 | 1.62 |
| 1082 | 0.30 | 2.2 | 1.95 | 2.2 | 3.05 | 5.58 | 1.91 | 1.62 |
| 1082.5 | 0.30 | 2.21 | 1.95 | 2.21 | 3.05 | 5.56 | 1.91 | 1.61 |
| 1083 | 0.30 | 2.21 | 1.95 | 2.21 | 3.05 | 5.55 | 1.9 | 1.61 |
| 1083.5 | 0.30 | 2.22 | 1.95 | 2.21 | 3.05 | 5.54 | 1.9 | 1.61 |
| 1084 | 0.30 | 2.22 | 1.96 | 2.22 | 3.04 | 5.54 | 1.9 | 1.61 |
| 1084.5 | 0.30 | 2.22 | 1.96 | 2.22 | 3.03 | 5.53 | 1.9 | 1.61 |
| 1085 | 0.30 | 2.22 | 1.96 | 2.23 | 3.03 | 5.54 | 1.89 | 1.61 |
| 1085.5 | 0.30 | 2.22 | 1.95 | 2.24 | 3.03 | 5.57 | 1.89 | 1.62 |
| 1086 | 0.30 | 2.21 | 1.95 | 2.24 | 3.04 | 5.6 | 1.89 | 1.62 |
| 1086.5 | 0.30 | 2.21 | 1.95 | 2.23 | 3.05 | 5.6 | 1.9 | 1.61 |
| 1087 | 0.30 | 2.2 | 1.95 | 2.22 | 3.04 | 5.58 | 1.89 | 1.61 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1087.5 | 0.30 | 2.19 | 1.95 | 2.21 | 3.04 | 5.55 | 1.89 | 1.6 |
| 1088 | 0.30 | 2.19 | 1.95 | 2.21 | 3.04 | 5.54 | 1.89 | 1.6 |
| 1088.5 | 0.29 | 2.19 | 1.95 | 2.2 | 3.03 | 5.54 | 1.89 | 1.6 |
| 1089 | 0.30 | 2.19 | 1.95 | 2.19 | 3.02 | 5.52 | 1.89 | 1.6 |
| 1089.5 | 0.30 | 2.2 | 1.95 | 2.19 | 3.01 | 5.49 | 1.88 | 1.6 |
| 1090 | 0.30 | 2.2 | 1.93 | 2.19 | 3.01 | 5.48 | 1.88 | 1.6 |
| 1090.5 | 0.30 | 2.19 | 1.92 | 2.19 | 3.02 | 5.48 | 1.88 | 1.61 |
| 1091 | 0.30 | 2.18 | 1.92 | 2.2 | 3.03 | 5.5 | 1.88 | 1.61 |
| 1091.5 | 0.30 | 2.18 | 1.92 | 2.2 | 3.02 | 5.52 | 1.89 | 1.61 |
| 1092 | 0.30 | 2.18 | 1.92 | 2.2 | 3.01 | 5.53 | 1.89 | 1.61 |
| 1092.5 | 0.30 | 2.18 | 1.92 | 2.2 | 3.01 | 5.52 | 1.89 | 1.61 |
| 1093 | 0.30 | 2.18 | 1.91 | 2.2 | 3 | 5.52 | 1.9 | 1.61 |
| 1093.5 | 0.30 | 2.19 | 1.91 | 2.2 | 3 | 5.52 | 1.9 | 1.61 |
| 1094 | 0.30 | 2.19 | 1.9 | 2.2 | 3 | 5.52 | 1.9 | 1.6 |
| 1094.5 | 0.30 | 2.19 | 1.91 | 2.19 | 3 | 5.53 | 1.9 | 1.6 |
| 1095 | 0.30 | 2.19 | 1.92 | 2.19 | 3 | 5.54 | 1.9 | 1.59 |
| 1095.5 | 0.30 | 2.19 | 1.93 | 2.2 | 3 | 5.54 | 1.9 | 1.59 |
| 1096 | 0.30 | 2.19 | 1.95 | 2.2 | 3 | 5.54 | 1.9 | 1.6 |
| 1096.5 | 0.30 | 2.19 | 1.95 | 2.21 | 3.01 | 5.52 | 1.89 | 1.6 |
| 1097 | 0.30 | 2.19 | 1.95 | 2.21 | 3.02 | 5.51 | 1.89 | 1.6 |
| 1097.5 | 0.30 | 2.19 | 1.94 | 2.21 | 3.02 | 5.52 | 1.88 | 1.6 |
| 1098 | 0.30 | 2.19 | 1.92 | 2.21 | 3.02 | 5.54 | 1.88 | 1.6 |
| 1098.5 | 0.30 | 2.19 | 1.92 | 2.2 | 3.01 | 5.55 | 1.88 | 1.6 |
| 1099 | 0.30 | 2.19 | 1.91 | 2.2 | 3 | 5.54 | 1.88 | 1.6 |
| 1099.5 | 0.30 | 2.19 | 1.91 | 2.2 | 3 | 5.54 | 1.88 | 1.59 |
| 1100 | 0.30 | 2.18 | 1.92 | 2.21 | 3.02 | 5.54 | 1.88 | 1.59 |
| 1100.5 | 0.30 | 2.19 | 1.92 | 2.21 | 3.03 | 5.54 | 1.88 | 1.6 |
| 1101 | 0.30 | 2.19 | 1.92 | 2.21 | 3.03 | 5.54 | 1.89 | 1.6 |
| 1101.5 | 0.30 | 2.19 | 1.92 | 2.2 | 3.01 | 5.53 | 1.89 | 1.6 |
| 1102 | 0.30 | 2.2 | 1.92 | 2.2 | 2.99 | 5.52 | 1.89 | 1.6 |
| 1102.5 | 0.30 | 2.2 | 1.93 | 2.2 | 2.98 | 5.53 | 1.89 | 1.6 |
| 1103 | 0.30 | 2.2 | 1.93 | 2.19 | 2.98 | 5.56 | 1.89 | 1.6 |
| 1103.5 | 0.30 | 2.19 | 1.92 | 2.19 | 2.98 | 5.6 | 1.88 | 1.6 |
| 1104 | 0.30 | 2.18 | 1.92 | 2.19 | 2.99 | 5.63 | 1.88 | 1.6 |
| 1104.5 | 0.30 | 2.18 | 1.92 | 2.2 | 3 | 5.61 | 1.88 | 1.6 |
| 1105 | 0.30 | 2.18 | 1.92 | 2.2 | 3 | 5.56 | 1.88 | 1.6 |
| 1105.5 | 0.30 | 2.18 | 1.91 | 2.19 | 3 | 5.5 | 1.88 | 1.6 |
| 1106 | 0.30 | 2.18 | 1.91 | 2.19 | 2.99 | 5.46 | 1.88 | 1.6 |
| 1106.5 | 0.30 | 2.18 | 1.91 | 2.19 | 2.98 | 5.45 | 1.88 | 1.6 |
| 1107 | 0.30 | 2.18 | 1.9 | 2.19 | 2.98 | 5.46 | 1.88 | 1.6 |
| 1107.5 | 0.30 | 2.18 | 1.9 | 2.19 | 2.98 | 5.48 | 1.88 | 1.59 |
| 1108 | 0.30 | 2.18 | 1.9 | 2.18 | 2.98 | 5.49 | 1.88 | 1.59 |
| 1108.5 | 0.30 | 2.17 | 1.9 | 2.18 | 2.98 | 5.5 | 1.88 | 1.59 |
| 1109 | 0.30 | 2.17 | 1.9 | 2.18 | 2.98 | 5.51 | 1.89 | 1.59 |
| 1109.5 | 0.30 | 2.17 | 1.91 | 2.19 | 2.98 | 5.52 | 1.89 | 1.59 |
| 1110 | 0.30 | 2.17 | 1.91 | 2.19 | 2.98 | 5.54 | 1.88 | 1.59 |
| 1110.5 | 0.30 | 2.18 | 1.91 | 2.2 | 2.98 | 5.56 | 1.87 | 1.59 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1111 | 0.30 | 2.18 | 1.92 | 2.19 | 2.98 | 5.58 | 1.87 | 1.59 |
| 1111.5 | 0.30 | 2.18 | 1.92 | 2.18 | 2.99 | 5.57 | 1.87 | 1.59 |
| 1112 | 0.30 | 2.18 | 1.92 | 2.18 | 2.99 | 5.56 | 1.87 | 1.59 |
| 1112.5 | 0.30 | 2.17 | 1.92 | 2.18 | 3 | 5.55 | 1.87 | 1.59 |
| 1113 | 0.30 | 2.17 | 1.91 | 2.18 | 3 | 5.56 | 1.86 | 1.59 |
| 1113.5 | 0.30 | 2.17 | 1.91 | 2.19 | 3 | 5.57 | 1.85 | 1.59 |
| 1114 | 0.30 | 2.17 | 1.9 | 2.19 | 3 | 5.57 | 1.85 | 1.59 |
| 1114.5 | 0.30 | 2.17 | 1.9 | 2.19 | 3 | 5.55 | 1.86 | 1.59 |
| 1115 | 0.30 | 2.18 | 1.9 | 2.19 | 2.99 | 5.51 | 1.86 | 1.59 |
| 1115.5 | 0.30 | 2.18 | 1.9 | 2.18 | 2.99 | 5.5 | 1.87 | 1.59 |
| 1116 | 0.30 | 2.17 | 1.9 | 2.17 | 2.99 | 5.5 | 1.87 | 1.59 |
| 1116.5 | 0.30 | 2.16 | 1.89 | 2.17 | 2.99 | 5.51 | 1.87 | 1.59 |
| 1117 | 0.30 | 2.16 | 1.89 | 2.17 | 2.98 | 5.51 | 1.87 | 1.6 |
| 1117.5 | 0.30 | 2.15 | 1.89 | 2.17 | 2.98 | 5.49 | 1.87 | 1.6 |
| 1118 | 0.30 | 2.15 | 1.88 | 2.16 | 2.98 | 5.47 | 1.87 | 1.6 |
| 1118.5 | 0.30 | 2.15 | 1.89 | 2.16 | 2.98 | 5.45 | 1.87 | 1.59 |
| 1119 | 0.30 | 2.16 | 1.89 | 2.15 | 2.98 | 5.44 | 1.87 | 1.59 |
| 1119.5 | 0.30 | 2.16 | 1.89 | 2.15 | 2.97 | 5.44 | 1.87 | 1.58 |
| 1120 | 0.30 | 2.16 | 1.89 | 2.15 | 2.97 | 5.45 | 1.87 | 1.58 |
| 1120.5 | 0.30 | 2.15 | 1.89 | 2.15 | 2.95 | 5.45 | 1.87 | 1.58 |
| 1121 | 0.30 | 2.15 | 1.89 | 2.15 | 2.94 | 5.43 | 1.86 | 1.58 |
| 1121.5 | 0.30 | 2.14 | 1.9 | 2.14 | 2.93 | 5.42 | 1.85 | 1.58 |
| 1122 | 0.30 | 2.14 | 1.9 | 2.14 | 2.92 | 5.41 | 1.85 | 1.58 |
| 1122.5 | 0.30 | 2.14 | 1.9 | 2.14 | 2.93 | 5.42 | 1.85 | 1.58 |
| 1123 | 0.30 | 2.15 | 1.9 | 2.15 | 2.94 | 5.44 | 1.85 | 1.58 |
| 1123.5 | 0.30 | 2.15 | 1.9 | 2.16 | 2.96 | 5.44 | 1.84 | 1.58 |
| 1124 | 0.30 | 2.15 | 1.9 | 2.17 | 2.97 | 5.45 | 1.84 | 1.58 |
| 1124.5 | 0.30 | 2.15 | 1.9 | 2.17 | 2.97 | 5.45 | 1.84 | 1.58 |
| 1125 | 0.30 | 2.15 | 1.89 | 2.17 | 2.97 | 5.45 | 1.84 | 1.58 |
| 1125.5 | 0.30 | 2.15 | 1.89 | 2.17 | 2.97 | 5.46 | 1.84 | 1.58 |
| 1126 | 0.30 | 2.15 | 1.88 | 2.16 | 2.96 | 5.45 | 1.84 | 1.58 |
| 1126.5 | 0.30 | 2.15 | 1.88 | 2.17 | 2.96 | 5.45 | 1.85 | 1.59 |
| 1127 | 0.30 | 2.16 | 1.88 | 2.18 | 2.96 | 5.45 | 1.85 | 1.59 |
| 1127.5 | 0.30 | 2.16 | 1.88 | 2.18 | 2.97 | 5.47 | 1.85 | 1.59 |
| 1128 | 0.30 | 2.17 | 1.88 | 2.18 | 2.97 | 5.49 | 1.84 | 1.59 |
| 1128.5 | 0.30 | 2.16 | 1.88 | 2.17 | 2.97 | 5.5 | 1.84 | 1.59 |
| 1129 | 0.30 | 2.15 | 1.88 | 2.17 | 2.96 | 5.49 | 1.84 | 1.59 |
| 1129.5 | 0.30 | 2.14 | 1.88 | 2.16 | 2.96 | 5.47 | 1.84 | 1.58 |
| 1130 | 0.30 | 2.13 | 1.88 | 2.15 | 2.95 | 5.45 | 1.84 | 1.58 |
| 1130.5 | 0.30 | 2.13 | 1.88 | 2.15 | 2.95 | 5.44 | 1.83 | 1.58 |
| 1131 | 0.30 | 2.13 | 1.88 | 2.15 | 2.95 | 5.44 | 1.84 | 1.58 |
| 1131.5 | 0.30 | 2.14 | 1.89 | 2.15 | 2.95 | 5.45 | 1.84 | 1.58 |
| 1132 | 0.30 | 2.14 | 1.89 | 2.15 | 2.96 | 5.45 | 1.84 | 1.58 |
| 1132.5 | 0.30 | 2.14 | 1.89 | 2.15 | 2.96 | 5.46 | 1.85 | 1.58 |
| 1133 | 0.30 | 2.14 | 1.88 | 2.15 | 2.96 | 5.46 | 1.85 | 1.58 |
| 1133.5 | 0.30 | 2.14 | 1.88 | 2.14 | 2.95 | 5.45 | 1.85 | 1.58 |
| 1134 | 0.30 | 2.14 | 1.88 | 2.13 | 2.95 | 5.45 | 1.85 | 1.58 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1134.5 | 0.30 | 2.14 | 1.88 | 2.13 | 2.95 | 5.44 | 1.85 | 1.58 |
| 1135 | 0.30 | 2.15 | 1.89 | 2.14 | 2.95 | 5.44 | 1.84 | 1.59 |
| 1135.5 | 0.30 | 2.15 | 1.89 | 2.14 | 2.95 | 5.44 | 1.84 | 1.59 |
| 1136 | 0.30 | 2.15 | 1.89 | 2.15 | 2.95 | 5.44 | 1.84 | 1.58 |
| 1136.5 | 0.30 | 2.15 | 1.88 | 2.15 | 2.95 | 5.45 | 1.84 | 1.58 |
| 1137 | 0.30 | 2.15 | 1.88 | 2.15 | 2.94 | 5.45 | 1.84 | 1.58 |
| 1137.5 | 0.30 | 2.15 | 1.88 | 2.15 | 2.94 | 5.46 | 1.85 | 1.58 |
| 1138 | 0.30 | 2.15 | 1.88 | 2.15 | 2.94 | 5.46 | 1.85 | 1.59 |
| 1138.5 | 0.30 | 2.15 | 1.88 | 2.15 | 2.94 | 5.45 | 1.84 | 1.59 |
| 1139 | 0.30 | 2.15 | 1.88 | 2.15 | 2.94 | 5.44 | 1.84 | 1.59 |
| 1139.5 | 0.30 | 2.14 | 1.88 | 2.15 | 2.94 | 5.41 | 1.84 | 1.59 |
| 1140 | 0.30 | 2.13 | 1.88 | 2.15 | 2.93 | 5.4 | 1.84 | 1.58 |
| 1140.5 | 0.30 | 2.12 | 1.88 | 2.15 | 2.92 | 5.4 | 1.85 | 1.57 |
| 1141 | 0.30 | 2.12 | 1.89 | 2.15 | 2.92 | 5.41 | 1.85 | 1.57 |
| 1141.5 | 0.30 | 2.13 | 1.89 | 2.15 | 2.92 | 5.43 | 1.84 | 1.57 |
| 1142 | 0.30 | 2.14 | 1.89 | 2.15 | 2.93 | 5.44 | 1.84 | 1.57 |
| 1142.5 | 0.30 | 2.14 | 1.89 | 2.15 | 2.93 | 5.44 | 1.83 | 1.57 |
| 1143 | 0.30 | 2.14 | 1.88 | 2.15 | 2.93 | 5.44 | 1.83 | 1.57 |
| 1143.5 | 0.30 | 2.13 | 1.88 | 2.15 | 2.93 | 5.44 | 1.82 | 1.57 |
| 1144 | 0.31 | 2.13 | 1.89 | 2.14 | 2.92 | 5.44 | 1.83 | 1.57 |
| 1144.5 | 0.31 | 2.13 | 1.89 | 2.14 | 2.92 | 5.42 | 1.83 | 1.57 |
| 1145 | 0.31 | 2.13 | 1.88 | 2.14 | 2.91 | 5.41 | 1.83 | 1.58 |
| 1145.5 | 0.31 | 2.13 | 1.88 | 2.13 | 2.91 | 5.41 | 1.84 | 1.58 |
| 1146 | 0.31 | 2.13 | 1.87 | 2.14 | 2.9 | 5.42 | 1.84 | 1.58 |
| 1146.5 | 0.31 | 2.13 | 1.87 | 2.14 | 2.9 | 5.43 | 1.84 | 1.58 |
| 1147 | 0.31 | 2.13 | 1.87 | 2.14 | 2.9 | 5.43 | 1.84 | 1.58 |
| 1147.5 | 0.31 | 2.13 | 1.87 | 2.14 | 2.91 | 5.42 | 1.84 | 1.57 |
| 1148 | 0.31 | 2.13 | 1.87 | 2.14 | 2.91 | 5.41 | 1.83 | 1.57 |
| 1148.5 | 0.31 | 2.14 | 1.88 | 2.14 | 2.91 | 5.4 | 1.83 | 1.57 |
| 1149 | 0.31 | 2.14 | 1.87 | 2.14 | 2.91 | 5.39 | 1.83 | 1.57 |
| 1149.5 | 0.31 | 2.14 | 1.87 | 2.13 | 2.92 | 5.4 | 1.83 | 1.57 |
| 1150 | 0.31 | 2.13 | 1.87 | 2.13 | 2.92 | 5.41 | 1.83 | 1.58 |
| 1150.5 | 0.31 | 2.13 | 1.87 | 2.12 | 2.92 | 5.42 | 1.83 | 1.58 |
| 1151 | 0.31 | 2.13 | 1.87 | 2.12 | 2.92 | 5.42 | 1.82 | 1.58 |
| 1151.5 | 0.31 | 2.13 | 1.87 | 2.12 | 2.92 | 5.42 | 1.82 | 1.58 |
| 1152 | 0.31 | 2.13 | 1.87 | 2.12 | 2.92 | 5.42 | 1.82 | 1.58 |
| 1152.5 | 0.31 | 2.13 | 1.87 | 2.12 | 2.92 | 5.43 | 1.82 | 1.58 |
| 1153 | 0.31 | 2.13 | 1.87 | 2.13 | 2.93 | 5.43 | 1.83 | 1.58 |
| 1153.5 | 0.31 | 2.13 | 1.88 | 2.13 | 2.93 | 5.43 | 1.83 | 1.58 |
| 1154 | 0.32 | 2.13 | 1.88 | 2.13 | 2.93 | 5.43 | 1.84 | 1.58 |
| 1154.5 | 0.32 | 2.13 | 1.88 | 2.14 | 2.92 | 5.41 | 1.84 | 1.58 |
| 1155 | 0.32 | 2.12 | 1.88 | 2.14 | 2.92 | 5.4 | 1.84 | 1.58 |
| 1155.5 | 0.32 | 2.12 | 1.88 | 2.14 | 2.91 | 5.39 | 1.84 | 1.58 |
| 1156 | 0.31 | 2.11 | 1.87 | 2.14 | 2.91 | 5.38 | 1.84 | 1.58 |
| 1156.5 | 0.31 | 2.11 | 1.87 | 2.13 | 2.91 | 5.39 | 1.84 | 1.58 |
| 1157 | 0.31 | 2.11 | 1.87 | 2.13 | 2.91 | 5.4 | 1.84 | 1.58 |
| 1157.5 | 0.32 | 2.11 | 1.87 | 2.12 | 2.91 | 5.41 | 1.84 | 1.58 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1158 | 0.32 | 2.11 | 1.87 | 2.13 | 2.91 | 5.41 | 1.84 | 1.58 |
| 1158.5 | 0.32 | 2.12 | 1.87 | 2.13 | 2.91 | 5.41 | 1.84 | 1.58 |
| 1159 | 0.32 | 2.12 | 1.87 | 2.13 | 2.91 | 5.42 | 1.84 | 1.58 |
| 1159.5 | 0.32 | 2.12 | 1.87 | 2.13 | 2.91 | 5.43 | 1.83 | 1.58 |
| 1160 | 0.32 | 2.11 | 1.87 | 2.13 | 2.91 | 5.44 | 1.83 | 1.58 |
| 1160.5 | 0.32 | 2.11 | 1.87 | 2.13 | 2.9 | 5.44 | 1.83 | 1.58 |
| 1161 | 0.32 | 2.11 | 1.86 | 2.13 | 2.89 | 5.44 | 1.83 | 1.58 |
| 1161.5 | 0.32 | 2.11 | 1.86 | 2.12 | 2.89 | 5.45 | 1.83 | 1.58 |
| 1162 | 0.32 | 2.12 | 1.86 | 2.12 | 2.88 | 5.45 | 1.83 | 1.58 |
| 1162.5 | 0.32 | 2.12 | 1.86 | 2.12 | 2.88 | 5.45 | 1.83 | 1.57 |
| 1163 | 0.32 | 2.12 | 1.86 | 2.12 | 2.88 | 5.44 | 1.83 | 1.57 |
| 1163.5 | 0.32 | 2.12 | 1.86 | 2.12 | 2.89 | 5.43 | 1.83 | 1.57 |
| 1164 | 0.32 | 2.12 | 1.87 | 2.12 | 2.88 | 5.41 | 1.83 | 1.57 |
| 1164.5 | 0.32 | 2.12 | 1.87 | 2.12 | 2.88 | 5.4 | 1.83 | 1.57 |
| 1165 | 0.32 | 2.12 | 1.87 | 2.11 | 2.88 | 5.4 | 1.83 | 1.57 |
| 1165.5 | 0.32 | 2.13 | 1.87 | 2.11 | 2.89 | 5.4 | 1.83 | 1.57 |
| 1166 | 0.32 | 2.13 | 1.86 | 2.11 | 2.89 | 5.4 | 1.82 | 1.57 |
| 1166.5 | 0.32 | 2.12 | 1.86 | 2.1 | 2.89 | 5.4 | 1.82 | 1.57 |
| 1167 | 0.32 | 2.12 | 1.86 | 2.1 | 2.89 | 5.39 | 1.81 | 1.57 |
| 1167.5 | 0.32 | 2.11 | 1.85 | 2.11 | 2.89 | 5.38 | 1.81 | 1.57 |
| 1168 | 0.32 | 2.11 | 1.85 | 2.11 | 2.89 | 5.38 | 1.81 | 1.57 |
| 1168.5 | 0.32 | 2.11 | 1.85 | 2.11 | 2.89 | 5.37 | 1.81 | 1.57 |
| 1169 | 0.32 | 2.11 | 1.86 | 2.11 | 2.89 | 5.37 | 1.82 | 1.57 |
| 1169.5 | 0.32 | 2.11 | 1.86 | 2.11 | 2.89 | 5.37 | 1.82 | 1.57 |
| 1170 | 0.32 | 2.12 | 1.86 | 2.12 | 2.89 | 5.38 | 1.82 | 1.57 |
| 1170.5 | 0.32 | 2.12 | 1.86 | 2.12 | 2.9 | 5.39 | 1.81 | 1.57 |
| 1171 | 0.33 | 2.12 | 1.86 | 2.12 | 2.89 | 5.4 | 1.81 | 1.57 |
| 1171.5 | 0.33 | 2.12 | 1.85 | 2.12 | 2.89 | 5.4 | 1.81 | 1.57 |
| 1172 | 0.33 | 2.12 | 1.85 | 2.12 | 2.88 | 5.4 | 1.81 | 1.57 |
| 1172.5 | 0.33 | 2.11 | 1.85 | 2.12 | 2.88 | 5.4 | 1.8 | 1.58 |
| 1173 | 0.33 | 2.11 | 1.85 | 2.11 | 2.88 | 5.4 | 1.81 | 1.58 |
| 1173.5 | 0.33 | 2.12 | 1.85 | 2.11 | 2.87 | 5.4 | 1.81 | 1.58 |
| 1174 | 0.33 | 2.12 | 1.85 | 2.11 | 2.87 | 5.4 | 1.81 | 1.58 |
| 1174.5 | 0.33 | 2.13 | 1.85 | 2.12 | 2.87 | 5.39 | 1.81 | 1.58 |
| 1175 | 0.33 | 2.13 | 1.85 | 2.12 | 2.87 | 5.39 | 1.81 | 1.58 |
| 1175.5 | 0.33 | 2.13 | 1.85 | 2.12 | 2.87 | 5.4 | 1.81 | 1.58 |
| 1176 | 0.33 | 2.13 | 1.85 | 2.11 | 2.87 | 5.4 | 1.81 | 1.58 |
| 1176.5 | 0.33 | 2.13 | 1.85 | 2.11 | 2.87 | 5.4 | 1.82 | 1.58 |
| 1177 | 0.33 | 2.12 | 1.85 | 2.11 | 2.86 | 5.39 | 1.82 | 1.57 |
| 1177.5 | 0.33 | 2.12 | 1.84 | 2.11 | 2.86 | 5.39 | 1.82 | 1.57 |
| 1178 | 0.34 | 2.11 | 1.84 | 2.11 | 2.86 | 5.38 | 1.82 | 1.57 |
| 1178.5 | 0.34 | 2.11 | 1.84 | 2.11 | 2.86 | 5.37 | 1.81 | 1.57 |
| 1179 | 0.34 | 2.11 | 1.84 | 2.11 | 2.86 | 5.37 | 1.81 | 1.57 |
| 1179.5 | 0.34 | 2.11 | 1.84 | 2.11 | 2.86 | 5.36 | 1.81 | 1.56 |
| 1180 | 0.34 | 2.11 | 1.85 | 2.11 | 2.86 | 5.37 | 1.81 | 1.57 |
| 1180.5 | 0.34 | 2.11 | 1.85 | 2.11 | 2.86 | 5.38 | 1.81 | 1.57 |
| 1181 | 0.34 | 2.11 | 1.85 | 2.11 | 2.87 | 5.4 | 1.81 | 1.57 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1181.5 | 0.34 | 2.11 | 1.85 | 2.11 | 2.87 | 5.41 | 1.81 | 1.57 |
| 1182 | 0.34 | 2.12 | 1.86 | 2.11 | 2.88 | 5.4 | 1.82 | 1.58 |
| 1182.5 | 0.34 | 2.12 | 1.86 | 2.11 | 2.88 | 5.39 | 1.82 | 1.57 |
| 1183 | 0.35 | 2.12 | 1.86 | 2.11 | 2.89 | 5.38 | 1.82 | 1.57 |
| 1183.5 | 0.35 | 2.12 | 1.86 | 2.11 | 2.89 | 5.36 | 1.82 | 1.57 |
| 1184 | 0.35 | 2.12 | 1.86 | 2.11 | 2.88 | 5.35 | 1.82 | 1.57 |
| 1184.5 | 0.35 | 2.11 | 1.86 | 2.11 | 2.88 | 5.35 | 1.82 | 1.57 |
| 1185 | 0.35 | 2.11 | 1.86 | 2.11 | 2.88 | 5.35 | 1.82 | 1.57 |
| 1185.5 | 0.35 | 2.12 | 1.86 | 2.11 | 2.88 | 5.36 | 1.82 | 1.58 |
| 1186 | 0.35 | 2.12 | 1.86 | 2.11 | 2.89 | 5.38 | 1.82 | 1.58 |
| 1186.5 | 0.35 | 2.12 | 1.86 | 2.11 | 2.89 | 5.4 | 1.82 | 1.58 |
| 1187 | 0.35 | 2.12 | 1.86 | 2.11 | 2.89 | 5.41 | 1.83 | 1.58 |
| 1187.5 | 0.36 | 2.12 | 1.86 | 2.11 | 2.88 | 5.42 | 1.83 | 1.58 |
| 1188 | 0.36 | 2.12 | 1.86 | 2.11 | 2.88 | 5.41 | 1.83 | 1.58 |
| 1188.5 | 0.36 | 2.12 | 1.86 | 2.11 | 2.88 | 5.4 | 1.83 | 1.58 |
| 1189 | 0.36 | 2.12 | 1.86 | 2.11 | 2.87 | 5.39 | 1.83 | 1.58 |
| 1189.5 | 0.36 | 2.12 | 1.85 | 2.11 | 2.87 | 5.39 | 1.83 | 1.58 |
| 1190 | 0.36 | 2.11 | 1.85 | 2.11 | 2.87 | 5.38 | 1.82 | 1.58 |
| 1190.5 | 0.36 | 2.11 | 1.85 | 2.12 | 2.87 | 5.38 | 1.82 | 1.57 |
| 1191 | 0.36 | 2.11 | 1.85 | 2.12 | 2.87 | 5.37 | 1.82 | 1.57 |
| 1191.5 | 0.36 | 2.11 | 1.85 | 2.12 | 2.86 | 5.36 | 1.82 | 1.57 |
| 1192 | 0.36 | 2.11 | 1.85 | 2.11 | 2.85 | 5.36 | 1.82 | 1.58 |
| 1192.5 | 0.37 | 2.11 | 1.85 | 2.11 | 2.85 | 5.36 | 1.82 | 1.58 |
| 1193 | 0.37 | 2.11 | 1.85 | 2.11 | 2.85 | 5.36 | 1.82 | 1.58 |
| 1193.5 | 0.37 | 2.11 | 1.85 | 2.11 | 2.86 | 5.36 | 1.82 | 1.58 |
| 1194 | 0.37 | 2.12 | 1.85 | 2.11 | 2.86 | 5.38 | 1.81 | 1.58 |
| 1194.5 | 0.37 | 2.12 | 1.85 | 2.12 | 2.87 | 5.39 | 1.81 | 1.58 |
| 1195 | 0.37 | 2.12 | 1.85 | 2.11 | 2.87 | 5.39 | 1.82 | 1.58 |
| 1195.5 | 0.37 | 2.12 | 1.85 | 2.11 | 2.87 | 5.39 | 1.82 | 1.58 |
| 1196 | 0.37 | 2.13 | 1.85 | 2.11 | 2.87 | 5.38 | 1.82 | 1.58 |
| 1196.5 | 0.37 | 2.13 | 1.85 | 2.11 | 2.87 | 5.37 | 1.82 | 1.58 |
| 1197 | 0.37 | 2.12 | 1.85 | 2.11 | 2.87 | 5.36 | 1.82 | 1.59 |
| 1197.5 | 0.37 | 2.12 | 1.85 | 2.11 | 2.86 | 5.35 | 1.82 | 1.59 |
| 1198 | 0.38 | 2.12 | 1.85 | 2.11 | 2.86 | 5.35 | 1.82 | 1.59 |
| 1198.5 | 0.38 | 2.12 | 1.85 | 2.1 | 2.86 | 5.35 | 1.82 | 1.59 |
| 1199 | 0.38 | 2.12 | 1.85 | 2.1 | 2.86 | 5.36 | 1.82 | 1.6 |
| 1199.5 | 0.38 | 2.12 | 1.85 | 2.11 | 2.86 | 5.37 | 1.82 | 1.6 |
| 1200 | 0.38 | 2.12 | 1.85 | 2.11 | 2.86 | 5.38 | 1.82 | 1.59 |
| 1200.5 | 0.38 | 2.12 | 1.85 | 2.11 | 2.86 | 5.38 | 1.82 | 1.59 |
| 1201 | 0.38 | 2.12 | 1.85 | 2.11 | 2.85 | 5.37 | 1.82 | 1.59 |
| 1201.5 | 0.38 | 2.12 | 1.85 | 2.11 | 2.84 | 5.37 | 1.81 | 1.58 |
| 1202 | 0.38 | 2.12 | 1.85 | 2.11 | 2.84 | 5.36 | 1.81 | 1.58 |
| 1202.5 | 0.38 | 2.12 | 1.85 | 2.11 | 2.84 | 5.36 | 1.8 | 1.58 |
| 1203 | 0.38 | 2.11 | 1.85 | 2.11 | 2.84 | 5.36 | 1.8 | 1.58 |
| 1203.5 | 0.38 | 2.11 | 1.84 | 2.11 | 2.85 | 5.36 | 1.81 | 1.58 |
| 1204 | 0.38 | 2.1 | 1.84 | 2.11 | 2.85 | 5.36 | 1.81 | 1.58 |
| 1204.5 | 0.38 | 2.1 | 1.84 | 2.11 | 2.85 | 5.36 | 1.81 | 1.58 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1205 | 0.38 | 2.11 | 1.85 | 2.11 | 2.84 | 5.34 | 1.82 | 1.58 |
| 1205.5 | 0.38 | 2.11 | 1.85 | 2.11 | 2.83 | 5.33 | 1.82 | 1.58 |
| 1206 | 0.38 | 2.11 | 1.85 | 2.1 | 2.83 | 5.32 | 1.82 | 1.58 |
| 1206.5 | 0.38 | 2.11 | 1.85 | 2.1 | 2.83 | 5.31 | 1.82 | 1.58 |
| 1207 | 0.38 | 2.11 | 1.85 | 2.1 | 2.83 | 5.31 | 1.81 | 1.58 |
| 1207.5 | 0.38 | 2.1 | 1.84 | 2.09 | 2.84 | 5.31 | 1.81 | 1.57 |
| 1208 | 0.38 | 2.1 | 1.84 | 2.09 | 2.85 | 5.32 | 1.8 | 1.57 |
| 1208.5 | 0.38 | 2.1 | 1.84 | 2.08 | 2.85 | 5.32 | 1.8 | 1.57 |
| 1209 | 0.37 | 2.1 | 1.84 | 2.08 | 2.84 | 5.32 | 1.8 | 1.57 |
| 1209.5 | 0.37 | 2.1 | 1.84 | 2.08 | 2.83 | 5.32 | 1.8 | 1.57 |
| 1210 | 0.37 | 2.1 | 1.84 | 2.08 | 2.82 | 5.33 | 1.81 | 1.57 |
| 1210.5 | 0.37 | 2.09 | 1.84 | 2.08 | 2.81 | 5.34 | 1.81 | 1.57 |
| 1211 | 0.37 | 2.09 | 1.84 | 2.08 | 2.81 | 5.35 | 1.81 | 1.57 |
| 1211.5 | 0.37 | 2.09 | 1.84 | 2.08 | 2.81 | 5.35 | 1.81 | 1.57 |
| 1212 | 0.37 | 2.09 | 1.84 | 2.08 | 2.82 | 5.35 | 1.81 | 1.56 |
| 1212.5 | 0.36 | 2.09 | 1.84 | 2.08 | 2.82 | 5.34 | 1.8 | 1.56 |
| 1213 | 0.36 | 2.09 | 1.84 | 2.08 | 2.82 | 5.33 | 1.8 | 1.56 |
| 1213.5 | 0.36 | 2.09 | 1.83 | 2.08 | 2.81 | 5.31 | 1.79 | 1.56 |
| 1214 | 0.36 | 2.09 | 1.83 | 2.07 | 2.81 | 5.3 | 1.79 | 1.56 |
| 1214.5 | 0.36 | 2.08 | 1.83 | 2.07 | 2.82 | 5.31 | 1.79 | 1.56 |
| 1215 | 0.36 | 2.08 | 1.83 | 2.07 | 2.82 | 5.31 | 1.79 | 1.56 |
| 1215.5 | 0.36 | 2.08 | 1.83 | 2.07 | 2.82 | 5.32 | 1.79 | 1.56 |
| 1216 | 0.36 | 2.08 | 1.83 | 2.07 | 2.82 | 5.33 | 1.79 | 1.56 |
| 1216.5 | 0.36 | 2.08 | 1.83 | 2.07 | 2.82 | 5.32 | 1.79 | 1.56 |
| 1217 | 0.36 | 2.08 | 1.83 | 2.07 | 2.81 | 5.31 | 1.78 | 1.56 |
| 1217.5 | 0.35 | 2.09 | 1.83 | 2.07 | 2.81 | 5.3 | 1.78 | 1.56 |
| 1218 | 0.35 | 2.09 | 1.83 | 2.07 | 2.8 | 5.3 | 1.78 | 1.56 |
| 1218.5 | 0.35 | 2.09 | 1.82 | 2.07 | 2.8 | 5.3 | 1.78 | 1.56 |
| 1219 | 0.35 | 2.08 | 1.82 | 2.07 | 2.8 | 5.3 | 1.78 | 1.56 |
| 1219.5 | 0.35 | 2.08 | 1.82 | 2.07 | 2.79 | 5.29 | 1.78 | 1.56 |
| 1220 | 0.35 | 2.07 | 1.81 | 2.06 | 2.79 | 5.28 | 1.78 | 1.56 |
| 1220.5 | 0.34 | 2.07 | 1.81 | 2.06 | 2.79 | 5.27 | 1.77 | 1.55 |
| 1221 | 0.34 | 2.07 | 1.81 | 2.06 | 2.79 | 5.27 | 1.77 | 1.55 |
| 1221.5 | 0.34 | 2.07 | 1.81 | 2.06 | 2.79 | 5.28 | 1.77 | 1.55 |
| 1222 | 0.34 | 2.07 | 1.81 | 2.06 | 2.79 | 5.29 | 1.77 | 1.55 |
| 1222.5 | 0.34 | 2.07 | 1.81 | 2.06 | 2.8 | 5.3 | 1.77 | 1.54 |
| 1223 | 0.34 | 2.07 | 1.8 | 2.06 | 2.8 | 5.3 | 1.77 | 1.54 |
| 1223.5 | 0.34 | 2.06 | 1.8 | 2.06 | 2.8 | 5.28 | 1.77 | 1.54 |
| 1224 | 0.34 | 2.06 | 1.8 | 2.06 | 2.8 | 5.26 | 1.77 | 1.54 |
| 1224.5 | 0.34 | 2.06 | 1.8 | 2.05 | 2.79 | 5.24 | 1.77 | 1.54 |
| 1225 | 0.34 | 2.06 | 1.81 | 2.05 | 2.79 | 5.23 | 1.77 | 1.54 |
| 1225.5 | 0.34 | 2.06 | 1.81 | 2.06 | 2.79 | 5.23 | 1.77 | 1.54 |
| 1226 | 0.34 | 2.06 | 1.81 | 2.06 | 2.79 | 5.24 | 1.77 | 1.54 |
| 1226.5 | 0.34 | 2.06 | 1.81 | 2.06 | 2.79 | 5.24 | 1.77 | 1.54 |
| 1227 | 0.34 | 2.06 | 1.8 | 2.05 | 2.78 | 5.25 | 1.76 | 1.54 |
| 1227.5 | 0.34 | 2.06 | 1.8 | 2.05 | 2.78 | 5.26 | 1.76 | 1.54 |
| 1228 | 0.34 | 2.06 | 1.8 | 2.05 | 2.78 | 5.26 | 1.76 | 1.53 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1228.5 | 0.34 | 2.07 | 1.79 | 2.05 | 2.77 | 5.25 | 1.76 | 1.53 |
| 1229 | 0.33 | 2.07 | 1.79 | 2.05 | 2.77 | 5.25 | 1.75 | 1.53 |
| 1229.5 | 0.33 | 2.06 | 1.79 | 2.05 | 2.77 | 5.24 | 1.76 | 1.53 |
| 1230 | 0.33 | 2.06 | 1.79 | 2.05 | 2.77 | 5.23 | 1.76 | 1.53 |
| 1230.5 | 0.33 | 2.06 | 1.79 | 2.05 | 2.77 | 5.23 | 1.76 | 1.53 |
| 1231 | 0.33 | 2.05 | 1.79 | 2.05 | 2.77 | 5.23 | 1.76 | 1.53 |
| 1231.5 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.24 | 1.76 | 1.53 |
| 1232 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.25 | 1.75 | 1.53 |
| 1232.5 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.25 | 1.75 | 1.54 |
| 1233 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.25 | 1.75 | 1.54 |
| 1233.5 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.25 | 1.75 | 1.53 |
| 1234 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.23 | 1.75 | 1.53 |
| 1234.5 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.22 | 1.74 | 1.53 |
| 1235 | 0.33 | 2.05 | 1.79 | 2.04 | 2.76 | 5.22 | 1.74 | 1.53 |
| 1235.5 | 0.33 | 2.05 | 1.79 | 2.04 | 2.77 | 5.22 | 1.74 | 1.53 |
| 1236 | 0.33 | 2.05 | 1.79 | 2.04 | 2.77 | 5.23 | 1.75 | 1.53 |
| 1236.5 | 0.33 | 2.05 | 1.79 | 2.04 | 2.77 | 5.23 | 1.75 | 1.54 |
| 1237 | 0.33 | 2.05 | 1.79 | 2.03 | 2.77 | 5.24 | 1.74 | 1.53 |
| 1237.5 | 0.33 | 2.05 | 1.78 | 2.03 | 2.76 | 5.23 | 1.74 | 1.53 |
| 1238 | 0.33 | 2.05 | 1.78 | 2.03 | 2.76 | 5.23 | 1.74 | 1.53 |
| 1238.5 | 0.33 | 2.04 | 1.78 | 2.03 | 2.75 | 5.22 | 1.74 | 1.53 |
| 1239 | 0.33 | 2.04 | 1.78 | 2.04 | 2.75 | 5.22 | 1.74 | 1.53 |
| 1239.5 | 0.32 | 2.03 | 1.78 | 2.04 | 2.74 | 5.22 | 1.74 | 1.53 |
| 1240 | 0.32 | 2.03 | 1.78 | 2.03 | 2.74 | 5.21 | 1.74 | 1.52 |
| 1240.5 | 0.32 | 2.03 | 1.78 | 2.03 | 2.74 | 5.21 | 1.74 | 1.52 |
| 1241 | 0.32 | 2.03 | 1.78 | 2.02 | 2.74 | 5.22 | 1.74 | 1.52 |
| 1241.5 | 0.32 | 2.03 | 1.78 | 2.02 | 2.74 | 5.22 | 1.74 | 1.52 |
| 1242 | 0.32 | 2.03 | 1.78 | 2.02 | 2.75 | 5.22 | 1.74 | 1.52 |
| 1242.5 | 0.32 | 2.04 | 1.78 | 2.02 | 2.74 | 5.21 | 1.73 | 1.52 |
| 1243 | 0.32 | 2.04 | 1.78 | 2.02 | 2.74 | 5.19 | 1.73 | 1.52 |
| 1243.5 | 0.32 | 2.04 | 1.77 | 2.02 | 2.74 | 5.18 | 1.73 | 1.53 |
| 1244 | 0.32 | 2.04 | 1.77 | 2.02 | 2.75 | 5.17 | 1.73 | 1.53 |
| 1244.5 | 0.32 | 2.03 | 1.77 | 2.02 | 2.75 | 5.17 | 1.73 | 1.52 |
| 1245 | 0.32 | 2.03 | 1.77 | 2.02 | 2.75 | 5.16 | 1.73 | 1.52 |
| 1245.5 | 0.32 | 2.03 | 1.77 | 2.01 | 2.75 | 5.16 | 1.72 | 1.52 |
| 1246 | 0.32 | 2.03 | 1.76 | 2.01 | 2.74 | 5.17 | 1.72 | 1.52 |
| 1246.5 | 0.32 | 2.02 | 1.76 | 2.01 | 2.74 | 5.17 | 1.72 | 1.52 |
| 1247 | 0.32 | 2.02 | 1.76 | 2.01 | 2.74 | 5.18 | 1.72 | 1.52 |
| 1247.5 | 0.31 | 2.02 | 1.76 | 2.01 | 2.73 | 5.18 | 1.72 | 1.51 |
| 1248 | 0.31 | 2.02 | 1.76 | 2.01 | 2.73 | 5.16 | 1.72 | 1.51 |
| 1248.5 | 0.31 | 2.02 | 1.76 | 2.01 | 2.73 | 5.15 | 1.72 | 1.51 |
| 1249 | 0.31 | 2.02 | 1.76 | 2.01 | 2.72 | 5.14 | 1.72 | 1.51 |
| 1249.5 | 0.31 | 2.02 | 1.76 | 2.01 | 2.73 | 5.14 | 1.72 | 1.51 |
| 1250 | 0.31 | 2.02 | 1.76 | 2.01 | 2.73 | 5.15 | 1.72 | 1.51 |
| 1250.5 | 0.31 | 2.01 | 1.76 | 2.01 | 2.73 | 5.16 | 1.73 | 1.51 |
| 1251 | 0.31 | 2.01 | 1.75 | 2.01 | 2.73 | 5.16 | 1.73 | 1.51 |
| 1251.5 | 0.31 | 2.01 | 1.75 | 2 | 2.73 | 5.16 | 1.73 | 1.51 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1252 | 0.35 | 2.02 | 1.75 | 2 | 2.72 | 5.16 | 1.72 | 1.51 |
| 1252.5 | 0.35 | 2.02 | 1.75 | 2 | 2.72 | 5.16 | 1.72 | 1.51 |
| 1253 | 0.35 | 2.02 | 1.75 | 2.01 | 2.72 | 5.15 | 1.72 | 1.51 |
| 1253.5 | 0.35 | 2.02 | 1.75 | 2.01 | 2.72 | 5.15 | 1.72 | 1.51 |
| 1254 | 0.35 | 2.01 | 1.75 | 2.01 | 2.72 | 5.15 | 1.72 | 1.5 |
| 1254.5 | 0.35 | 2.01 | 1.76 | 2.01 | 2.72 | 5.15 | 1.72 | 1.5 |
| 1255 | 0.35 | 2.01 | 1.76 | 2.01 | 2.72 | 5.15 | 1.72 | 1.5 |
| 1255.5 | 0.35 | 2.01 | 1.76 | 2.01 | 2.72 | 5.15 | 1.71 | 1.5 |
| 1256 | 0.35 | 2.01 | 1.76 | 2.01 | 2.72 | 5.14 | 1.72 | 1.5 |
| 1256.5 | 0.35 | 2.01 | 1.75 | 2.01 | 2.71 | 5.13 | 1.71 | 1.5 |
| 1257 | 0.35 | 2.01 | 1.75 | 2 | 2.71 | 5.13 | 1.71 | 1.5 |
| 1257.5 | 0.35 | 2.01 | 1.75 | 2 | 2.71 | 5.13 | 1.71 | 1.5 |
| 1258 | 0.35 | 2.01 | 1.75 | 2 | 2.7 | 5.13 | 1.71 | 1.5 |
| 1258.5 | 0.35 | 2.01 | 1.75 | 2 | 2.7 | 5.14 | 1.71 | 1.5 |
| 1259 | 0.35 | 2.02 | 1.75 | 1.99 | 2.7 | 5.15 | 1.71 | 1.51 |
| 1259.5 | 0.35 | 2.02 | 1.75 | 1.99 | 2.7 | 5.16 | 1.71 | 1.51 |
| 1260 | 0.35 | 2.02 | 1.75 | 1.99 | 2.7 | 5.17 | 1.71 | 1.51 |
| 1260.5 | 0.35 | 2.02 | 1.74 | 1.99 | 2.7 | 5.17 | 1.71 | 1.5 |
| 1261 | 0.35 | 2.01 | 1.74 | 1.99 | 2.7 | 5.16 | 1.7 | 1.5 |
| 1261.5 | 0.35 | 2.01 | 1.74 | 1.99 | 2.7 | 5.16 | 1.7 | 1.5 |
| 1262 | 0.35 | 2.01 | 1.74 | 2 | 2.7 | 5.16 | 1.7 | 1.5 |
| 1262.5 | 0.35 | 2 | 1.74 | 2 | 2.71 | 5.16 | 1.7 | 1.5 |
| 1263 | 0.35 | 2 | 1.74 | 1.99 | 2.71 | 5.17 | 1.71 | 1.5 |
| 1263.5 | 0.35 | 2 | 1.74 | 1.99 | 2.71 | 5.17 | 1.71 | 1.5 |
| 1264 | 0.35 | 2 | 1.74 | 1.99 | 2.7 | 5.16 | 1.71 | 1.5 |
| 1264.5 | 0.35 | 2 | 1.74 | 1.99 | 2.7 | 5.15 | 1.71 | 1.5 |
| 1265 | 0.35 | 2 | 1.74 | 1.99 | 2.7 | 5.14 | 1.7 | 1.5 |
| 1265.5 | 0.35 | 2 | 1.74 | 1.99 | 2.7 | 5.12 | 1.7 | 1.5 |
| 1266 | 0.35 | 2 | 1.74 | 1.99 | 2.7 | 5.12 | 1.7 | 1.5 |
| 1266.5 | 0.35 | 2 | 1.74 | 1.99 | 2.7 | 5.12 | 1.7 | 1.5 |
| 1267 | 0.35 | 2 | 1.75 | 1.99 | 2.69 | 5.12 | 1.7 | 1.5 |
| 1267.5 | 0.35 | 2 | 1.75 | 1.99 | 2.69 | 5.13 | 1.7 | 1.5 |
| 1268 | 0.35 | 2 | 1.75 | 1.99 | 2.69 | 5.13 | 1.7 | 1.5 |
| 1268.5 | 0.35 | 2 | 1.75 | 1.98 | 2.69 | 5.13 | 1.7 | 1.5 |
| 1269 | 0.35 | 2 | 1.74 | 1.98 | 2.69 | 5.12 | 1.7 | 1.5 |
| 1269.5 | 0.35 | 1.99 | 1.74 | 1.98 | 2.69 | 5.11 | 1.7 | 1.5 |
| 1270 | 0.35 | 1.99 | 1.74 | 1.98 | 2.68 | 5.11 | 1.7 | 1.5 |
| 1270.5 | 0.35 | 1.99 | 1.74 | 1.98 | 2.68 | 5.11 | 1.7 | 1.5 |
| 1271 | 0.35 | 1.99 | 1.74 | 1.98 | 2.68 | 5.11 | 1.7 | 1.5 |
| 1271.5 | 0.35 | 1.99 | 1.74 | 1.98 | 2.68 | 5.12 | 1.7 | 1.5 |
| 1272 | 0.35 | 1.99 | 1.74 | 1.98 | 2.68 | 5.12 | 1.7 | 1.5 |
| 1272.5 | 0.35 | 1.99 | 1.74 | 1.98 | 2.68 | 5.13 | 1.7 | 1.49 |
| 1273 | 0.35 | 1.99 | 1.74 | 1.98 | 2.68 | 5.13 | 1.69 | 1.49 |
| 1273.5 | 0.35 | 1.99 | 1.73 | 1.98 | 2.68 | 5.13 | 1.7 | 1.49 |
| 1274 | 0.35 | 1.99 | 1.73 | 1.98 | 2.69 | 5.12 | 1.7 | 1.49 |
| 1274.5 | 0.35 | 1.99 | 1.73 | 1.98 | 2.69 | 5.12 | 1.69 | 1.49 |
| 1275 | 0.35 | 1.99 | 1.73 | 1.98 | 2.69 | 5.11 | 1.69 | 1.49 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1275.5 | 0.35 | 1.99 | 1.73 | 1.97 | 2.69 | 5.11 | 1.69 | 1.49 |
| 1276 | 0.35 | 1.98 | 1.74 | 1.97 | 2.69 | 5.11 | 1.69 | 1.49 |
| 1276.5 | 0.35 | 1.98 | 1.74 | 1.97 | 2.69 | 5.11 | 1.69 | 1.49 |
| 1277 | 0.35 | 1.98 | 1.73 | 1.97 | 2.68 | 5.11 | 1.69 | 1.49 |
| 1277.5 | 0.35 | 1.98 | 1.73 | 1.97 | 2.68 | 5.1 | 1.69 | 1.49 |
| 1278 | 0.35 | 1.99 | 1.73 | 1.97 | 2.68 | 5.09 | 1.69 | 1.49 |
| 1278.5 | 0.35 | 1.99 | 1.73 | 1.97 | 2.68 | 5.09 | 1.69 | 1.49 |
| 1279 | 0.35 | 1.99 | 1.73 | 1.97 | 2.68 | 5.08 | 1.69 | 1.49 |
| 1279.5 | 0.35 | 1.99 | 1.73 | 1.97 | 2.68 | 5.08 | 1.69 | 1.49 |
| 1280 | 0.35 | 1.99 | 1.73 | 1.97 | 2.68 | 5.08 | 1.69 | 1.49 |
| 1280.5 | 0.35 | 1.99 | 1.72 | 1.97 | 2.68 | 5.07 | 1.69 | 1.49 |
| 1281 | 0.35 | 1.99 | 1.72 | 1.97 | 2.68 | 5.07 | 1.69 | 1.49 |
| 1281.5 | 0.35 | 1.98 | 1.72 | 1.97 | 2.67 | 5.06 | 1.69 | 1.49 |
| 1282 | 0.35 | 1.98 | 1.72 | 1.96 | 2.67 | 5.06 | 1.69 | 1.49 |
| 1282.5 | 0.35 | 1.98 | 1.72 | 1.96 | 2.67 | 5.06 | 1.69 | 1.48 |
| 1283 | 0.35 | 1.97 | 1.72 | 1.96 | 2.67 | 5.06 | 1.69 | 1.48 |
| 1283.5 | 0.35 | 1.97 | 1.72 | 1.96 | 2.67 | 5.06 | 1.68 | 1.48 |
| 1284 | 0.35 | 1.97 | 1.72 | 1.96 | 2.66 | 5.06 | 1.68 | 1.48 |
| 1284.5 | 0.35 | 1.97 | 1.72 | 1.96 | 2.66 | 5.06 | 1.68 | 1.48 |
| 1285 | 0.35 | 1.97 | 1.72 | 1.96 | 2.66 | 5.06 | 1.68 | 1.48 |
| 1285.5 | 0.35 | 1.97 | 1.72 | 1.96 | 2.66 | 5.06 | 1.68 | 1.48 |
| 1286 | 0.35 | 1.97 | 1.72 | 1.96 | 2.66 | 5.05 | 1.68 | 1.48 |
| 1286.5 | 0.35 | 1.97 | 1.72 | 1.96 | 2.66 | 5.05 | 1.67 | 1.48 |
| 1287 | 0.36 | 1.97 | 1.72 | 1.96 | 2.65 | 5.05 | 1.67 | 1.48 |
| 1287.5 | 0.36 | 1.97 | 1.71 | 1.96 | 2.65 | 5.06 | 1.67 | 1.48 |
| 1288 | 0.36 | 1.97 | 1.71 | 1.96 | 2.65 | 5.06 | 1.67 | 1.48 |
| 1288.5 | 0.36 | 1.97 | 1.71 | 1.96 | 2.65 | 5.06 | 1.67 | 1.48 |
| 1289 | 0.36 | 1.97 | 1.71 | 1.95 | 2.64 | 5.05 | 1.68 | 1.48 |
| 1289.5 | 0.36 | 1.97 | 1.71 | 1.95 | 2.64 | 5.05 | 1.68 | 1.48 |
| 1290 | 0.36 | 1.96 | 1.71 | 1.95 | 2.64 | 5.06 | 1.67 | 1.48 |
| 1290.5 | 0.36 | 1.96 | 1.71 | 1.95 | 2.64 | 5.06 | 1.67 | 1.48 |
| 1291 | 0.36 | 1.96 | 1.71 | 1.95 | 2.64 | 5.06 | 1.67 | 1.48 |
| 1291.5 | 0.36 | 1.97 | 1.71 | 1.95 | 2.64 | 5.06 | 1.68 | 1.48 |
| 1292 | 0.36 | 1.97 | 1.72 | 1.95 | 2.65 | 5.06 | 1.68 | 1.48 |
| 1292.5 | 0.36 | 1.97 | 1.72 | 1.94 | 2.65 | 5.05 | 1.68 | 1.48 |
| 1293 | 0.36 | 1.97 | 1.72 | 1.94 | 2.64 | 5.04 | 1.68 | 1.48 |
| 1293.5 | 0.36 | 1.96 | 1.71 | 1.94 | 2.64 | 5.03 | 1.68 | 1.47 |
| 1294 | 0.36 | 1.96 | 1.71 | 1.94 | 2.64 | 5.02 | 1.67 | 1.47 |
| 1294.5 | 0.36 | 1.96 | 1.71 | 1.95 | 2.63 | 5.02 | 1.67 | 1.47 |
| 1295 | 0.36 | 1.96 | 1.7 | 1.95 | 2.63 | 5.02 | 1.67 | 1.47 |
| 1295.5 | 0.36 | 1.96 | 1.7 | 1.95 | 2.63 | 5.02 | 1.67 | 1.47 |
| 1296 | 0.36 | 1.96 | 1.7 | 1.95 | 2.63 | 5.02 | 1.66 | 1.47 |
| 1296.5 | 0.36 | 1.96 | 1.7 | 1.95 | 2.63 | 5.02 | 1.66 | 1.47 |
| 1297 | 0.36 | 1.95 | 1.7 | 1.95 | 2.63 | 5.01 | 1.67 | 1.47 |
| 1297.5 | 0.36 | 1.95 | 1.7 | 1.95 | 2.63 | 5.01 | 1.67 | 1.47 |
| 1298 | 0.36 | 1.95 | 1.7 | 1.94 | 2.63 | 5.01 | 1.67 | 1.47 |
| 1298.5 | 0.36 | 1.95 | 1.7 | 1.94 | 2.63 | 5.02 | 1.67 | 1.47 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1299 | 0.36 | 1.95 | 1.7 | 1.94 | 2.63 | 5.02 | 1.67 | 1.47 |
| 1299.5 | 0.36 | 1.96 | 1.7 | 1.94 | 2.62 | 5.03 | 1.67 | 1.47 |
| 1300 | 0.36 | 1.96 | 1.69 | 1.94 | 2.62 | 5.03 | 1.66 | 1.47 |
| 1300.5 | 0.36 | 1.96 | 1.69 | 1.94 | 2.63 | 5.03 | 1.66 | 1.47 |
| 1301 | 0.36 | 1.96 | 1.69 | 1.94 | 2.63 | 5.03 | 1.66 | 1.47 |
| 1301.5 | 0.36 | 1.96 | 1.69 | 1.94 | 2.63 | 5.03 | 1.66 | 1.47 |
| 1302 | 0.36 | 1.96 | 1.7 | 1.94 | 2.63 | 5.03 | 1.66 | 1.47 |
| 1302.5 | 0.36 | 1.96 | 1.7 | 1.94 | 2.63 | 5.04 | 1.66 | 1.47 |
| 1303 | 0.36 | 1.96 | 1.7 | 1.94 | 2.63 | 5.05 | 1.66 | 1.47 |
| 1303.5 | 0.36 | 1.96 | 1.7 | 1.94 | 2.63 | 5.05 | 1.66 | 1.47 |
| 1304 | 0.36 | 1.96 | 1.7 | 1.94 | 2.63 | 5.05 | 1.66 | 1.47 |
| 1304.5 | 0.36 | 1.96 | 1.7 | 1.94 | 2.63 | 5.05 | 1.66 | 1.47 |
| 1305 | 0.36 | 1.96 | 1.7 | 1.94 | 2.62 | 5.05 | 1.66 | 1.47 |
| 1305.5 | 0.36 | 1.96 | 1.7 | 1.94 | 2.62 | 5.04 | 1.66 | 1.47 |
| 1306 | 0.36 | 1.95 | 1.7 | 1.93 | 2.61 | 5.03 | 1.66 | 1.47 |
| 1306.5 | 0.36 | 1.95 | 1.69 | 1.93 | 2.61 | 5.03 | 1.66 | 1.47 |
| 1307 | 0.36 | 1.95 | 1.69 | 1.93 | 2.61 | 5.02 | 1.66 | 1.47 |
| 1307.5 | 0.36 | 1.95 | 1.69 | 1.93 | 2.61 | 5.02 | 1.66 | 1.47 |
| 1308 | 0.36 | 1.95 | 1.69 | 1.93 | 2.62 | 5.01 | 1.66 | 1.47 |
| 1308.5 | 0.36 | 1.94 | 1.69 | 1.93 | 2.61 | 5.01 | 1.66 | 1.47 |
| 1309 | 0.36 | 1.94 | 1.69 | 1.93 | 2.61 | 5.01 | 1.66 | 1.47 |
| 1309.5 | 0.36 | 1.94 | 1.69 | 1.93 | 2.61 | 5.01 | 1.65 | 1.47 |
| 1310 | 0.36 | 1.94 | 1.69 | 1.93 | 2.61 | 5.02 | 1.65 | 1.47 |
| 1310.5 | 0.36 | 1.94 | 1.69 | 1.92 | 2.61 | 5.02 | 1.65 | 1.47 |
| 1311 | 0.36 | 1.94 | 1.7 | 1.92 | 2.61 | 5.02 | 1.65 | 1.46 |
| 1311.5 | 0.36 | 1.94 | 1.69 | 1.92 | 2.61 | 5.01 | 1.65 | 1.46 |
| 1312 | 0.36 | 1.94 | 1.69 | 1.92 | 2.61 | 5.01 | 1.65 | 1.46 |
| 1312.5 | 0.36 | 1.94 | 1.69 | 1.92 | 2.61 | 5 | 1.65 | 1.46 |
| 1313 | 0.36 | 1.94 | 1.69 | 1.92 | 2.61 | 5 | 1.65 | 1.46 |
| 1313.5 | 0.36 | 1.94 | 1.69 | 1.93 | 2.61 | 4.99 | 1.65 | 1.46 |
| 1314 | 0.36 | 1.94 | 1.69 | 1.92 | 2.61 | 4.99 | 1.65 | 1.46 |
| 1314.5 | 0.36 | 1.93 | 1.68 | 1.92 | 2.61 | 4.99 | 1.65 | 1.46 |
| 1315 | 0.36 | 1.93 | 1.68 | 1.92 | 2.6 | 4.99 | 1.65 | 1.46 |
| 1315.5 | 0.36 | 1.93 | 1.68 | 1.92 | 2.6 | 5 | 1.65 | 1.46 |
| 1316 | 0.36 | 1.93 | 1.68 | 1.92 | 2.6 | 5.01 | 1.65 | 1.46 |
| 1316.5 | 0.36 | 1.93 | 1.68 | 1.92 | 2.61 | 5.01 | 1.65 | 1.46 |
| 1317 | 0.36 | 1.93 | 1.68 | 1.92 | 2.61 | 5.01 | 1.65 | 1.46 |
| 1317.5 | 0.36 | 1.93 | 1.68 | 1.92 | 2.61 | 5 | 1.65 | 1.46 |
| 1318 | 0.36 | 1.94 | 1.68 | 1.92 | 2.6 | 4.99 | 1.65 | 1.46 |
| 1318.5 | 0.36 | 1.94 | 1.68 | 1.91 | 2.6 | 4.98 | 1.65 | 1.46 |
| 1319 | 0.36 | 1.94 | 1.68 | 1.91 | 2.6 | 4.98 | 1.65 | 1.46 |
| 1319.5 | 0.36 | 1.94 | 1.68 | 1.91 | 2.6 | 4.98 | 1.65 | 1.46 |
| 1320 | 0.36 | 1.94 | 1.68 | 1.91 | 2.6 | 4.98 | 1.65 | 1.46 |
| 1320.5 | 0.36 | 1.94 | 1.68 | 1.91 | 2.6 | 4.98 | 1.65 | 1.46 |
| 1321 | 0.36 | 1.94 | 1.68 | 1.91 | 2.6 | 4.98 | 1.65 | 1.46 |
| 1321.5 | 0.36 | 1.93 | 1.68 | 1.91 | 2.6 | 4.98 | 1.65 | 1.46 |
| 1322 | 0.36 | 1.93 | 1.68 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1322.5 | 0.36 | 1.93 | 1.68 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1323 | 0.36 | 1.93 | 1.67 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1323.5 | 0.36 | 1.93 | 1.67 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1324 | 0.36 | 1.93 | 1.67 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1324.5 | 0.36 | 1.93 | 1.67 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1325 | 0.36 | 1.93 | 1.67 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1325.5 | 0.36 | 1.93 | 1.67 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1326 | 0.36 | 1.93 | 1.68 | 1.91 | 2.59 | 4.98 | 1.64 | 1.46 |
| 1326.5 | 0.36 | 1.93 | 1.68 | 1.91 | 2.59 | 4.97 | 1.64 | 1.46 |
| 1327 | 0.36 | 1.93 | 1.68 | 1.91 | 2.59 | 4.97 | 1.64 | 1.45 |
| 1327.5 | 0.36 | 1.93 | 1.68 | 1.91 | 2.59 | 4.96 | 1.64 | 1.45 |
| 1328 | 0.36 | 1.93 | 1.68 | 1.91 | 2.59 | 4.96 | 1.64 | 1.45 |
| 1328.5 | 0.37 | 1.93 | 1.68 | 1.91 | 2.59 | 4.96 | 1.64 | 1.45 |
| 1329 | 0.37 | 1.92 | 1.67 | 1.91 | 2.58 | 4.96 | 1.64 | 1.45 |
| 1329.5 | 0.37 | 1.92 | 1.67 | 1.91 | 2.58 | 4.96 | 1.64 | 1.45 |
| 1330 | 0.37 | 1.92 | 1.67 | 1.91 | 2.58 | 4.95 | 1.64 | 1.46 |
| 1330.5 | 0.37 | 1.92 | 1.67 | 1.91 | 2.58 | 4.95 | 1.64 | 1.46 |
| 1331 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.94 | 1.63 | 1.46 |
| 1331.5 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.94 | 1.63 | 1.46 |
| 1332 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.94 | 1.63 | 1.46 |
| 1332.5 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.94 | 1.63 | 1.46 |
| 1333 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.94 | 1.63 | 1.46 |
| 1333.5 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.94 | 1.63 | 1.46 |
| 1334 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.94 | 1.63 | 1.46 |
| 1334.5 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1335 | 0.37 | 1.92 | 1.67 | 1.9 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1335.5 | 0.37 | 1.92 | 1.66 | 1.9 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1336 | 0.37 | 1.92 | 1.66 | 1.9 | 2.57 | 4.96 | 1.63 | 1.45 |
| 1336.5 | 0.37 | 1.92 | 1.66 | 1.9 | 2.57 | 4.96 | 1.63 | 1.45 |
| 1337 | 0.37 | 1.91 | 1.66 | 1.9 | 2.57 | 4.96 | 1.63 | 1.45 |
| 1337.5 | 0.37 | 1.91 | 1.66 | 1.9 | 2.57 | 4.96 | 1.63 | 1.45 |
| 1338 | 0.37 | 1.91 | 1.66 | 1.9 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1338.5 | 0.37 | 1.91 | 1.66 | 1.9 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1339 | 0.37 | 1.91 | 1.66 | 1.9 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1339.5 | 0.37 | 1.91 | 1.66 | 1.9 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1340 | 0.37 | 1.91 | 1.66 | 1.89 | 2.57 | 4.95 | 1.63 | 1.45 |
| 1340.5 | 0.37 | 1.91 | 1.66 | 1.89 | 2.57 | 4.96 | 1.63 | 1.45 |
| 1341 | 0.37 | 1.92 | 1.66 | 1.89 | 2.56 | 4.96 | 1.63 | 1.45 |
| 1341.5 | 0.37 | 1.92 | 1.66 | 1.89 | 2.56 | 4.97 | 1.63 | 1.45 |
| 1342 | 0.37 | 1.91 | 1.66 | 1.89 | 2.56 | 4.97 | 1.63 | 1.45 |
| 1342.5 | 0.37 | 1.91 | 1.66 | 1.89 | 2.56 | 4.97 | 1.63 | 1.45 |
| 1343 | 0.37 | 1.91 | 1.66 | 1.89 | 2.56 | 4.96 | 1.63 | 1.45 |
| 1343.5 | 0.37 | 1.91 | 1.66 | 1.89 | 2.56 | 4.95 | 1.63 | 1.45 |
| 1344 | 0.37 | 1.91 | 1.66 | 1.89 | 2.56 | 4.94 | 1.62 | 1.45 |
| 1344.5 | 0.37 | 1.91 | 1.66 | 1.89 | 2.56 | 4.93 | 1.62 | 1.45 |
| 1345 | 0.37 | 1.91 | 1.66 | 1.89 | 2.55 | 4.92 | 1.62 | 1.45 |
| 1345.5 | 0.37 | 1.9 | 1.66 | 1.89 | 2.55 | 4.91 | 1.62 | 1.45 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1346 | 0.37 | 1.9 | 1.66 | 1.89 | 2.55 | 4.91 | 1.62 | 1.45 |
| 1346.5 | 0.37 | 1.9 | 1.66 | 1.89 | 2.55 | 4.91 | 1.62 | 1.45 |
| 1347 | 0.37 | 1.9 | 1.66 | 1.88 | 2.55 | 4.91 | 1.62 | 1.45 |
| 1347.5 | 0.37 | 1.9 | 1.66 | 1.88 | 2.55 | 4.91 | 1.62 | 1.45 |
| 1348 | 0.37 | 1.9 | 1.66 | 1.88 | 2.55 | 4.92 | 1.62 | 1.44 |
| 1348.5 | 0.37 | 1.9 | 1.65 | 1.88 | 2.55 | 4.92 | 1.62 | 1.44 |
| 1349 | 0.37 | 1.9 | 1.65 | 1.88 | 2.55 | 4.92 | 1.62 | 1.44 |
| 1349.5 | 0.37 | 1.9 | 1.66 | 1.88 | 2.54 | 4.93 | 1.61 | 1.44 |
| 1350 | 0.37 | 1.91 | 1.66 | 1.88 | 2.54 | 4.93 | 1.61 | 1.44 |
| 1350.5 | 0.37 | 1.91 | 1.66 | 1.89 | 2.54 | 4.93 | 1.61 | 1.44 |
| 1351 | 0.37 | 1.91 | 1.65 | 1.89 | 2.54 | 4.93 | 1.61 | 1.44 |
| 1351.5 | 0.37 | 1.91 | 1.65 | 1.89 | 2.54 | 4.92 | 1.61 | 1.44 |
| 1352 | 0.37 | 1.91 | 1.65 | 1.89 | 2.54 | 4.92 | 1.61 | 1.44 |
| 1352.5 | 0.37 | 1.91 | 1.65 | 1.89 | 2.54 | 4.91 | 1.61 | 1.44 |
| 1353 | 0.37 | 1.91 | 1.65 | 1.89 | 2.54 | 4.91 | 1.61 | 1.44 |
| 1353.5 | 0.37 | 1.91 | 1.65 | 1.89 | 2.54 | 4.9 | 1.62 | 1.44 |
| 1354 | 0.37 | 1.9 | 1.65 | 1.88 | 2.54 | 4.9 | 1.61 | 1.44 |
| 1354.5 | 0.37 | 1.9 | 1.65 | 1.88 | 2.54 | 4.9 | 1.61 | 1.44 |
| 1355 | 0.37 | 1.9 | 1.65 | 1.88 | 2.54 | 4.9 | 1.61 | 1.44 |
| 1355.5 | 0.37 | 1.9 | 1.65 | 1.88 | 2.54 | 4.9 | 1.61 | 1.44 |
| 1356 | 0.37 | 1.9 | 1.65 | 1.88 | 2.54 | 4.9 | 1.61 | 1.44 |
| 1356.5 | 0.37 | 1.9 | 1.65 | 1.88 | 2.54 | 4.9 | 1.61 | 1.44 |
| 1357 | 0.37 | 1.9 | 1.65 | 1.88 | 2.54 | 4.9 | 1.61 | 1.44 |
| 1357.5 | 0.37 | 1.9 | 1.65 | 1.88 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1358 | 0.37 | 1.89 | 1.64 | 1.88 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1358.5 | 0.37 | 1.89 | 1.64 | 1.88 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1359 | 0.37 | 1.89 | 1.64 | 1.88 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1359.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1360 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.61 | 1.44 |
| 1360.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.61 | 1.44 |
| 1361 | 0.37 | 1.89 | 1.64 | 1.87 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1361.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1362 | 0.37 | 1.89 | 1.64 | 1.87 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1362.5 | 0.37 | 1.9 | 1.64 | 1.87 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1363 | 0.37 | 1.89 | 1.64 | 1.87 | 2.53 | 4.9 | 1.61 | 1.44 |
| 1363.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.61 | 1.44 |
| 1364 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.61 | 1.44 |
| 1364.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.6 | 1.44 |
| 1365 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.6 | 1.44 |
| 1365.5 | 0.37 | 1.89 | 1.64 | 1.86 | 2.52 | 4.89 | 1.6 | 1.44 |
| 1366 | 0.37 | 1.89 | 1.64 | 1.86 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1366.5 | 0.37 | 1.89 | 1.64 | 1.86 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1367 | 0.37 | 1.89 | 1.64 | 1.86 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1367.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1368 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.6 | 1.44 |
| 1368.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.6 | 1.44 |
| 1369 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.6 | 1.44 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1369.5 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.6 | 1.44 |
| 1370 | 0.37 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.6 | 1.44 |
| 1370.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1371 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1371.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1372 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1372.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1373 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.6 | 1.44 |
| 1373.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.61 | 1.44 |
| 1374 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.9 | 1.61 | 1.44 |
| 1374.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.61 | 1.44 |
| 1375 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.61 | 1.44 |
| 1375.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.61 | 1.44 |
| 1376 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.89 | 1.61 | 1.44 |
| 1376.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.89 | 1.61 | 1.44 |
| 1377 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.89 | 1.61 | 1.44 |
| 1377.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.88 | 1.61 | 1.44 |
| 1378 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.88 | 1.61 | 1.44 |
| 1378.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.88 | 1.61 | 1.44 |
| 1379 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.88 | 1.61 | 1.44 |
| 1379.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.87 | 1.61 | 1.45 |
| 1380 | 0.38 | 1.9 | 1.64 | 1.87 | 2.52 | 4.87 | 1.61 | 1.45 |
| 1380.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.87 | 1.61 | 1.45 |
| 1381 | 0.38 | 1.89 | 1.64 | 1.87 | 2.52 | 4.87 | 1.61 | 1.45 |
| 1381.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.51 | 4.88 | 1.61 | 1.45 |
| 1382 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.88 | 1.61 | 1.45 |
| 1382.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.89 | 1.61 | 1.45 |
| 1383 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.89 | 1.61 | 1.45 |
| 1383.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.89 | 1.61 | 1.45 |
| 1384 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.9 | 1.61 | 1.45 |
| 1384.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.9 | 1.61 | 1.45 |
| 1385 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.89 | 1.61 | 1.45 |
| 1385.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.51 | 4.89 | 1.61 | 1.45 |
| 1386 | 0.38 | 1.89 | 1.64 | 1.86 | 2.51 | 4.89 | 1.61 | 1.45 |
| 1386.5 | 0.38 | 1.89 | 1.64 | 1.86 | 2.51 | 4.89 | 1.61 | 1.44 |
| 1387 | 0.38 | 1.89 | 1.64 | 1.86 | 2.51 | 4.89 | 1.61 | 1.44 |
| 1387.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.51 | 4.89 | 1.61 | 1.44 |
| 1388 | 0.38 | 1.89 | 1.64 | 1.87 | 2.51 | 4.89 | 1.6 | 1.44 |
| 1388.5 | 0.38 | 1.89 | 1.64 | 1.87 | 2.51 | 4.89 | 1.6 | 1.44 |
| 1389 | 0.38 | 1.89 | 1.64 | 1.87 | 2.51 | 4.89 | 1.6 | 1.44 |
| 1389.5 | 0.38 | 1.9 | 1.64 | 1.87 | 2.51 | 4.89 | 1.6 | 1.44 |
| 1390 | 0.38 | 1.9 | 1.64 | 1.86 | 2.5 | 4.89 | 1.6 | 1.44 |
| 1390.5 | 0.38 | 1.9 | 1.63 | 1.86 | 2.5 | 4.89 | 1.6 | 1.44 |
| 1391 | 0.38 | 1.89 | 1.63 | 1.86 | 2.51 | 4.89 | 1.6 | 1.44 |
| 1391.5 | 0.38 | 1.89 | 1.63 | 1.86 | 2.51 | 4.88 | 1.6 | 1.44 |
| 1392 | 0.38 | 1.89 | 1.63 | 1.86 | 2.51 | 4.88 | 1.6 | 1.44 |
| 1392.5 | 0.38 | 1.89 | 1.63 | 1.86 | 2.51 | 4.88 | 1.6 | 1.44 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1393 | 0.38 | 1.89 | 1.63 | 1.86 | 2.51 | 4.88 | 1.6 | 1.44 |
| 1393.5 | 0.38 | 1.89 | 1.63 | 1.85 | 2.51 | 4.87 | 1.6 | 1.44 |
| 1394 | 0.38 | 1.89 | 1.63 | 1.85 | 2.5 | 4.87 | 1.6 | 1.44 |
| 1394.5 | 0.38 | 1.89 | 1.63 | 1.85 | 2.5 | 4.86 | 1.6 | 1.44 |
| 1395 | 0.38 | 1.89 | 1.63 | 1.85 | 2.5 | 4.86 | 1.59 | 1.44 |
| 1395.5 | 0.38 | 1.89 | 1.63 | 1.86 | 2.49 | 4.86 | 1.59 | 1.44 |
| 1396 | 0.38 | 1.89 | 1.63 | 1.86 | 2.49 | 4.86 | 1.59 | 1.44 |
| 1396.5 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.87 | 1.6 | 1.44 |
| 1397 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.87 | 1.6 | 1.44 |
| 1397.5 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.88 | 1.6 | 1.44 |
| 1398 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.88 | 1.6 | 1.44 |
| 1398.5 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.88 | 1.6 | 1.44 |
| 1399 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.88 | 1.6 | 1.44 |
| 1399.5 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.88 | 1.6 | 1.44 |
| 1400 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.87 | 1.6 | 1.44 |
| 1400.5 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.87 | 1.6 | 1.44 |
| 1401 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.86 | 1.6 | 1.44 |
| 1401.5 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.86 | 1.6 | 1.44 |
| 1402 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.86 | 1.6 | 1.44 |
| 1402.5 | 0.38 | 1.88 | 1.63 | 1.86 | 2.49 | 4.85 | 1.6 | 1.44 |
| 1403 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.85 | 1.6 | 1.44 |
| 1403.5 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.85 | 1.6 | 1.44 |
| 1404 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.85 | 1.6 | 1.44 |
| 1404.5 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.85 | 1.59 | 1.44 |
| 1405 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.85 | 1.59 | 1.44 |
| 1405.5 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.85 | 1.59 | 1.44 |
| 1406 | 0.38 | 1.87 | 1.63 | 1.85 | 2.49 | 4.85 | 1.59 | 1.44 |
| 1406.5 | 0.38 | 1.87 | 1.63 | 1.85 | 2.49 | 4.84 | 1.59 | 1.44 |
| 1407 | 0.38 | 1.87 | 1.63 | 1.85 | 2.49 | 4.84 | 1.59 | 1.44 |
| 1407.5 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.83 | 1.59 | 1.44 |
| 1408 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.83 | 1.59 | 1.44 |
| 1408.5 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.83 | 1.59 | 1.44 |
| 1409 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.83 | 1.59 | 1.44 |
| 1409.5 | 0.38 | 1.88 | 1.63 | 1.85 | 2.49 | 4.83 | 1.59 | 1.44 |
| 1410 | 0.38 | 1.88 | 1.62 | 1.85 | 2.49 | 4.82 | 1.59 | 1.44 |
| 1410.5 | 0.38 | 1.88 | 1.62 | 1.84 | 2.48 | 4.82 | 1.59 | 1.44 |
| 1411 | 0.38 | 1.88 | 1.62 | 1.84 | 2.48 | 4.82 | 1.59 | 1.44 |
| 1411.5 | 0.38 | 1.88 | 1.62 | 1.84 | 2.48 | 4.82 | 1.59 | 1.44 |
| 1412 | 0.39 | 1.88 | 1.62 | 1.84 | 2.48 | 4.82 | 1.59 | 1.44 |
| 1412.5 | 0.39 | 1.88 | 1.62 | 1.85 | 2.48 | 4.83 | 1.59 | 1.44 |
| 1413 | 0.39 | 1.88 | 1.62 | 1.85 | 2.47 | 4.84 | 1.59 | 1.44 |
| 1413.5 | 0.39 | 1.88 | 1.62 | 1.85 | 2.47 | 4.85 | 1.59 | 1.44 |
| 1414 | 0.39 | 1.88 | 1.62 | 1.85 | 2.47 | 4.85 | 1.59 | 1.44 |
| 1414.5 | 0.39 | 1.88 | 1.62 | 1.85 | 2.47 | 4.85 | 1.59 | 1.44 |
| 1415 | 0.39 | 1.88 | 1.62 | 1.85 | 2.48 | 4.84 | 1.59 | 1.44 |
| 1415.5 | 0.39 | 1.88 | 1.63 | 1.85 | 2.48 | 4.84 | 1.59 | 1.44 |
| 1416 | 0.39 | 1.88 | 1.62 | 1.85 | 2.48 | 4.83 | 1.59 | 1.44 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1416.5 | 0.39 | 1.88 | 1.62 | 1.85 | 2.48 | 4.82 | 1.59 | 1.44 |
| 1417 | 0.39 | 1.88 | 1.62 | 1.85 | 2.48 | 4.82 | 1.59 | 1.44 |
| 1417.5 | 0.39 | 1.88 | 1.62 | 1.84 | 2.48 | 4.82 | 1.59 | 1.44 |
| 1418 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.82 | 1.59 | 1.44 |
| 1418.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.82 | 1.59 | 1.44 |
| 1419 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.83 | 1.59 | 1.44 |
| 1419.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.83 | 1.59 | 1.44 |
| 1420 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.83 | 1.59 | 1.44 |
| 1420.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.83 | 1.59 | 1.44 |
| 1421 | 0.39 | 1.87 | 1.62 | 1.84 | 2.46 | 4.83 | 1.59 | 1.44 |
| 1421.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.46 | 4.82 | 1.59 | 1.44 |
| 1422 | 0.39 | 1.87 | 1.62 | 1.84 | 2.46 | 4.82 | 1.59 | 1.44 |
| 1422.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.82 | 1.59 | 1.44 |
| 1423 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.81 | 1.59 | 1.43 |
| 1423.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.81 | 1.58 | 1.43 |
| 1424 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.81 | 1.58 | 1.43 |
| 1424.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.82 | 1.58 | 1.43 |
| 1425 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.82 | 1.58 | 1.43 |
| 1425.5 | 0.39 | 1.87 | 1.62 | 1.84 | 2.47 | 4.82 | 1.58 | 1.43 |
| 1426 | 0.39 | 1.87 | 1.61 | 1.84 | 2.46 | 4.82 | 1.58 | 1.43 |
| 1426.5 | 0.39 | 1.87 | 1.61 | 1.84 | 2.46 | 4.81 | 1.58 | 1.43 |
| 1427 | 0.39 | 1.87 | 1.61 | 1.83 | 2.46 | 4.81 | 1.58 | 1.43 |
| 1427.5 | 0.39 | 1.87 | 1.61 | 1.83 | 2.46 | 4.81 | 1.58 | 1.43 |
| 1428 | 0.39 | 1.87 | 1.61 | 1.83 | 2.46 | 4.8 | 1.58 | 1.43 |
| 1428.5 | 0.39 | 1.87 | 1.61 | 1.83 | 2.46 | 4.8 | 1.58 | 1.43 |
| 1429 | 0.39 | 1.87 | 1.61 | 1.83 | 2.45 | 4.8 | 1.58 | 1.43 |
| 1429.5 | 0.39 | 1.87 | 1.61 | 1.83 | 2.45 | 4.8 | 1.58 | 1.43 |
| 1430 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.8 | 1.58 | 1.43 |
| 1430.5 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.8 | 1.58 | 1.43 |
| 1431 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.8 | 1.58 | 1.43 |
| 1431.5 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.8 | 1.58 | 1.43 |
| 1432 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.79 | 1.58 | 1.43 |
| 1432.5 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.79 | 1.58 | 1.43 |
| 1433 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.79 | 1.58 | 1.43 |
| 1433.5 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.79 | 1.57 | 1.43 |
| 1434 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.79 | 1.57 | 1.43 |
| 1434.5 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.79 | 1.58 | 1.43 |
| 1435 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.78 | 1.58 | 1.43 |
| 1435.5 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.78 | 1.58 | 1.43 |
| 1436 | 0.39 | 1.86 | 1.61 | 1.83 | 2.45 | 4.78 | 1.58 | 1.43 |
| 1436.5 | 0.39 | 1.86 | 1.6 | 1.83 | 2.45 | 4.79 | 1.58 | 1.43 |
| 1437 | 0.39 | 1.86 | 1.6 | 1.83 | 2.44 | 4.79 | 1.58 | 1.43 |
| 1437.5 | 0.39 | 1.86 | 1.6 | 1.82 | 2.44 | 4.79 | 1.58 | 1.43 |
| 1438 | 0.39 | 1.86 | 1.6 | 1.82 | 2.44 | 4.79 | 1.57 | 1.43 |
| 1438.5 | 0.39 | 1.86 | 1.6 | 1.82 | 2.44 | 4.78 | 1.57 | 1.43 |
| 1439 | 0.39 | 1.86 | 1.6 | 1.82 | 2.44 | 4.78 | 1.57 | 1.43 |
| 1439.5 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.78 | 1.57 | 1.43 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1440 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.77 | 1.57 | 1.43 |
| 1440.5 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.77 | 1.57 | 1.43 |
| 1441 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.77 | 1.57 | 1.43 |
| 1441.5 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.77 | 1.57 | 1.43 |
| 1442 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.78 | 1.57 | 1.43 |
| 1442.5 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.78 | 1.57 | 1.43 |
| 1443 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.78 | 1.57 | 1.43 |
| 1443.5 | 0.39 | 1.85 | 1.6 | 1.82 | 2.44 | 4.78 | 1.56 | 1.43 |
| 1444 | 0.39 | 1.84 | 1.6 | 1.82 | 2.44 | 4.77 | 1.56 | 1.43 |
| 1444.5 | 0.39 | 1.84 | 1.6 | 1.82 | 2.44 | 4.77 | 1.56 | 1.43 |
| 1445 | 0.39 | 1.84 | 1.6 | 1.82 | 2.44 | 4.76 | 1.56 | 1.42 |
| 1445.5 | 0.39 | 1.84 | 1.6 | 1.82 | 2.44 | 4.76 | 1.56 | 1.42 |
| 1446 | 0.39 | 1.84 | 1.6 | 1.82 | 2.44 | 4.75 | 1.56 | 1.42 |
| 1446.5 | 0.39 | 1.84 | 1.6 | 1.82 | 2.44 | 4.75 | 1.56 | 1.42 |
| 1447 | 0.39 | 1.84 | 1.6 | 1.81 | 2.44 | 4.75 | 1.56 | 1.42 |
| 1447.5 | 0.39 | 1.84 | 1.6 | 1.81 | 2.44 | 4.75 | 1.56 | 1.42 |
| 1448 | 0.39 | 1.84 | 1.6 | 1.81 | 2.44 | 4.75 | 1.56 | 1.42 |
| 1448.5 | 0.39 | 1.84 | 1.6 | 1.81 | 2.43 | 4.75 | 1.56 | 1.42 |
| 1449 | 0.39 | 1.84 | 1.6 | 1.81 | 2.43 | 4.75 | 1.56 | 1.42 |
| 1449.5 | 0.39 | 1.84 | 1.6 | 1.81 | 2.43 | 4.76 | 1.56 | 1.42 |
| 1450 | 0.39 | 1.84 | 1.6 | 1.81 | 2.43 | 4.77 | 1.56 | 1.42 |
| 1450.5 | 0.39 | 1.84 | 1.59 | 1.81 | 2.43 | 4.78 | 1.56 | 1.42 |
| 1451 | 0.39 | 1.84 | 1.59 | 1.81 | 2.43 | 4.78 | 1.56 | 1.42 |
| 1451.5 | 0.39 | 1.84 | 1.59 | 1.81 | 2.42 | 4.78 | 1.56 | 1.42 |
| 1452 | 0.39 | 1.84 | 1.59 | 1.81 | 2.42 | 4.78 | 1.56 | 1.42 |
| 1452.5 | 0.39 | 1.84 | 1.59 | 1.81 | 2.42 | 4.77 | 1.56 | 1.42 |
| 1453 | 0.39 | 1.84 | 1.59 | 1.81 | 2.42 | 4.76 | 1.56 | 1.42 |
| 1453.5 | 0.39 | 1.84 | 1.59 | 1.8 | 2.42 | 4.75 | 1.56 | 1.42 |
| 1454 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.75 | 1.55 | 1.42 |
| 1454.5 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.74 | 1.55 | 1.42 |
| 1455 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.74 | 1.55 | 1.42 |
| 1455.5 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.74 | 1.55 | 1.42 |
| 1456 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.74 | 1.55 | 1.42 |
| 1456.5 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.74 | 1.55 | 1.41 |
| 1457 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.74 | 1.55 | 1.41 |
| 1457.5 | 0.40 | 1.84 | 1.59 | 1.8 | 2.42 | 4.74 | 1.55 | 1.41 |
| 1458 | 0.40 | 1.83 | 1.59 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1458.5 | 0.40 | 1.83 | 1.59 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1459 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1459.5 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1460 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1460.5 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1461 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1461.5 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1462 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1462.5 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1463 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1463.5 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1464 | 0.40 | 1.83 | 1.58 | 1.8 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1464.5 | 0.40 | 1.83 | 1.58 | 1.79 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1465 | 0.40 | 1.83 | 1.58 | 1.79 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1465.5 | 0.40 | 1.83 | 1.58 | 1.79 | 2.41 | 4.74 | 1.55 | 1.41 |
| 1466 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.74 | 1.55 | 1.41 |
| 1466.5 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.74 | 1.54 | 1.41 |
| 1467 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.74 | 1.54 | 1.41 |
| 1467.5 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.74 | 1.54 | 1.41 |
| 1468 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.73 | 1.54 | 1.41 |
| 1468.5 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.73 | 1.54 | 1.41 |
| 1469 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.73 | 1.54 | 1.41 |
| 1469.5 | 0.40 | 1.83 | 1.58 | 1.79 | 2.4 | 4.73 | 1.54 | 1.41 |
| 1470 | 0.40 | 1.82 | 1.58 | 1.79 | 2.4 | 4.73 | 1.54 | 1.41 |
| 1470.5 | 0.40 | 1.82 | 1.58 | 1.79 | 2.4 | 4.73 | 1.54 | 1.41 |
| 1471 | 0.40 | 1.82 | 1.58 | 1.79 | 2.4 | 4.73 | 1.54 | 1.41 |
| 1471.5 | 0.40 | 1.82 | 1.58 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1472 | 0.40 | 1.82 | 1.58 | 1.79 | 2.39 | 4.72 | 1.55 | 1.41 |
| 1472.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.55 | 1.41 |
| 1473 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.55 | 1.41 |
| 1473.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1474 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1474.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1475 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1475.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.71 | 1.54 | 1.41 |
| 1476 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.71 | 1.54 | 1.41 |
| 1476.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.71 | 1.54 | 1.41 |
| 1477 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.7 | 1.54 | 1.41 |
| 1477.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.7 | 1.54 | 1.41 |
| 1478 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.7 | 1.54 | 1.41 |
| 1478.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.71 | 1.54 | 1.41 |
| 1479 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.71 | 1.54 | 1.41 |
| 1479.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1480 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1480.5 | 0.40 | 1.82 | 1.57 | 1.79 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1481 | 0.40 | 1.82 | 1.57 | 1.78 | 2.39 | 4.73 | 1.54 | 1.41 |
| 1481.5 | 0.40 | 1.82 | 1.57 | 1.78 | 2.39 | 4.73 | 1.54 | 1.41 |
| 1482 | 0.40 | 1.82 | 1.57 | 1.78 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1482.5 | 0.40 | 1.82 | 1.57 | 1.78 | 2.39 | 4.72 | 1.54 | 1.41 |
| 1483 | 0.40 | 1.82 | 1.57 | 1.78 | 2.39 | 4.71 | 1.54 | 1.41 |
| 1483.5 | 0.40 | 1.82 | 1.57 | 1.78 | 2.39 | 4.71 | 1.54 | 1.41 |
| 1484 | 0.40 | 1.82 | 1.57 | 1.78 | 2.38 | 4.7 | 1.54 | 1.41 |
| 1484.5 | 0.40 | 1.82 | 1.57 | 1.78 | 2.38 | 4.7 | 1.54 | 1.41 |
| 1485 | 0.40 | 1.82 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |
| 1485.5 | 0.40 | 1.82 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |
| 1486 | 0.40 | 1.82 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |
| 1486.5 | 0.40 | 1.82 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1487 | 0.40 | 1.82 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |
| 1487.5 | 0.40 | 1.82 | 1.57 | 1.78 | 2.37 | 4.69 | 1.54 | 1.41 |
| 1488 | 0.40 | 1.81 | 1.57 | 1.78 | 2.37 | 4.7 | 1.54 | 1.41 |
| 1488.5 | 0.40 | 1.81 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |
| 1489 | 0.40 | 1.81 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |
| 1489.5 | 0.40 | 1.81 | 1.57 | 1.78 | 2.38 | 4.69 | 1.54 | 1.41 |
| 1490 | 0.40 | 1.81 | 1.57 | 1.78 | 2.38 | 4.68 | 1.54 | 1.41 |
| 1490.5 | 0.40 | 1.81 | 1.57 | 1.78 | 2.38 | 4.68 | 1.53 | 1.4 |
| 1491 | 0.40 | 1.81 | 1.56 | 1.78 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1491.5 | 0.40 | 1.81 | 1.56 | 1.78 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1492 | 0.40 | 1.81 | 1.56 | 1.77 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1492.5 | 0.40 | 1.81 | 1.56 | 1.77 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1493 | 0.40 | 1.81 | 1.56 | 1.77 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1493.5 | 0.40 | 1.81 | 1.56 | 1.77 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1494 | 0.40 | 1.81 | 1.56 | 1.77 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1494.5 | 0.40 | 1.81 | 1.56 | 1.77 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1495 | 0.40 | 1.81 | 1.56 | 1.77 | 2.38 | 4.67 | 1.53 | 1.4 |
| 1495.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.38 | 4.68 | 1.53 | 1.4 |
| 1496 | 0.41 | 1.81 | 1.56 | 1.77 | 2.38 | 4.68 | 1.53 | 1.4 |
| 1496.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.4 |
| 1497 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.4 |
| 1497.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.4 |
| 1498 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.4 |
| 1498.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.4 |
| 1499 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.4 |
| 1499.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.4 |
| 1500 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.54 | 1.4 |
| 1500.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.67 | 1.54 | 1.4 |
| 1501 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.67 | 1.54 | 1.4 |
| 1501.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.67 | 1.54 | 1.4 |
| 1502 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.66 | 1.54 | 1.4 |
| 1502.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.66 | 1.54 | 1.4 |
| 1503 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.66 | 1.53 | 1.4 |
| 1503.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.66 | 1.53 | 1.41 |
| 1504 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.67 | 1.53 | 1.41 |
| 1504.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.67 | 1.53 | 1.41 |
| 1505 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.67 | 1.53 | 1.41 |
| 1505.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.37 | 4.68 | 1.53 | 1.41 |
| 1506 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1506.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1507 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1507.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1508 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1508.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1509 | 0.41 | 1.81 | 1.57 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1509.5 | 0.41 | 1.81 | 1.57 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |
| 1510 | 0.41 | 1.82 | 1.57 | 1.77 | 2.36 | 4.68 | 1.53 | 1.41 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1510.5 | 0.41 | 1.82 | 1.57 | 1.77 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1511 | 0.41 | 1.82 | 1.57 | 1.77 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1511.5 | 0.41 | 1.82 | 1.57 | 1.78 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1512 | 0.41 | 1.82 | 1.57 | 1.78 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1512.5 | 0.41 | 1.82 | 1.57 | 1.78 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1513 | 0.41 | 1.82 | 1.57 | 1.78 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1513.5 | 0.41 | 1.81 | 1.57 | 1.78 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1514 | 0.41 | 1.81 | 1.57 | 1.77 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1514.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1515 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1515.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.36 | 4.67 | 1.53 | 1.41 |
| 1516 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.67 | 1.53 | 1.41 |
| 1516.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.67 | 1.53 | 1.41 |
| 1517 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.68 | 1.54 | 1.41 |
| 1517.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.68 | 1.54 | 1.41 |
| 1518 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.68 | 1.54 | 1.41 |
| 1518.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.67 | 1.54 | 1.41 |
| 1519 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.67 | 1.54 | 1.41 |
| 1519.5 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.67 | 1.53 | 1.4 |
| 1520 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.67 | 1.53 | 1.4 |
| 1520.5 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.66 | 1.53 | 1.4 |
| 1521 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.66 | 1.53 | 1.4 |
| 1521.5 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.66 | 1.53 | 1.41 |
| 1522 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1522.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1523 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1523.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1524 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1524.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1525 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1525.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1526 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1526.5 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1527 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1527.5 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1528 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1528.5 | 0.41 | 1.81 | 1.56 | 1.76 | 2.35 | 4.65 | 1.53 | 1.41 |
| 1529 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.66 | 1.54 | 1.41 |
| 1529.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.66 | 1.54 | 1.41 |
| 1530 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.66 | 1.54 | 1.41 |
| 1530.5 | 0.41 | 1.81 | 1.56 | 1.77 | 2.35 | 4.66 | 1.54 | 1.41 |
| 1531 | 0.41 | 1.82 | 1.56 | 1.77 | 2.35 | 4.66 | 1.54 | 1.41 |
| 1531.5 | 0.41 | 1.82 | 1.56 | 1.77 | 2.35 | 4.66 | 1.54 | 1.42 |
| 1532 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.54 | 1.42 |
| 1532.5 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.54 | 1.42 |
| 1533 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.54 | 1.42 |
| 1533.5 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.54 | 1.42 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1534 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.53 | 1.42 |
| 1534.5 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.53 | 1.42 |
| 1535 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.53 | 1.42 |
| 1535.5 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.53 | 1.42 |
| 1536 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.54 | 1.42 |
| 1536.5 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.67 | 1.54 | 1.42 |
| 1537 | 0.41 | 1.82 | 1.57 | 1.77 | 2.35 | 4.66 | 1.54 | 1.42 |
| 1537.5 | 0.42 | 1.82 | 1.57 | 1.77 | 2.35 | 4.66 | 1.54 | 1.42 |
| 1538 | 0.42 | 1.82 | 1.57 | 1.77 | 2.35 | 4.66 | 1.54 | 1.42 |
| 1538.5 | 0.42 | 1.82 | 1.57 | 1.77 | 2.35 | 4.66 | 1.54 | 1.42 |
| 1539 | 0.42 | 1.82 | 1.57 | 1.77 | 2.35 | 4.66 | 1.54 | 1.42 |
| 1539.5 | 0.42 | 1.81 | 1.57 | 1.77 | 2.35 | 4.65 | 1.54 | 1.42 |
| 1540 | 0.42 | 1.81 | 1.57 | 1.77 | 2.35 | 4.65 | 1.53 | 1.42 |
| 1540.5 | 0.42 | 1.81 | 1.57 | 1.77 | 2.35 | 4.65 | 1.53 | 1.42 |
| 1541 | 0.42 | 1.81 | 1.57 | 1.77 | 2.34 | 4.64 | 1.53 | 1.42 |
| 1541.5 | 0.42 | 1.81 | 1.57 | 1.77 | 2.34 | 4.64 | 1.53 | 1.42 |
| 1542 | 0.42 | 1.81 | 1.56 | 1.77 | 2.34 | 4.64 | 1.53 | 1.42 |
| 1542.5 | 0.42 | 1.81 | 1.56 | 1.77 | 2.34 | 4.63 | 1.53 | 1.41 |
| 1543 | 0.42 | 1.81 | 1.56 | 1.77 | 2.34 | 4.63 | 1.53 | 1.41 |
| 1543.5 | 0.42 | 1.8 | 1.56 | 1.76 | 2.34 | 4.62 | 1.53 | 1.41 |
| 1544 | 0.42 | 1.8 | 1.56 | 1.76 | 2.34 | 4.62 | 1.53 | 1.41 |
| 1544.5 | 0.42 | 1.8 | 1.55 | 1.76 | 2.34 | 4.61 | 1.52 | 1.41 |
| 1545 | 0.42 | 1.8 | 1.55 | 1.76 | 2.33 | 4.61 | 1.52 | 1.41 |
| 1545.5 | 0.42 | 1.8 | 1.55 | 1.76 | 2.33 | 4.61 | 1.52 | 1.4 |
| 1546 | 0.42 | 1.8 | 1.55 | 1.75 | 2.33 | 4.6 | 1.52 | 1.4 |
| 1546.5 | 0.42 | 1.79 | 1.54 | 1.75 | 2.33 | 4.6 | 1.51 | 1.4 |
| 1547 | 0.42 | 1.79 | 1.54 | 1.75 | 2.32 | 4.6 | 1.51 | 1.4 |
| 1547.5 | 0.42 | 1.79 | 1.54 | 1.74 | 2.32 | 4.6 | 1.51 | 1.39 |
| 1548 | 0.42 | 1.79 | 1.54 | 1.74 | 2.32 | 4.6 | 1.51 | 1.39 |
| 1548.5 | 0.42 | 1.78 | 1.53 | 1.74 | 2.31 | 4.6 | 1.5 | 1.39 |
| 1549 | 0.42 | 1.78 | 1.53 | 1.73 | 2.31 | 4.6 | 1.5 | 1.38 |
| 1549.5 | 0.42 | 1.78 | 1.53 | 1.73 | 2.31 | 4.59 | 1.5 | 1.38 |
| 1550 | 0.42 | 1.77 | 1.53 | 1.73 | 2.3 | 4.59 | 1.49 | 1.38 |
| 1550.5 | 0.42 | 1.77 | 1.52 | 1.73 | 2.3 | 4.59 | 1.49 | 1.38 |
| 1551 | 0.42 | 1.77 | 1.52 | 1.73 | 2.3 | 4.58 | 1.49 | 1.37 |
| 1551.5 | 0.42 | 1.77 | 1.52 | 1.72 | 2.3 | 4.58 | 1.49 | 1.37 |
| 1552 | 0.42 | 1.76 | 1.52 | 1.72 | 2.3 | 4.57 | 1.48 | 1.37 |
| 1552.5 | 0.42 | 1.76 | 1.52 | 1.72 | 2.29 | 4.57 | 1.48 | 1.37 |
| 1553 | 0.42 | 1.76 | 1.51 | 1.72 | 2.29 | 4.56 | 1.48 | 1.37 |
| 1553.5 | 0.42 | 1.76 | 1.51 | 1.72 | 2.29 | 4.56 | 1.48 | 1.37 |
| 1554 | 0.42 | 1.76 | 1.51 | 1.71 | 2.29 | 4.56 | 1.48 | 1.36 |
| 1554.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1555 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1555.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1556 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1556.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.36 |
| 1557 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.36 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1557.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.36 |
| 1558 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.54 | 1.47 | 1.36 |
| 1558.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.54 | 1.47 | 1.36 |
| 1559 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.54 | 1.47 | 1.36 |
| 1559.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1560 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1560.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1561 | 0.42 | 1.75 | 1.5 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1561.5 | 0.42 | 1.75 | 1.5 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1562 | 0.42 | 1.75 | 1.5 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1562.5 | 0.42 | 1.75 | 1.5 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1563 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1563.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.47 | 1.36 |
| 1564 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1564.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1565 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1565.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1566 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1566.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1567 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.36 |
| 1567.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.29 | 4.55 | 1.48 | 1.37 |
| 1568 | 0.42 | 1.76 | 1.51 | 1.71 | 2.29 | 4.55 | 1.48 | 1.37 |
| 1568.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1569 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1569.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1570 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.37 |
| 1570.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.37 |
| 1571 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.37 |
| 1571.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.37 |
| 1572 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.37 |
| 1572.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.37 |
| 1573 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.54 | 1.48 | 1.37 |
| 1573.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1574 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1574.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1575 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1575.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.55 | 1.48 | 1.37 |
| 1576 | 0.42 | 1.76 | 1.51 | 1.71 | 2.28 | 4.56 | 1.48 | 1.37 |
| 1576.5 | 0.42 | 1.76 | 1.51 | 1.71 | 2.27 | 4.56 | 1.48 | 1.37 |
| 1577 | 0.42 | 1.75 | 1.51 | 1.71 | 2.27 | 4.56 | 1.48 | 1.37 |
| 1577.5 | 0.42 | 1.75 | 1.51 | 1.71 | 2.27 | 4.56 | 1.48 | 1.36 |
| 1578 | 0.42 | 1.75 | 1.5 | 1.71 | 2.27 | 4.55 | 1.48 | 1.36 |
| 1578.5 | 0.42 | 1.75 | 1.5 | 1.71 | 2.27 | 4.55 | 1.47 | 1.36 |
| 1579 | 0.43 | 1.75 | 1.5 | 1.71 | 2.27 | 4.55 | 1.47 | 1.36 |
| 1579.5 | 0.43 | 1.75 | 1.5 | 1.7 | 2.27 | 4.54 | 1.47 | 1.36 |
| 1580 | 0.43 | 1.75 | 1.5 | 1.7 | 2.27 | 4.54 | 1.47 | 1.36 |
| 1580.5 | 0.43 | 1.75 | 1.5 | 1.7 | 2.27 | 4.53 | 1.47 | 1.36 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1581 | 0.43 | 1.75 | 1.5 | 1.7 | 2.26 | 4.53 | 1.47 | 1.36 |
| 1581.5 | 0.43 | 1.74 | 1.5 | 1.7 | 2.26 | 4.53 | 1.47 | 1.36 |
| 1582 | 0.43 | 1.74 | 1.5 | 1.7 | 2.26 | 4.52 | 1.47 | 1.36 |
| 1582.5 | 0.43 | 1.74 | 1.5 | 1.7 | 2.26 | 4.52 | 1.47 | 1.36 |
| 1583 | 0.43 | 1.74 | 1.5 | 1.69 | 2.26 | 4.52 | 1.46 | 1.36 |
| 1583.5 | 0.43 | 1.74 | 1.5 | 1.69 | 2.26 | 4.51 | 1.46 | 1.35 |
| 1584 | 0.43 | 1.74 | 1.49 | 1.69 | 2.26 | 4.51 | 1.46 | 1.35 |
| 1584.5 | 0.43 | 1.74 | 1.49 | 1.69 | 2.26 | 4.51 | 1.46 | 1.35 |
| 1585 | 0.43 | 1.74 | 1.49 | 1.69 | 2.26 | 4.51 | 1.46 | 1.35 |
| 1585.5 | 0.43 | 1.73 | 1.49 | 1.69 | 2.26 | 4.51 | 1.46 | 1.35 |
| 1586 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.51 | 1.46 | 1.35 |
| 1586.5 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.51 | 1.46 | 1.35 |
| 1587 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.51 | 1.46 | 1.35 |
| 1587.5 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1588 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1588.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.49 | 1.45 | 1.35 |
| 1589 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.49 | 1.45 | 1.35 |
| 1589.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.49 | 1.45 | 1.35 |
| 1590 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.49 | 1.45 | 1.35 |
| 1590.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.49 | 1.45 | 1.35 |
| 1591 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.49 | 1.45 | 1.35 |
| 1591.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.45 | 1.35 |
| 1592 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.45 | 1.35 |
| 1592.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.45 | 1.35 |
| 1593 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1593.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1594 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1594.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1595 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1595.5 | 0.43 | 1.73 | 1.48 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1596 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1596.5 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1597 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1597.5 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1598 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.5 | 1.46 | 1.35 |
| 1598.5 | 0.43 | 1.73 | 1.49 | 1.69 | 2.25 | 4.5 | 1.45 | 1.35 |
| 1599 | 0.43 | 1.73 | 1.49 | 1.69 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1599.5 | 0.43 | 1.73 | 1.49 | 1.69 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1600 | 0.43 | 1.73 | 1.49 | 1.68 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1600.5 | 0.43 | 1.73 | 1.49 | 1.68 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1601 | 0.43 | 1.73 | 1.48 | 1.68 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1601.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1602 | 0.43 | 1.73 | 1.48 | 1.68 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1602.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1603 | 0.43 | 1.73 | 1.48 | 1.68 | 2.24 | 4.5 | 1.45 | 1.35 |
| 1603.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.24 | 4.49 | 1.45 | 1.35 |
| 1604 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.49 | 1.45 | 1.35 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1604.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.49 | 1.45 | 1.35 |
| 1605 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.48 | 1.45 | 1.35 |
| 1605.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.48 | 1.45 | 1.35 |
| 1606 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.48 | 1.45 | 1.35 |
| 1606.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.48 | 1.45 | 1.34 |
| 1607 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.48 | 1.45 | 1.34 |
| 1607.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.47 | 1.45 | 1.34 |
| 1608 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.47 | 1.45 | 1.34 |
| 1608.5 | 0.43 | 1.73 | 1.48 | 1.68 | 2.23 | 4.47 | 1.45 | 1.34 |
| 1609 | 0.43 | 1.73 | 1.47 | 1.68 | 2.23 | 4.47 | 1.44 | 1.34 |
| 1609.5 | 0.43 | 1.72 | 1.47 | 1.67 | 2.23 | 4.47 | 1.44 | 1.34 |
| 1610 | 0.43 | 1.72 | 1.47 | 1.67 | 2.23 | 4.47 | 1.44 | 1.34 |
| 1610.5 | 0.43 | 1.72 | 1.47 | 1.67 | 2.23 | 4.47 | 1.44 | 1.34 |
| 1611 | 0.43 | 1.72 | 1.47 | 1.67 | 2.23 | 4.46 | 1.44 | 1.34 |
| 1611.5 | 0.43 | 1.72 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.34 |
| 1612 | 0.43 | 1.72 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.34 |
| 1612.5 | 0.43 | 1.72 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.34 |
| 1613 | 0.43 | 1.72 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.33 |
| 1613.5 | 0.43 | 1.72 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.33 |
| 1614 | 0.43 | 1.71 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.33 |
| 1614.5 | 0.43 | 1.71 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.33 |
| 1615 | 0.43 | 1.71 | 1.47 | 1.67 | 2.22 | 4.46 | 1.44 | 1.33 |
| 1615.5 | 0.43 | 1.71 | 1.47 | 1.66 | 2.21 | 4.46 | 1.44 | 1.33 |
| 1616 | 0.43 | 1.71 | 1.47 | 1.66 | 2.21 | 4.45 | 1.43 | 1.33 |
| 1616.5 | 0.43 | 1.71 | 1.47 | 1.66 | 2.21 | 4.45 | 1.43 | 1.33 |
| 1617 | 0.43 | 1.71 | 1.46 | 1.66 | 2.21 | 4.45 | 1.43 | 1.33 |
| 1617.5 | 0.43 | 1.71 | 1.46 | 1.66 | 2.21 | 4.44 | 1.43 | 1.33 |
| 1618 | 0.43 | 1.71 | 1.46 | 1.66 | 2.2 | 4.44 | 1.43 | 1.33 |
| 1618.5 | 0.43 | 1.7 | 1.46 | 1.66 | 2.2 | 4.44 | 1.43 | 1.33 |
| 1619 | 0.43 | 1.7 | 1.46 | 1.65 | 2.2 | 4.44 | 1.43 | 1.32 |
| 1619.5 | 0.43 | 1.7 | 1.46 | 1.65 | 2.2 | 4.44 | 1.43 | 1.32 |
| 1620 | 0.43 | 1.7 | 1.45 | 1.65 | 2.2 | 4.44 | 1.42 | 1.32 |
| 1620.5 | 0.43 | 1.7 | 1.45 | 1.65 | 2.2 | 4.44 | 1.42 | 1.32 |
| 1621 | 0.44 | 1.7 | 1.45 | 1.65 | 2.2 | 4.43 | 1.42 | 1.32 |
| 1621.5 | 0.44 | 1.69 | 1.45 | 1.65 | 2.2 | 4.43 | 1.42 | 1.32 |
| 1622 | 0.44 | 1.69 | 1.45 | 1.65 | 2.19 | 4.43 | 1.42 | 1.32 |
| 1622.5 | 0.44 | 1.69 | 1.45 | 1.65 | 2.19 | 4.43 | 1.42 | 1.32 |
| 1623 | 0.44 | 1.69 | 1.45 | 1.65 | 2.19 | 4.43 | 1.41 | 1.32 |
| 1623.5 | 0.44 | 1.69 | 1.45 | 1.65 | 2.19 | 4.42 | 1.41 | 1.32 |
| 1624 | 0.44 | 1.69 | 1.45 | 1.65 | 2.19 | 4.42 | 1.41 | 1.32 |
| 1624.5 | 0.44 | 1.69 | 1.45 | 1.65 | 2.19 | 4.42 | 1.41 | 1.31 |
| 1625 | 0.44 | 1.69 | 1.44 | 1.64 | 2.19 | 4.41 | 1.41 | 1.31 |
| 1625.5 | 0.44 | 1.69 | 1.44 | 1.64 | 2.18 | 4.41 | 1.41 | 1.31 |
| 1626 | 0.44 | 1.69 | 1.44 | 1.64 | 2.18 | 4.41 | 1.41 | 1.31 |
| 1626.5 | 0.44 | 1.69 | 1.44 | 1.64 | 2.18 | 4.4 | 1.41 | 1.31 |
| 1627 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.4 | 1.41 | 1.31 |
| 1627.5 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.4 | 1.41 | 1.31 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1628 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.4 | 1.41 | 1.31 |
| 1628.5 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.4 | 1.41 | 1.31 |
| 1629 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.4 | 1.41 | 1.31 |
| 1629.5 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.4 | 1.41 | 1.31 |
| 1630 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.4 | 1.4 | 1.31 |
| 1630.5 | 0.44 | 1.68 | 1.44 | 1.64 | 2.18 | 4.39 | 1.4 | 1.31 |
| 1631 | 0.44 | 1.68 | 1.44 | 1.63 | 2.18 | 4.39 | 1.4 | 1.31 |
| 1631.5 | 0.44 | 1.68 | 1.43 | 1.63 | 2.17 | 4.39 | 1.4 | 1.3 |
| 1632 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.39 | 1.4 | 1.3 |
| 1632.5 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.39 | 1.4 | 1.3 |
| 1633 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.39 | 1.4 | 1.3 |
| 1633.5 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.38 | 1.4 | 1.3 |
| 1634 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.38 | 1.4 | 1.3 |
| 1634.5 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.38 | 1.4 | 1.3 |
| 1635 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.38 | 1.4 | 1.3 |
| 1635.5 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.38 | 1.4 | 1.3 |
| 1636 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.38 | 1.4 | 1.3 |
| 1636.5 | 0.44 | 1.67 | 1.43 | 1.63 | 2.17 | 4.38 | 1.4 | 1.3 |
| 1637 | 0.44 | 1.67 | 1.43 | 1.63 | 2.16 | 4.38 | 1.4 | 1.3 |
| 1637.5 | 0.44 | 1.67 | 1.42 | 1.63 | 2.16 | 4.37 | 1.4 | 1.3 |
| 1638 | 0.44 | 1.67 | 1.42 | 1.63 | 2.16 | 4.37 | 1.39 | 1.3 |
| 1638.5 | 0.44 | 1.67 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.3 |
| 1639 | 0.44 | 1.67 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.3 |
| 1639.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.3 |
| 1640 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.3 |
| 1640.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.35 | 1.39 | 1.3 |
| 1641 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.35 | 1.39 | 1.3 |
| 1641.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.35 | 1.39 | 1.3 |
| 1642 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.3 |
| 1642.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.3 |
| 1643 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.3 |
| 1643.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.16 | 4.36 | 1.39 | 1.29 |
| 1644 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.37 | 1.39 | 1.29 |
| 1644.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.37 | 1.39 | 1.29 |
| 1645 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.37 | 1.39 | 1.29 |
| 1645.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.36 | 1.39 | 1.29 |
| 1646 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.36 | 1.39 | 1.29 |
| 1646.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.36 | 1.39 | 1.29 |
| 1647 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.36 | 1.39 | 1.29 |
| 1647.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.36 | 1.39 | 1.29 |
| 1648 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1648.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1649 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1649.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1650 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1650.5 | 0.44 | 1.66 | 1.42 | 1.62 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1651 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.39 | 1.29 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1651.5 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1652 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.39 | 1.29 |
| 1652.5 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.38 | 1.29 |
| 1653 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.38 | 1.29 |
| 1653.5 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.38 | 1.29 |
| 1654 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.38 | 1.29 |
| 1654.5 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.38 | 1.29 |
| 1655 | 0.44 | 1.66 | 1.42 | 1.61 | 2.15 | 4.35 | 1.38 | 1.29 |
| 1655.5 | 0.44 | 1.66 | 1.42 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1656 | 0.44 | 1.66 | 1.42 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1656.5 | 0.44 | 1.66 | 1.42 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1657 | 0.44 | 1.66 | 1.42 | 1.61 | 2.14 | 4.36 | 1.38 | 1.29 |
| 1657.5 | 0.44 | 1.66 | 1.42 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1658 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1658.5 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1659 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1659.5 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.35 | 1.38 | 1.29 |
| 1660 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1660.5 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1661 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1661.5 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1662 | 0.44 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1662.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1663 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1663.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1664 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1664.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1665 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1665.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1666 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1666.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1667 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1667.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1668 | 0.45 | 1.65 | 1.41 | 1.61 | 2.14 | 4.34 | 1.38 | 1.29 |
| 1668.5 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1669 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1669.5 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1670 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1670.5 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1671 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1671.5 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1672 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.34 | 1.38 | 1.29 |
| 1672.5 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1673 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1673.5 | 0.45 | 1.65 | 1.41 | 1.6 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1674 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1674.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1675 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1675.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1676 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1676.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1677 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1677.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1678 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1678.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1679 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1679.5 | 0.45 | 1.65 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1680 | 0.45 | 1.66 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.29 |
| 1680.5 | 0.45 | 1.66 | 1.41 | 1.61 | 2.13 | 4.33 | 1.38 | 1.3 |
| 1681 | 0.45 | 1.66 | 1.41 | 1.61 | 2.13 | 4.34 | 1.38 | 1.3 |
| 1681.5 | 0.45 | 1.66 | 1.41 | 1.61 | 2.13 | 4.34 | 1.38 | 1.3 |
| 1682 | 0.45 | 1.66 | 1.42 | 1.61 | 2.13 | 4.34 | 1.38 | 1.3 |
| 1682.5 | 0.45 | 1.66 | 1.42 | 1.61 | 2.13 | 4.34 | 1.38 | 1.3 |
| 1683 | 0.45 | 1.66 | 1.42 | 1.61 | 2.13 | 4.34 | 1.39 | 1.3 |
| 1683.5 | 0.45 | 1.66 | 1.42 | 1.61 | 2.13 | 4.34 | 1.39 | 1.3 |
| 1684 | 0.45 | 1.66 | 1.42 | 1.61 | 2.13 | 4.35 | 1.39 | 1.3 |
| 1684.5 | 0.45 | 1.66 | 1.42 | 1.61 | 2.13 | 4.35 | 1.39 | 1.3 |
| 1685 | 0.45 | 1.66 | 1.42 | 1.61 | 2.14 | 4.35 | 1.39 | 1.3 |
| 1685.5 | 0.45 | 1.66 | 1.42 | 1.61 | 2.14 | 4.35 | 1.39 | 1.3 |
| 1686 | 0.45 | 1.66 | 1.42 | 1.61 | 2.14 | 4.36 | 1.39 | 1.31 |
| 1686.5 | 0.45 | 1.67 | 1.42 | 1.61 | 2.14 | 4.36 | 1.39 | 1.31 |
| 1687 | 0.45 | 1.67 | 1.43 | 1.62 | 2.14 | 4.36 | 1.39 | 1.31 |
| 1687.5 | 0.45 | 1.67 | 1.43 | 1.62 | 2.14 | 4.36 | 1.39 | 1.31 |
| 1688 | 0.45 | 1.67 | 1.43 | 1.62 | 2.14 | 4.36 | 1.4 | 1.31 |
| 1688.5 | 0.45 | 1.67 | 1.43 | 1.62 | 2.14 | 4.37 | 1.4 | 1.31 |
| 1689 | 0.45 | 1.67 | 1.43 | 1.62 | 2.14 | 4.37 | 1.4 | 1.32 |
| 1689.5 | 0.45 | 1.68 | 1.43 | 1.62 | 2.15 | 4.37 | 1.4 | 1.32 |
| 1690 | 0.45 | 1.68 | 1.44 | 1.62 | 2.15 | 4.37 | 1.41 | 1.32 |
| 1690.5 | 0.45 | 1.68 | 1.44 | 1.63 | 2.15 | 4.38 | 1.41 | 1.32 |
| 1691 | 0.45 | 1.68 | 1.44 | 1.63 | 2.15 | 4.38 | 1.41 | 1.32 |
| 1691.5 | 0.45 | 1.69 | 1.44 | 1.63 | 2.15 | 4.38 | 1.41 | 1.33 |
| 1692 | 0.45 | 1.69 | 1.44 | 1.63 | 2.16 | 4.39 | 1.42 | 1.33 |
| 1692.5 | 0.45 | 1.69 | 1.45 | 1.64 | 2.16 | 4.39 | 1.42 | 1.33 |
| 1693 | 0.45 | 1.69 | 1.45 | 1.64 | 2.16 | 4.4 | 1.42 | 1.33 |
| 1693.5 | 0.45 | 1.7 | 1.45 | 1.64 | 2.16 | 4.4 | 1.42 | 1.34 |
| 1694 | 0.45 | 1.7 | 1.45 | 1.64 | 2.17 | 4.41 | 1.43 | 1.34 |
| 1694.5 | 0.45 | 1.7 | 1.46 | 1.65 | 2.17 | 4.41 | 1.43 | 1.34 |
| 1695 | 0.45 | 1.71 | 1.46 | 1.65 | 2.17 | 4.42 | 1.43 | 1.35 |
| 1695.5 | 0.45 | 1.71 | 1.46 | 1.65 | 2.18 | 4.43 | 1.43 | 1.35 |
| 1696 | 0.45 | 1.71 | 1.47 | 1.65 | 2.18 | 4.43 | 1.44 | 1.35 |
| 1696.5 | 0.45 | 1.72 | 1.47 | 1.66 | 2.18 | 4.44 | 1.44 | 1.36 |
| 1697 | 0.45 | 1.72 | 1.47 | 1.66 | 2.19 | 4.44 | 1.45 | 1.36 |
| 1697.5 | 0.45 | 1.73 | 1.48 | 1.66 | 2.19 | 4.45 | 1.45 | 1.36 |
| 1698 | 0.45 | 1.73 | 1.48 | 1.67 | 2.19 | 4.45 | 1.45 | 1.37 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1698.5 | 0.45 | 1.73 | 1.49 | 1.67 | 2.2 | 4.46 | 1.46 | 1.37 |
| 1699 | 0.45 | 1.74 | 1.49 | 1.67 | 2.2 | 4.46 | 1.46 | 1.38 |
| 1699.5 | 0.45 | 1.74 | 1.49 | 1.68 | 2.2 | 4.47 | 1.47 | 1.38 |
| 1700 | 0.45 | 1.75 | 1.5 | 1.68 | 2.21 | 4.48 | 1.47 | 1.39 |
| 1700.5 | 0.45 | 1.75 | 1.5 | 1.68 | 2.21 | 4.48 | 1.47 | 1.39 |
| 1701 | 0.45 | 1.75 | 1.5 | 1.69 | 2.22 | 4.49 | 1.48 | 1.4 |
| 1701.5 | 0.45 | 1.76 | 1.51 | 1.69 | 2.22 | 4.5 | 1.48 | 1.4 |
| 1702 | 0.45 | 1.76 | 1.51 | 1.69 | 2.22 | 4.51 | 1.49 | 1.4 |
| 1702.5 | 0.45 | 1.77 | 1.51 | 1.7 | 2.23 | 4.52 | 1.49 | 1.41 |
| 1703 | 0.45 | 1.77 | 1.52 | 1.7 | 2.23 | 4.53 | 1.5 | 1.41 |
| 1703.5 | 0.45 | 1.78 | 1.52 | 1.71 | 2.23 | 4.53 | 1.5 | 1.42 |
| 1704 | 0.45 | 1.78 | 1.53 | 1.71 | 2.24 | 4.54 | 1.5 | 1.42 |
| 1704.5 | 0.46 | 1.78 | 1.53 | 1.72 | 2.24 | 4.55 | 1.51 | 1.42 |
| 1705 | 0.46 | 1.79 | 1.54 | 1.72 | 2.25 | 4.56 | 1.51 | 1.43 |
| 1705.5 | 0.46 | 1.79 | 1.54 | 1.72 | 2.25 | 4.56 | 1.52 | 1.43 |
| 1706 | 0.46 | 1.8 | 1.54 | 1.73 | 2.25 | 4.57 | 1.52 | 1.44 |
| 1706.5 | 0.46 | 1.8 | 1.55 | 1.73 | 2.26 | 4.58 | 1.53 | 1.44 |
| 1707 | 0.46 | 1.81 | 1.55 | 1.74 | 2.26 | 4.58 | 1.53 | 1.45 |
| 1707.5 | 0.46 | 1.81 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.45 |
| 1708 | 0.46 | 1.82 | 1.56 | 1.75 | 2.28 | 4.6 | 1.54 | 1.46 |
| 1708.5 | 0.46 | 1.82 | 1.57 | 1.75 | 2.28 | 4.61 | 1.55 | 1.46 |
| 1709 | 0.46 | 1.83 | 1.57 | 1.76 | 2.29 | 4.61 | 1.55 | 1.47 |
| 1709.5 | 0.46 | 1.84 | 1.58 | 1.76 | 2.29 | 4.62 | 1.56 | 1.47 |
| 1710 | 0.46 | 1.84 | 1.58 | 1.76 | 2.3 | 4.63 | 1.56 | 1.48 |
| 1710.5 | 0.46 | 1.85 | 1.59 | 1.77 | 2.3 | 4.64 | 1.56 | 1.48 |
| 1711 | 0.46 | 1.85 | 1.59 | 1.77 | 2.31 | 4.65 | 1.57 | 1.49 |
| 1711.5 | 0.46 | 1.86 | 1.59 | 1.77 | 2.31 | 4.65 | 1.57 | 1.49 |
| 1712 | 0.46 | 1.86 | 1.6 | 1.78 | 2.31 | 4.66 | 1.58 | 1.49 |
| 1712.5 | 0.46 | 1.86 | 1.6 | 1.78 | 2.32 | 4.66 | 1.58 | 1.5 |
| 1713 | 0.46 | 1.86 | 1.6 | 1.78 | 2.32 | 4.67 | 1.58 | 1.5 |
| 1713.5 | 0.46 | 1.87 | 1.6 | 1.78 | 2.32 | 4.67 | 1.58 | 1.5 |
| 1714 | 0.46 | 1.87 | 1.61 | 1.78 | 2.32 | 4.67 | 1.58 | 1.5 |
| 1714.5 | 0.46 | 1.87 | 1.61 | 1.78 | 2.32 | 4.67 | 1.59 | 1.5 |
| 1715 | 0.46 | 1.87 | 1.61 | 1.78 | 2.32 | 4.67 | 1.59 | 1.5 |
| 1715.5 | 0.46 | 1.87 | 1.61 | 1.78 | 2.32 | 4.67 | 1.59 | 1.5 |
| 1716 | 0.46 | 1.87 | 1.61 | 1.78 | 2.32 | 4.67 | 1.59 | 1.5 |
| 1716.5 | 0.46 | 1.87 | 1.61 | 1.78 | 2.32 | 4.67 | 1.59 | 1.5 |
| 1717 | 0.46 | 1.87 | 1.61 | 1.78 | 2.32 | 4.67 | 1.58 | 1.5 |
| 1717.5 | 0.46 | 1.86 | 1.61 | 1.78 | 2.32 | 4.66 | 1.58 | 1.5 |
| 1718 | 0.46 | 1.86 | 1.6 | 1.78 | 2.32 | 4.66 | 1.58 | 1.5 |
| 1718.5 | 0.46 | 1.86 | 1.6 | 1.78 | 2.31 | 4.66 | 1.58 | 1.5 |
| 1719 | 0.46 | 1.86 | 1.6 | 1.78 | 2.31 | 4.65 | 1.58 | 1.5 |
| 1719.5 | 0.46 | 1.86 | 1.6 | 1.77 | 2.31 | 4.65 | 1.57 | 1.5 |
| 1720 | 0.46 | 1.85 | 1.59 | 1.77 | 2.3 | 4.65 | 1.57 | 1.49 |
| 1720.5 | 0.46 | 1.85 | 1.59 | 1.77 | 2.3 | 4.64 | 1.57 | 1.49 |
| 1721 | 0.46 | 1.85 | 1.59 | 1.77 | 2.3 | 4.64 | 1.57 | 1.49 |
| 1721.5 | 0.46 | 1.84 | 1.59 | 1.76 | 2.29 | 4.63 | 1.56 | 1.49 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1722 | 0.46 | 1.84 | 1.58 | 1.76 | 2.29 | 4.63 | 1.56 | 1.48 |
| 1722.5 | 0.46 | 1.84 | 1.58 | 1.76 | 2.29 | 4.62 | 1.56 | 1.48 |
| 1723 | 0.46 | 1.83 | 1.58 | 1.76 | 2.28 | 4.62 | 1.56 | 1.48 |
| 1723.5 | 0.46 | 1.83 | 1.58 | 1.75 | 2.28 | 4.62 | 1.55 | 1.47 |
| 1724 | 0.46 | 1.83 | 1.57 | 1.75 | 2.28 | 4.61 | 1.55 | 1.47 |
| 1724.5 | 0.46 | 1.82 | 1.57 | 1.75 | 2.28 | 4.61 | 1.55 | 1.47 |
| 1725 | 0.46 | 1.82 | 1.57 | 1.74 | 2.27 | 4.6 | 1.54 | 1.47 |
| 1725.5 | 0.46 | 1.82 | 1.56 | 1.74 | 2.27 | 4.6 | 1.54 | 1.46 |
| 1726 | 0.46 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.46 |
| 1726.5 | 0.46 | 1.81 | 1.56 | 1.73 | 2.26 | 4.58 | 1.54 | 1.46 |
| 1727 | 0.46 | 1.81 | 1.56 | 1.73 | 2.26 | 4.58 | 1.53 | 1.45 |
| 1727.5 | 0.46 | 1.81 | 1.55 | 1.73 | 2.26 | 4.57 | 1.53 | 1.45 |
| 1728 | 0.46 | 1.81 | 1.55 | 1.73 | 2.25 | 4.57 | 1.53 | 1.45 |
| 1728.5 | 0.46 | 1.8 | 1.55 | 1.72 | 2.25 | 4.56 | 1.52 | 1.45 |
| 1729 | 0.46 | 1.8 | 1.54 | 1.72 | 2.25 | 4.56 | 1.52 | 1.44 |
| 1729.5 | 0.46 | 1.8 | 1.54 | 1.72 | 2.24 | 4.55 | 1.52 | 1.44 |
| 1730 | 0.46 | 1.79 | 1.54 | 1.72 | 2.24 | 4.55 | 1.52 | 1.44 |
| 1730.5 | 0.46 | 1.79 | 1.53 | 1.71 | 2.24 | 4.55 | 1.51 | 1.43 |
| 1731 | 0.46 | 1.79 | 1.53 | 1.71 | 2.24 | 4.54 | 1.51 | 1.43 |
| 1731.5 | 0.46 | 1.79 | 1.53 | 1.71 | 2.23 | 4.54 | 1.51 | 1.43 |
| 1732 | 0.46 | 1.79 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.43 |
| 1732.5 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.43 |
| 1733 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.52 | 1.51 | 1.43 |
| 1733.5 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.52 | 1.51 | 1.43 |
| 1734 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.52 | 1.5 | 1.43 |
| 1734.5 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.52 | 1.5 | 1.42 |
| 1735 | 0.46 | 1.78 | 1.53 | 1.7 | 2.23 | 4.52 | 1.5 | 1.42 |
| 1735.5 | 0.46 | 1.78 | 1.53 | 1.7 | 2.23 | 4.52 | 1.5 | 1.42 |
| 1736 | 0.46 | 1.78 | 1.53 | 1.7 | 2.23 | 4.52 | 1.5 | 1.43 |
| 1736.5 | 0.46 | 1.78 | 1.53 | 1.7 | 2.23 | 4.52 | 1.5 | 1.43 |
| 1737 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.52 | 1.5 | 1.43 |
| 1737.5 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.52 | 1.5 | 1.43 |
| 1738 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.43 |
| 1738.5 | 0.46 | 1.78 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.43 |
| 1739 | 0.46 | 1.79 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.43 |
| 1739.5 | 0.46 | 1.79 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.43 |
| 1740 | 0.46 | 1.79 | 1.53 | 1.71 | 2.24 | 4.53 | 1.51 | 1.43 |
| 1740.5 | 0.46 | 1.79 | 1.53 | 1.71 | 2.24 | 4.54 | 1.51 | 1.44 |
| 1741 | 0.46 | 1.79 | 1.54 | 1.71 | 2.24 | 4.54 | 1.51 | 1.44 |
| 1741.5 | 0.46 | 1.79 | 1.54 | 1.72 | 2.24 | 4.54 | 1.52 | 1.44 |
| 1742 | 0.46 | 1.8 | 1.54 | 1.72 | 2.25 | 4.54 | 1.52 | 1.44 |
| 1742.5 | 0.46 | 1.8 | 1.54 | 1.72 | 2.25 | 4.55 | 1.52 | 1.44 |
| 1743 | 0.46 | 1.8 | 1.54 | 1.72 | 2.25 | 4.55 | 1.52 | 1.44 |
| 1743.5 | 0.46 | 1.8 | 1.55 | 1.72 | 2.25 | 4.55 | 1.52 | 1.45 |
| 1744 | 0.46 | 1.8 | 1.55 | 1.73 | 2.25 | 4.56 | 1.53 | 1.45 |
| 1744.5 | 0.46 | 1.81 | 1.55 | 1.73 | 2.26 | 4.57 | 1.53 | 1.45 |
| 1745 | 0.46 | 1.81 | 1.55 | 1.73 | 2.26 | 4.57 | 1.53 | 1.45 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1745.5 | 0.46 | 1.81 | 1.55 | 1.73 | 2.26 | 4.58 | 1.53 | 1.46 |
| 1746 | 0.47 | 1.81 | 1.56 | 1.74 | 2.26 | 4.58 | 1.54 | 1.46 |
| 1746.5 | 0.47 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.46 |
| 1747 | 0.47 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.46 |
| 1747.5 | 0.47 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.46 |
| 1748 | 0.47 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.47 |
| 1748.5 | 0.47 | 1.82 | 1.56 | 1.75 | 2.27 | 4.6 | 1.54 | 1.47 |
| 1749 | 0.47 | 1.83 | 1.57 | 1.75 | 2.27 | 4.6 | 1.55 | 1.47 |
| 1749.5 | 0.47 | 1.83 | 1.57 | 1.75 | 2.27 | 4.6 | 1.55 | 1.47 |
| 1750 | 0.47 | 1.83 | 1.57 | 1.75 | 2.27 | 4.6 | 1.55 | 1.47 |
| 1750.5 | 0.47 | 1.83 | 1.57 | 1.75 | 2.27 | 4.6 | 1.55 | 1.47 |
| 1751 | 0.47 | 1.83 | 1.57 | 1.75 | 2.27 | 4.6 | 1.55 | 1.47 |
| 1751.5 | 0.47 | 1.83 | 1.57 | 1.75 | 2.27 | 4.6 | 1.55 | 1.47 |
| 1752 | 0.47 | 1.83 | 1.57 | 1.75 | 2.27 | 4.6 | 1.54 | 1.47 |
| 1752.5 | 0.47 | 1.83 | 1.57 | 1.74 | 2.27 | 4.59 | 1.54 | 1.47 |
| 1753 | 0.47 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.47 |
| 1753.5 | 0.47 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.47 |
| 1754 | 0.47 | 1.82 | 1.56 | 1.74 | 2.27 | 4.59 | 1.54 | 1.46 |
| 1754.5 | 0.47 | 1.82 | 1.56 | 1.74 | 2.26 | 4.59 | 1.54 | 1.46 |
| 1755 | 0.47 | 1.82 | 1.56 | 1.74 | 2.26 | 4.58 | 1.54 | 1.46 |
| 1755.5 | 0.47 | 1.82 | 1.56 | 1.74 | 2.26 | 4.58 | 1.54 | 1.46 |
| 1756 | 0.47 | 1.81 | 1.56 | 1.74 | 2.26 | 4.58 | 1.54 | 1.46 |
| 1756.5 | 0.47 | 1.81 | 1.55 | 1.73 | 2.26 | 4.57 | 1.53 | 1.46 |
| 1757 | 0.47 | 1.81 | 1.55 | 1.73 | 2.25 | 4.57 | 1.53 | 1.46 |
| 1757.5 | 0.47 | 1.81 | 1.55 | 1.73 | 2.25 | 4.57 | 1.53 | 1.45 |
| 1758 | 0.47 | 1.8 | 1.55 | 1.73 | 2.25 | 4.56 | 1.53 | 1.45 |
| 1758.5 | 0.47 | 1.8 | 1.55 | 1.73 | 2.25 | 4.56 | 1.53 | 1.45 |
| 1759 | 0.47 | 1.8 | 1.54 | 1.72 | 2.24 | 4.56 | 1.52 | 1.45 |
| 1759.5 | 0.47 | 1.8 | 1.54 | 1.72 | 2.24 | 4.55 | 1.52 | 1.45 |
| 1760 | 0.47 | 1.79 | 1.54 | 1.72 | 2.24 | 4.55 | 1.52 | 1.44 |
| 1760.5 | 0.47 | 1.79 | 1.54 | 1.71 | 2.23 | 4.54 | 1.51 | 1.44 |
| 1761 | 0.47 | 1.79 | 1.53 | 1.71 | 2.23 | 4.54 | 1.51 | 1.44 |
| 1761.5 | 0.47 | 1.79 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.44 |
| 1762 | 0.47 | 1.78 | 1.53 | 1.71 | 2.23 | 4.53 | 1.51 | 1.43 |
| 1762.5 | 0.47 | 1.78 | 1.52 | 1.7 | 2.22 | 4.52 | 1.5 | 1.43 |
| 1763 | 0.47 | 1.78 | 1.52 | 1.7 | 2.22 | 4.52 | 1.5 | 1.43 |
| 1763.5 | 0.47 | 1.77 | 1.52 | 1.7 | 2.22 | 4.51 | 1.5 | 1.43 |
| 1764 | 0.47 | 1.77 | 1.51 | 1.7 | 2.22 | 4.51 | 1.5 | 1.42 |
| 1764.5 | 0.47 | 1.77 | 1.51 | 1.7 | 2.21 | 4.5 | 1.49 | 1.42 |
| 1765 | 0.47 | 1.76 | 1.51 | 1.69 | 2.21 | 4.5 | 1.49 | 1.42 |
| 1765.5 | 0.47 | 1.76 | 1.51 | 1.69 | 2.21 | 4.49 | 1.49 | 1.41 |
| 1766 | 0.47 | 1.76 | 1.5 | 1.69 | 2.2 | 4.49 | 1.49 | 1.41 |
| 1766.5 | 0.47 | 1.76 | 1.5 | 1.69 | 2.2 | 4.48 | 1.48 | 1.41 |
| 1767 | 0.47 | 1.76 | 1.5 | 1.69 | 2.2 | 4.48 | 1.48 | 1.41 |
| 1767.5 | 0.47 | 1.76 | 1.5 | 1.68 | 2.2 | 4.48 | 1.48 | 1.4 |
| 1768 | 0.47 | 1.75 | 1.5 | 1.68 | 2.19 | 4.47 | 1.48 | 1.4 |
| 1768.5 | 0.47 | 1.75 | 1.49 | 1.68 | 2.19 | 4.47 | 1.47 | 1.4 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1769 | 0.47 | 1.75 | 1.49 | 1.68 | 2.19 | 4.46 | 1.47 | 1.4 |
| 1769.5 | 0.47 | 1.75 | 1.49 | 1.67 | 2.19 | 4.46 | 1.47 | 1.4 |
| 1770 | 0.47 | 1.74 | 1.49 | 1.67 | 2.18 | 4.46 | 1.47 | 1.39 |
| 1770.5 | 0.47 | 1.74 | 1.48 | 1.67 | 2.18 | 4.45 | 1.47 | 1.39 |
| 1771 | 0.47 | 1.74 | 1.48 | 1.67 | 2.18 | 4.45 | 1.46 | 1.39 |
| 1771.5 | 0.47 | 1.74 | 1.48 | 1.66 | 2.18 | 4.44 | 1.46 | 1.39 |
| 1772 | 0.47 | 1.73 | 1.48 | 1.66 | 2.17 | 4.44 | 1.46 | 1.39 |
| 1772.5 | 0.47 | 1.73 | 1.48 | 1.66 | 2.17 | 4.43 | 1.46 | 1.38 |
| 1773 | 0.47 | 1.73 | 1.47 | 1.66 | 2.17 | 4.43 | 1.45 | 1.38 |
| 1773.5 | 0.47 | 1.73 | 1.47 | 1.66 | 2.17 | 4.42 | 1.45 | 1.38 |
| 1774 | 0.47 | 1.72 | 1.47 | 1.65 | 2.17 | 4.42 | 1.45 | 1.38 |
| 1774.5 | 0.47 | 1.72 | 1.47 | 1.65 | 2.16 | 4.41 | 1.45 | 1.38 |
| 1775 | 0.47 | 1.72 | 1.47 | 1.65 | 2.16 | 4.41 | 1.45 | 1.38 |
| 1775.5 | 0.47 | 1.72 | 1.47 | 1.65 | 2.16 | 4.41 | 1.44 | 1.37 |
| 1776 | 0.47 | 1.72 | 1.47 | 1.65 | 2.16 | 4.41 | 1.44 | 1.37 |
| 1776.5 | 0.47 | 1.72 | 1.46 | 1.65 | 2.16 | 4.4 | 1.44 | 1.37 |
| 1777 | 0.47 | 1.71 | 1.46 | 1.64 | 2.16 | 4.4 | 1.44 | 1.37 |
| 1777.5 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.4 | 1.44 | 1.37 |
| 1778 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.4 | 1.44 | 1.37 |
| 1778.5 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.4 | 1.43 | 1.37 |
| 1779 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.4 | 1.43 | 1.36 |
| 1779.5 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.4 | 1.43 | 1.36 |
| 1780 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.4 | 1.43 | 1.36 |
| 1780.5 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.39 | 1.43 | 1.36 |
| 1781 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.39 | 1.43 | 1.36 |
| 1781.5 | 0.47 | 1.71 | 1.46 | 1.64 | 2.15 | 4.39 | 1.43 | 1.36 |
| 1782 | 0.47 | 1.71 | 1.46 | 1.63 | 2.15 | 4.39 | 1.43 | 1.36 |
| 1782.5 | 0.47 | 1.71 | 1.45 | 1.63 | 2.14 | 4.38 | 1.43 | 1.36 |
| 1783 | 0.47 | 1.71 | 1.45 | 1.63 | 2.14 | 4.38 | 1.43 | 1.36 |
| 1783.5 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.43 | 1.36 |
| 1784 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.43 | 1.36 |
| 1784.5 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.43 | 1.36 |
| 1785 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.43 | 1.36 |
| 1785.5 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.42 | 1.36 |
| 1786 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.42 | 1.36 |
| 1786.5 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.42 | 1.35 |
| 1787 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.42 | 1.35 |
| 1787.5 | 0.47 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.42 | 1.35 |
| 1788 | 0.48 | 1.7 | 1.45 | 1.63 | 2.14 | 4.38 | 1.42 | 1.35 |
| 1788.5 | 0.48 | 1.7 | 1.44 | 1.63 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1789 | 0.48 | 1.69 | 1.44 | 1.63 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1789.5 | 0.48 | 1.69 | 1.44 | 1.63 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1790 | 0.48 | 1.69 | 1.44 | 1.63 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1790.5 | 0.48 | 1.69 | 1.44 | 1.63 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1791 | 0.48 | 1.69 | 1.44 | 1.63 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1791.5 | 0.48 | 1.69 | 1.44 | 1.62 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1792 | 0.48 | 1.69 | 1.44 | 1.62 | 2.13 | 4.38 | 1.42 | 1.35 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1792.5 | 0.48 | 1.69 | 1.44 | 1.62 | 2.13 | 4.38 | 1.42 | 1.35 |
| 1793 | 0.48 | 1.69 | 1.44 | 1.62 | 2.13 | 4.37 | 1.42 | 1.35 |
| 1793.5 | 0.48 | 1.69 | 1.44 | 1.62 | 2.13 | 4.37 | 1.42 | 1.35 |
| 1794 | 0.48 | 1.69 | 1.44 | 1.62 | 2.13 | 4.37 | 1.42 | 1.35 |
| 1794.5 | 0.48 | 1.69 | 1.44 | 1.62 | 2.13 | 4.37 | 1.42 | 1.35 |
| 1795 | 0.48 | 1.69 | 1.44 | 1.62 | 2.12 | 4.37 | 1.41 | 1.35 |
| 1795.5 | 0.48 | 1.69 | 1.44 | 1.62 | 2.12 | 4.37 | 1.41 | 1.35 |
| 1796 | 0.48 | 1.69 | 1.44 | 1.62 | 2.12 | 4.37 | 1.41 | 1.35 |
| 1796.5 | 0.48 | 1.69 | 1.44 | 1.62 | 2.12 | 4.36 | 1.41 | 1.35 |
| 1797 | 0.48 | 1.69 | 1.44 | 1.62 | 2.12 | 4.36 | 1.41 | 1.34 |
| 1797.5 | 0.48 | 1.69 | 1.43 | 1.62 | 2.12 | 4.36 | 1.41 | 1.34 |
| 1798 | 0.48 | 1.69 | 1.43 | 1.62 | 2.12 | 4.36 | 1.41 | 1.34 |
| 1798.5 | 0.48 | 1.69 | 1.43 | 1.62 | 2.12 | 4.36 | 1.41 | 1.34 |
| 1799 | 0.48 | 1.68 | 1.43 | 1.62 | 2.12 | 4.35 | 1.41 | 1.34 |
| 1799.5 | 0.48 | 1.68 | 1.43 | 1.62 | 2.12 | 4.35 | 1.41 | 1.34 |
| 1800 | 0.48 | 1.68 | 1.43 | 1.62 | 2.12 | 4.35 | 1.41 | 1.34 |
| 1800.5 | 0.48 | 1.68 | 1.43 | 1.62 | 2.12 | 4.35 | 1.41 | 1.34 |
| 1801 | 0.48 | 1.68 | 1.43 | 1.62 | 2.11 | 4.35 | 1.41 | 1.34 |
| 1801.5 | 0.48 | 1.68 | 1.43 | 1.61 | 2.11 | 4.34 | 1.41 | 1.34 |
| 1802 | 0.48 | 1.68 | 1.43 | 1.61 | 2.11 | 4.34 | 1.41 | 1.34 |
| 1802.5 | 0.48 | 1.68 | 1.43 | 1.61 | 2.11 | 4.34 | 1.41 | 1.34 |
| 1803 | 0.48 | 1.68 | 1.43 | 1.61 | 2.11 | 4.34 | 1.4 | 1.34 |
| 1803.5 | 0.48 | 1.68 | 1.43 | 1.61 | 2.11 | 4.34 | 1.4 | 1.34 |
| 1804 | 0.48 | 1.68 | 1.43 | 1.61 | 2.11 | 4.34 | 1.4 | 1.34 |
| 1804.5 | 0.48 | 1.68 | 1.43 | 1.61 | 2.1 | 4.34 | 1.4 | 1.34 |
| 1805 | 0.48 | 1.68 | 1.43 | 1.61 | 2.1 | 4.34 | 1.4 | 1.34 |
| 1805.5 | 0.48 | 1.68 | 1.42 | 1.61 | 2.1 | 4.34 | 1.4 | 1.33 |
| 1806 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.33 | 1.4 | 1.33 |
| 1806.5 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.33 | 1.4 | 1.33 |
| 1807 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.33 | 1.4 | 1.33 |
| 1807.5 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.33 | 1.4 | 1.33 |
| 1808 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.33 | 1.4 | 1.33 |
| 1808.5 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.33 | 1.4 | 1.33 |
| 1809 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.33 | 1.4 | 1.33 |
| 1809.5 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.32 | 1.4 | 1.33 |
| 1810 | 0.48 | 1.67 | 1.42 | 1.61 | 2.1 | 4.32 | 1.4 | 1.33 |
| 1810.5 | 0.48 | 1.67 | 1.42 | 1.6 | 2.1 | 4.32 | 1.4 | 1.33 |
| 1811 | 0.48 | 1.67 | 1.42 | 1.6 | 2.1 | 4.32 | 1.4 | 1.33 |
| 1811.5 | 0.48 | 1.67 | 1.42 | 1.6 | 2.1 | 4.32 | 1.4 | 1.33 |
| 1812 | 0.48 | 1.67 | 1.42 | 1.6 | 2.1 | 4.32 | 1.4 | 1.33 |
| 1812.5 | 0.48 | 1.67 | 1.42 | 1.6 | 2.1 | 4.32 | 1.39 | 1.33 |
| 1813 | 0.48 | 1.67 | 1.42 | 1.6 | 2.1 | 4.32 | 1.39 | 1.33 |
| 1813.5 | 0.48 | 1.67 | 1.42 | 1.6 | 2.1 | 4.32 | 1.39 | 1.33 |
| 1814 | 0.48 | 1.66 | 1.42 | 1.6 | 2.09 | 4.32 | 1.39 | 1.33 |
| 1814.5 | 0.48 | 1.66 | 1.42 | 1.6 | 2.09 | 4.32 | 1.39 | 1.33 |
| 1815 | 0.48 | 1.66 | 1.42 | 1.6 | 2.09 | 4.32 | 1.39 | 1.33 |
| 1815.5 | 0.48 | 1.66 | 1.41 | 1.6 | 2.09 | 4.31 | 1.39 | 1.33 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1816 | 0.48 | 1.66 | 1.41 | 1.6 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1816.5 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1817 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1817.5 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1818 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1818.5 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1819 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1819.5 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1820 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1820.5 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1821 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1821.5 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.39 | 1.32 |
| 1822 | 0.48 | 1.66 | 1.41 | 1.59 | 2.09 | 4.31 | 1.38 | 1.32 |
| 1822.5 | 0.48 | 1.65 | 1.41 | 1.59 | 2.08 | 4.31 | 1.38 | 1.32 |
| 1823 | 0.48 | 1.65 | 1.41 | 1.59 | 2.08 | 4.3 | 1.38 | 1.32 |
| 1823.5 | 0.48 | 1.65 | 1.41 | 1.59 | 2.08 | 4.3 | 1.38 | 1.32 |
| 1824 | 0.48 | 1.65 | 1.41 | 1.59 | 2.08 | 4.3 | 1.38 | 1.32 |
| 1824.5 | 0.48 | 1.65 | 1.4 | 1.59 | 2.08 | 4.3 | 1.38 | 1.32 |
| 1825 | 0.48 | 1.65 | 1.4 | 1.59 | 2.08 | 4.3 | 1.38 | 1.32 |
| 1825.5 | 0.48 | 1.65 | 1.4 | 1.59 | 2.08 | 4.3 | 1.38 | 1.32 |
| 1826 | 0.48 | 1.65 | 1.4 | 1.59 | 2.08 | 4.3 | 1.38 | 1.32 |
| 1826.5 | 0.48 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.32 |
| 1827 | 0.48 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.32 |
| 1827.5 | 0.48 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.31 |
| 1828 | 0.48 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.31 |
| 1828.5 | 0.48 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.31 |
| 1829 | 0.48 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.31 |
| 1829.5 | 0.49 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.31 |
| 1830 | 0.49 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.31 |
| 1830.5 | 0.49 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.38 | 1.31 |
| 1831 | 0.49 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.37 | 1.31 |
| 1831.5 | 0.49 | 1.65 | 1.4 | 1.58 | 2.08 | 4.29 | 1.37 | 1.31 |
| 1832 | 0.49 | 1.65 | 1.4 | 1.58 | 2.07 | 4.29 | 1.37 | 1.31 |
| 1832.5 | 0.49 | 1.64 | 1.4 | 1.58 | 2.07 | 4.29 | 1.37 | 1.31 |
| 1833 | 0.49 | 1.64 | 1.4 | 1.58 | 2.07 | 4.29 | 1.37 | 1.31 |
| 1833.5 | 0.49 | 1.64 | 1.4 | 1.58 | 2.07 | 4.29 | 1.37 | 1.31 |
| 1834 | 0.49 | 1.64 | 1.4 | 1.58 | 2.07 | 4.29 | 1.37 | 1.31 |
| 1834.5 | 0.49 | 1.64 | 1.4 | 1.57 | 2.07 | 4.29 | 1.37 | 1.31 |
| 1835 | 0.49 | 1.64 | 1.39 | 1.57 | 2.07 | 4.29 | 1.37 | 1.31 |
| 1835.5 | 0.49 | 1.64 | 1.39 | 1.57 | 2.07 | 4.28 | 1.37 | 1.31 |
| 1836 | 0.49 | 1.64 | 1.39 | 1.57 | 2.07 | 4.28 | 1.37 | 1.31 |
| 1836.5 | 0.49 | 1.64 | 1.39 | 1.57 | 2.07 | 4.28 | 1.37 | 1.31 |
| 1837 | 0.49 | 1.64 | 1.39 | 1.57 | 2.06 | 4.28 | 1.37 | 1.31 |
| 1837.5 | 0.49 | 1.64 | 1.39 | 1.57 | 2.06 | 4.28 | 1.37 | 1.31 |
| 1838 | 0.49 | 1.64 | 1.39 | 1.57 | 2.06 | 4.28 | 1.37 | 1.31 |
| 1838.5 | 0.49 | 1.64 | 1.39 | 1.57 | 2.06 | 4.28 | 1.37 | 1.31 |
| 1839 | 0.49 | 1.64 | 1.39 | 1.57 | 2.06 | 4.27 | 1.37 | 1.31 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1839.5 | 0.49 | 1.64 | 1.39 | 1.57 | 2.06 | 4.27 | 1.37 | 1.31 |
| 1840 | 0.49 | 1.64 | 1.39 | 1.57 | 2.06 | 4.27 | 1.37 | 1.31 |
| 1840.5 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.27 | 1.37 | 1.31 |
| 1841 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.27 | 1.37 | 1.31 |
| 1841.5 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.27 | 1.37 | 1.31 |
| 1842 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.27 | 1.37 | 1.31 |
| 1842.5 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.27 | 1.36 | 1.31 |
| 1843 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.27 | 1.36 | 1.3 |
| 1843.5 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.27 | 1.36 | 1.3 |
| 1844 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.26 | 1.36 | 1.3 |
| 1844.5 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.26 | 1.36 | 1.3 |
| 1845 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.26 | 1.36 | 1.3 |
| 1845.5 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.26 | 1.36 | 1.3 |
| 1846 | 0.49 | 1.63 | 1.39 | 1.57 | 2.06 | 4.26 | 1.36 | 1.3 |
| 1846.5 | 0.49 | 1.63 | 1.39 | 1.57 | 2.05 | 4.26 | 1.36 | 1.3 |
| 1847 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.26 | 1.36 | 1.3 |
| 1847.5 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.26 | 1.36 | 1.3 |
| 1848 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.26 | 1.36 | 1.3 |
| 1848.5 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.25 | 1.36 | 1.3 |
| 1849 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.25 | 1.36 | 1.3 |
| 1849.5 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.25 | 1.36 | 1.3 |
| 1850 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.25 | 1.36 | 1.3 |
| 1850.5 | 0.49 | 1.63 | 1.38 | 1.56 | 2.05 | 4.25 | 1.36 | 1.3 |
| 1851 | 0.49 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.36 | 1.3 |
| 1851.5 | 0.49 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.35 | 1.3 |
| 1852 | 0.49 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.35 | 1.29 |
| 1852.5 | 0.49 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.35 | 1.29 |
| 1853 | 0.49 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.35 | 1.29 |
| 1853.5 | 0.49 | 1.62 | 1.37 | 1.56 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1854 | 0.49 | 1.62 | 1.37 | 1.55 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1854.5 | 0.49 | 1.62 | 1.37 | 1.55 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1855 | 0.49 | 1.62 | 1.37 | 1.55 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1855.5 | 0.49 | 1.62 | 1.37 | 1.55 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1856 | 0.49 | 1.62 | 1.37 | 1.55 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1856.5 | 0.49 | 1.62 | 1.37 | 1.55 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1857 | 0.49 | 1.61 | 1.37 | 1.55 | 2.04 | 4.23 | 1.35 | 1.29 |
| 1857.5 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.23 | 1.35 | 1.29 |
| 1858 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.23 | 1.35 | 1.29 |
| 1858.5 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.35 | 1.29 |
| 1859 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.34 | 1.29 |
| 1859.5 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.34 | 1.29 |
| 1860 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.34 | 1.29 |
| 1860.5 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.34 | 1.29 |
| 1861 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.34 | 1.29 |
| 1861.5 | 0.49 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.34 | 1.28 |
| 1862 | 0.49 | 1.61 | 1.37 | 1.55 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1862.5 | 0.49 | 1.61 | 1.36 | 1.55 | 2.02 | 4.21 | 1.34 | 1.28 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1863 | 0.49 | 1.61 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1863.5 | 0.49 | 1.61 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1864 | 0.49 | 1.61 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1864.5 | 0.49 | 1.61 | 1.36 | 1.54 | 2.02 | 4.2 | 1.34 | 1.28 |
| 1865 | 0.49 | 1.61 | 1.36 | 1.54 | 2.02 | 4.2 | 1.34 | 1.28 |
| 1865.5 | 0.49 | 1.61 | 1.36 | 1.54 | 2.02 | 4.2 | 1.34 | 1.28 |
| 1866 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.2 | 1.34 | 1.28 |
| 1866.5 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.2 | 1.34 | 1.28 |
| 1867 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.2 | 1.34 | 1.28 |
| 1867.5 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.2 | 1.34 | 1.28 |
| 1868 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1868.5 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1869 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1869.5 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1870 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1870.5 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.21 | 1.34 | 1.28 |
| 1871 | 0.49 | 1.6 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1871.5 | 0.50 | 1.6 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1872 | 0.50 | 1.6 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1872.5 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1873 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1873.5 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1874 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1874.5 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1875 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1875.5 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1876 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1876.5 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1877 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1877.5 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.28 |
| 1878 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1878.5 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1879 | 0.50 | 1.61 | 1.36 | 1.54 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1879.5 | 0.50 | 1.61 | 1.37 | 1.54 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1880 | 0.50 | 1.61 | 1.37 | 1.54 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1880.5 | 0.50 | 1.61 | 1.37 | 1.54 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1881 | 0.50 | 1.61 | 1.37 | 1.54 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1881.5 | 0.50 | 1.61 | 1.37 | 1.55 | 2.02 | 4.22 | 1.34 | 1.29 |
| 1882 | 0.50 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.34 | 1.29 |
| 1882.5 | 0.50 | 1.61 | 1.37 | 1.55 | 2.03 | 4.22 | 1.35 | 1.29 |
| 1883 | 0.50 | 1.61 | 1.37 | 1.55 | 2.03 | 4.23 | 1.35 | 1.3 |
| 1883.5 | 0.50 | 1.61 | 1.37 | 1.55 | 2.03 | 4.23 | 1.35 | 1.3 |
| 1884 | 0.50 | 1.62 | 1.37 | 1.55 | 2.03 | 4.23 | 1.35 | 1.3 |
| 1884.5 | 0.50 | 1.62 | 1.37 | 1.55 | 2.03 | 4.23 | 1.35 | 1.3 |
| 1885 | 0.50 | 1.62 | 1.38 | 1.55 | 2.03 | 4.24 | 1.35 | 1.3 |
| 1885.5 | 0.50 | 1.62 | 1.38 | 1.55 | 2.03 | 4.24 | 1.35 | 1.3 |
| 1886 | 0.50 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.36 | 1.31 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1886.5 | 0.50 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.36 | 1.31 |
| 1887 | 0.50 | 1.62 | 1.38 | 1.56 | 2.04 | 4.24 | 1.36 | 1.31 |
| 1887.5 | 0.50 | 1.63 | 1.38 | 1.56 | 2.04 | 4.25 | 1.36 | 1.31 |
| 1888 | 0.50 | 1.63 | 1.39 | 1.56 | 2.04 | 4.25 | 1.37 | 1.31 |
| 1888.5 | 0.50 | 1.63 | 1.39 | 1.56 | 2.04 | 4.25 | 1.37 | 1.32 |
| 1889 | 0.50 | 1.63 | 1.39 | 1.57 | 2.05 | 4.25 | 1.37 | 1.32 |
| 1889.5 | 0.50 | 1.63 | 1.39 | 1.57 | 2.05 | 4.26 | 1.37 | 1.32 |
| 1890 | 0.50 | 1.63 | 1.39 | 1.57 | 2.05 | 4.26 | 1.37 | 1.32 |
| 1890.5 | 0.50 | 1.64 | 1.39 | 1.57 | 2.05 | 4.26 | 1.37 | 1.32 |
| 1891 | 0.50 | 1.64 | 1.4 | 1.57 | 2.05 | 4.27 | 1.38 | 1.32 |
| 1891.5 | 0.50 | 1.64 | 1.4 | 1.57 | 2.05 | 4.27 | 1.38 | 1.33 |
| 1892 | 0.50 | 1.64 | 1.4 | 1.58 | 2.05 | 4.27 | 1.38 | 1.33 |
| 1892.5 | 0.50 | 1.64 | 1.4 | 1.58 | 2.06 | 4.28 | 1.38 | 1.33 |
| 1893 | 0.50 | 1.64 | 1.4 | 1.58 | 2.06 | 4.28 | 1.38 | 1.33 |
| 1893.5 | 0.50 | 1.65 | 1.4 | 1.58 | 2.06 | 4.28 | 1.38 | 1.33 |
| 1894 | 0.50 | 1.65 | 1.4 | 1.58 | 2.06 | 4.29 | 1.38 | 1.33 |
| 1894.5 | 0.50 | 1.65 | 1.4 | 1.58 | 2.06 | 4.29 | 1.39 | 1.33 |
| 1895 | 0.50 | 1.65 | 1.4 | 1.58 | 2.06 | 4.29 | 1.39 | 1.33 |
| 1895.5 | 0.50 | 1.65 | 1.41 | 1.58 | 2.06 | 4.29 | 1.39 | 1.34 |
| 1896 | 0.50 | 1.65 | 1.41 | 1.58 | 2.06 | 4.3 | 1.39 | 1.34 |
| 1896.5 | 0.50 | 1.65 | 1.41 | 1.59 | 2.06 | 4.3 | 1.39 | 1.34 |
| 1897 | 0.50 | 1.66 | 1.41 | 1.59 | 2.06 | 4.3 | 1.39 | 1.34 |
| 1897.5 | 0.50 | 1.66 | 1.41 | 1.59 | 2.07 | 4.3 | 1.39 | 1.34 |
| 1898 | 0.50 | 1.66 | 1.41 | 1.59 | 2.07 | 4.3 | 1.39 | 1.34 |
| 1898.5 | 0.50 | 1.66 | 1.41 | 1.59 | 2.07 | 4.31 | 1.39 | 1.34 |
| 1899 | 0.50 | 1.66 | 1.42 | 1.59 | 2.07 | 4.31 | 1.4 | 1.35 |
| 1899.5 | 0.50 | 1.66 | 1.42 | 1.59 | 2.07 | 4.31 | 1.4 | 1.35 |
| 1900 | 0.50 | 1.66 | 1.42 | 1.59 | 2.07 | 4.31 | 1.4 | 1.35 |
| 1900.5 | 0.50 | 1.67 | 1.42 | 1.59 | 2.07 | 4.32 | 1.4 | 1.35 |
| 1901 | 0.50 | 1.67 | 1.42 | 1.59 | 2.08 | 4.32 | 1.4 | 1.35 |
| 1901.5 | 0.50 | 1.67 | 1.42 | 1.6 | 2.08 | 4.32 | 1.4 | 1.35 |
| 1902 | 0.50 | 1.67 | 1.42 | 1.6 | 2.08 | 4.32 | 1.4 | 1.36 |
| 1902.5 | 0.50 | 1.67 | 1.42 | 1.6 | 2.08 | 4.33 | 1.4 | 1.36 |
| 1903 | 0.50 | 1.67 | 1.43 | 1.6 | 2.08 | 4.33 | 1.41 | 1.36 |
| 1903.5 | 0.50 | 1.67 | 1.43 | 1.6 | 2.08 | 4.33 | 1.41 | 1.36 |
| 1904 | 0.50 | 1.67 | 1.43 | 1.6 | 2.08 | 4.33 | 1.41 | 1.36 |
| 1904.5 | 0.50 | 1.68 | 1.43 | 1.6 | 2.08 | 4.34 | 1.41 | 1.36 |
| 1905 | 0.50 | 1.68 | 1.43 | 1.6 | 2.09 | 4.34 | 1.41 | 1.37 |
| 1905.5 | 0.50 | 1.68 | 1.43 | 1.61 | 2.09 | 4.34 | 1.41 | 1.37 |
| 1906 | 0.50 | 1.68 | 1.43 | 1.61 | 2.09 | 4.35 | 1.42 | 1.37 |
| 1906.5 | 0.50 | 1.68 | 1.44 | 1.61 | 2.09 | 4.35 | 1.42 | 1.37 |
| 1907 | 0.50 | 1.68 | 1.44 | 1.61 | 2.09 | 4.35 | 1.42 | 1.37 |
| 1907.5 | 0.50 | 1.68 | 1.44 | 1.61 | 2.1 | 4.35 | 1.42 | 1.37 |
| 1908 | 0.50 | 1.69 | 1.44 | 1.62 | 2.1 | 4.36 | 1.42 | 1.38 |
| 1908.5 | 0.50 | 1.69 | 1.44 | 1.62 | 2.1 | 4.36 | 1.42 | 1.38 |
| 1909 | 0.50 | 1.69 | 1.44 | 1.62 | 2.1 | 4.36 | 1.43 | 1.38 |
| 1909.5 | 0.50 | 1.69 | 1.45 | 1.62 | 2.1 | 4.36 | 1.43 | 1.38 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1910 | 0.50 | 1.69 | 1.45 | 1.62 | 2.1 | 4.36 | 1.43 | 1.38 |
| 1910.5 | 0.50 | 1.7 | 1.45 | 1.62 | 2.1 | 4.36 | 1.43 | 1.38 |
| 1911 | 0.50 | 1.7 | 1.45 | 1.62 | 2.11 | 4.36 | 1.43 | 1.39 |
| 1911.5 | 0.50 | 1.7 | 1.45 | 1.63 | 2.11 | 4.37 | 1.43 | 1.39 |
| 1912 | 0.50 | 1.7 | 1.45 | 1.63 | 2.11 | 4.37 | 1.44 | 1.39 |
| 1912.5 | 0.50 | 1.7 | 1.45 | 1.63 | 2.11 | 4.37 | 1.44 | 1.39 |
| 1913 | 0.51 | 1.71 | 1.46 | 1.63 | 2.11 | 4.37 | 1.44 | 1.39 |
| 1913.5 | 0.51 | 1.71 | 1.46 | 1.63 | 2.11 | 4.38 | 1.44 | 1.4 |
| 1914 | 0.51 | 1.71 | 1.46 | 1.64 | 2.12 | 4.38 | 1.45 | 1.4 |
| 1914.5 | 0.51 | 1.71 | 1.46 | 1.64 | 2.12 | 4.39 | 1.45 | 1.4 |
| 1915 | 0.51 | 1.71 | 1.46 | 1.64 | 2.12 | 4.39 | 1.45 | 1.4 |
| 1915.5 | 0.51 | 1.72 | 1.46 | 1.64 | 2.12 | 4.39 | 1.45 | 1.4 |
| 1916 | 0.51 | 1.72 | 1.47 | 1.64 | 2.12 | 4.4 | 1.45 | 1.41 |
| 1916.5 | 0.51 | 1.72 | 1.47 | 1.65 | 2.13 | 4.4 | 1.46 | 1.41 |
| 1917 | 0.51 | 1.72 | 1.47 | 1.65 | 2.13 | 4.41 | 1.46 | 1.41 |
| 1917.5 | 0.51 | 1.72 | 1.47 | 1.65 | 2.13 | 4.41 | 1.46 | 1.41 |
| 1918 | 0.51 | 1.72 | 1.47 | 1.65 | 2.13 | 4.41 | 1.46 | 1.41 |
| 1918.5 | 0.51 | 1.73 | 1.48 | 1.65 | 2.13 | 4.42 | 1.46 | 1.42 |
| 1919 | 0.51 | 1.73 | 1.48 | 1.65 | 2.14 | 4.42 | 1.47 | 1.42 |
| 1919.5 | 0.51 | 1.73 | 1.48 | 1.66 | 2.14 | 4.43 | 1.47 | 1.42 |
| 1920 | 0.51 | 1.73 | 1.48 | 1.66 | 2.14 | 4.43 | 1.47 | 1.42 |
| 1920.5 | 0.51 | 1.73 | 1.48 | 1.66 | 2.14 | 4.44 | 1.47 | 1.42 |
| 1921 | 0.51 | 1.74 | 1.49 | 1.66 | 2.14 | 4.44 | 1.48 | 1.43 |
| 1921.5 | 0.51 | 1.74 | 1.49 | 1.66 | 2.15 | 4.44 | 1.48 | 1.43 |
| 1922 | 0.51 | 1.74 | 1.49 | 1.67 | 2.15 | 4.45 | 1.48 | 1.43 |
| 1922.5 | 0.51 | 1.74 | 1.49 | 1.67 | 2.15 | 4.45 | 1.48 | 1.44 |
| 1923 | 0.51 | 1.74 | 1.49 | 1.67 | 2.15 | 4.45 | 1.49 | 1.44 |
| 1923.5 | 0.51 | 1.75 | 1.5 | 1.67 | 2.15 | 4.46 | 1.49 | 1.44 |
| 1924 | 0.51 | 1.75 | 1.5 | 1.67 | 2.16 | 4.46 | 1.49 | 1.44 |
| 1924.5 | 0.51 | 1.75 | 1.5 | 1.68 | 2.16 | 4.46 | 1.49 | 1.45 |
| 1925 | 0.51 | 1.75 | 1.5 | 1.68 | 2.16 | 4.47 | 1.5 | 1.45 |
| 1925.5 | 0.51 | 1.75 | 1.5 | 1.68 | 2.16 | 4.47 | 1.5 | 1.45 |
| 1926 | 0.51 | 1.76 | 1.51 | 1.68 | 2.17 | 4.47 | 1.5 | 1.45 |
| 1926.5 | 0.51 | 1.76 | 1.51 | 1.68 | 2.17 | 4.48 | 1.5 | 1.46 |
| 1927 | 0.51 | 1.76 | 1.51 | 1.69 | 2.17 | 4.48 | 1.5 | 1.46 |
| 1927.5 | 0.51 | 1.76 | 1.51 | 1.69 | 2.17 | 4.49 | 1.51 | 1.46 |
| 1928 | 0.51 | 1.77 | 1.52 | 1.69 | 2.17 | 4.49 | 1.51 | 1.47 |
| 1928.5 | 0.51 | 1.77 | 1.52 | 1.69 | 2.18 | 4.49 | 1.51 | 1.47 |
| 1929 | 0.51 | 1.77 | 1.52 | 1.7 | 2.18 | 4.5 | 1.51 | 1.47 |
| 1929.5 | 0.51 | 1.77 | 1.52 | 1.7 | 2.18 | 4.5 | 1.52 | 1.47 |
| 1930 | 0.51 | 1.78 | 1.52 | 1.7 | 2.18 | 4.5 | 1.52 | 1.48 |
| 1930.5 | 0.51 | 1.78 | 1.53 | 1.7 | 2.18 | 4.51 | 1.52 | 1.48 |
| 1931 | 0.51 | 1.78 | 1.53 | 1.7 | 2.19 | 4.51 | 1.52 | 1.48 |
| 1931.5 | 0.51 | 1.78 | 1.53 | 1.71 | 2.19 | 4.51 | 1.52 | 1.48 |
| 1932 | 0.51 | 1.78 | 1.53 | 1.71 | 2.19 | 4.52 | 1.53 | 1.48 |
| 1932.5 | 0.51 | 1.79 | 1.53 | 1.71 | 2.19 | 4.52 | 1.53 | 1.49 |
| 1933 | 0.51 | 1.79 | 1.53 | 1.71 | 2.19 | 4.52 | 1.53 | 1.49 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1933.5 | 0.51 | 1.79 | 1.53 | 1.71 | 2.2 | 4.53 | 1.53 | 1.49 |
| 1934 | 0.51 | 1.79 | 1.54 | 1.71 | 2.2 | 4.53 | 1.53 | 1.49 |
| 1934.5 | 0.51 | 1.79 | 1.54 | 1.71 | 2.2 | 4.53 | 1.53 | 1.49 |
| 1935 | 0.51 | 1.8 | 1.54 | 1.72 | 2.2 | 4.53 | 1.54 | 1.49 |
| 1935.5 | 0.51 | 1.8 | 1.54 | 1.72 | 2.2 | 4.54 | 1.54 | 1.5 |
| 1936 | 0.51 | 1.8 | 1.54 | 1.72 | 2.2 | 4.54 | 1.54 | 1.5 |
| 1936.5 | 0.51 | 1.8 | 1.54 | 1.72 | 2.2 | 4.54 | 1.54 | 1.5 |
| 1937 | 0.51 | 1.8 | 1.54 | 1.72 | 2.21 | 4.54 | 1.54 | 1.5 |
| 1937.5 | 0.51 | 1.8 | 1.55 | 1.72 | 2.21 | 4.54 | 1.54 | 1.5 |
| 1938 | 0.51 | 1.8 | 1.55 | 1.72 | 2.21 | 4.55 | 1.54 | 1.5 |
| 1938.5 | 0.51 | 1.8 | 1.55 | 1.72 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1939 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1939.5 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1940 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1940.5 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1941 | 0.51 | 1.81 | 1.55 | 1.73 | 2.22 | 4.56 | 1.55 | 1.51 |
| 1941.5 | 0.51 | 1.81 | 1.55 | 1.73 | 2.22 | 4.56 | 1.55 | 1.51 |
| 1942 | 0.51 | 1.81 | 1.55 | 1.73 | 2.22 | 4.56 | 1.55 | 1.51 |
| 1942.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.51 |
| 1943 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1943.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1944 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1944.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1945 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1945.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1946 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1946.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1947 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1947.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.22 | 4.56 | 1.56 | 1.52 |
| 1948 | 0.51 | 1.81 | 1.56 | 1.73 | 2.21 | 4.56 | 1.56 | 1.52 |
| 1948.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.21 | 4.56 | 1.56 | 1.52 |
| 1949 | 0.51 | 1.81 | 1.56 | 1.73 | 2.21 | 4.56 | 1.56 | 1.52 |
| 1949.5 | 0.51 | 1.81 | 1.56 | 1.73 | 2.21 | 4.55 | 1.56 | 1.52 |
| 1950 | 0.51 | 1.81 | 1.56 | 1.73 | 2.21 | 4.55 | 1.55 | 1.52 |
| 1950.5 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.52 |
| 1951 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.52 |
| 1951.5 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1952 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1952.5 | 0.51 | 1.81 | 1.55 | 1.73 | 2.21 | 4.55 | 1.55 | 1.51 |
| 1953 | 0.51 | 1.81 | 1.55 | 1.72 | 2.21 | 4.54 | 1.55 | 1.51 |
| 1953.5 | 0.51 | 1.81 | 1.55 | 1.72 | 2.21 | 4.54 | 1.55 | 1.51 |
| 1954 | 0.51 | 1.81 | 1.55 | 1.72 | 2.21 | 4.54 | 1.55 | 1.51 |
| 1954.5 | 0.51 | 1.81 | 1.55 | 1.72 | 2.21 | 4.54 | 1.55 | 1.51 |
| 1955 | 0.52 | 1.81 | 1.55 | 1.72 | 2.21 | 4.54 | 1.54 | 1.51 |
| 1955.5 | 0.52 | 1.81 | 1.54 | 1.72 | 2.2 | 4.53 | 1.54 | 1.51 |
| 1956 | 0.52 | 1.8 | 1.54 | 1.72 | 2.2 | 4.53 | 1.54 | 1.5 |
| 1956.5 | 0.52 | 1.8 | 1.54 | 1.72 | 2.2 | 4.53 | 1.54 | 1.5 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1957 | 0.52 | 1.8 | 1.54 | 1.72 | 2.2 | 4.53 | 1.54 | 1.5 |
| 1957.5 | 0.52 | 1.8 | 1.54 | 1.71 | 2.2 | 4.52 | 1.54 | 1.5 |
| 1958 | 0.52 | 1.8 | 1.54 | 1.71 | 2.2 | 4.52 | 1.54 | 1.5 |
| 1958.5 | 0.52 | 1.8 | 1.54 | 1.71 | 2.2 | 4.52 | 1.54 | 1.5 |
| 1959 | 0.52 | 1.8 | 1.54 | 1.71 | 2.19 | 4.52 | 1.54 | 1.5 |
| 1959.5 | 0.52 | 1.79 | 1.53 | 1.71 | 2.19 | 4.51 | 1.53 | 1.49 |
| 1960 | 0.52 | 1.79 | 1.53 | 1.71 | 2.19 | 4.51 | 1.53 | 1.49 |
| 1960.5 | 0.52 | 1.79 | 1.53 | 1.71 | 2.19 | 4.51 | 1.53 | 1.49 |
| 1961 | 0.52 | 1.79 | 1.53 | 1.7 | 2.19 | 4.51 | 1.53 | 1.49 |
| 1961.5 | 0.52 | 1.79 | 1.53 | 1.7 | 2.18 | 4.5 | 1.53 | 1.49 |
| 1962 | 0.52 | 1.78 | 1.53 | 1.7 | 2.18 | 4.5 | 1.52 | 1.49 |
| 1962.5 | 0.52 | 1.78 | 1.52 | 1.7 | 2.18 | 4.5 | 1.52 | 1.48 |
| 1963 | 0.52 | 1.78 | 1.52 | 1.69 | 2.18 | 4.49 | 1.52 | 1.48 |
| 1963.5 | 0.52 | 1.78 | 1.52 | 1.69 | 2.17 | 4.49 | 1.52 | 1.48 |
| 1964 | 0.52 | 1.78 | 1.52 | 1.69 | 2.17 | 4.49 | 1.51 | 1.48 |
| 1964.5 | 0.52 | 1.77 | 1.52 | 1.69 | 2.17 | 4.48 | 1.51 | 1.48 |
| 1965 | 0.52 | 1.77 | 1.52 | 1.69 | 2.17 | 4.48 | 1.51 | 1.47 |
| 1965.5 | 0.52 | 1.77 | 1.51 | 1.69 | 2.17 | 4.48 | 1.51 | 1.47 |
| 1966 | 0.52 | 1.77 | 1.51 | 1.68 | 2.16 | 4.47 | 1.51 | 1.47 |
| 1966.5 | 0.52 | 1.77 | 1.51 | 1.68 | 2.16 | 4.47 | 1.51 | 1.47 |
| 1967 | 0.52 | 1.77 | 1.51 | 1.68 | 2.16 | 4.47 | 1.51 | 1.47 |
| 1967.5 | 0.52 | 1.76 | 1.51 | 1.68 | 2.16 | 4.47 | 1.5 | 1.47 |
| 1968 | 0.52 | 1.76 | 1.51 | 1.68 | 2.16 | 4.46 | 1.5 | 1.46 |
| 1968.5 | 0.52 | 1.76 | 1.51 | 1.68 | 2.16 | 4.46 | 1.5 | 1.46 |
| 1969 | 0.52 | 1.76 | 1.5 | 1.68 | 2.16 | 4.46 | 1.5 | 1.46 |
| 1969.5 | 0.52 | 1.76 | 1.5 | 1.67 | 2.15 | 4.46 | 1.5 | 1.46 |
| 1970 | 0.52 | 1.76 | 1.5 | 1.67 | 2.15 | 4.45 | 1.5 | 1.46 |
| 1970.5 | 0.52 | 1.75 | 1.5 | 1.67 | 2.15 | 4.45 | 1.49 | 1.46 |
| 1971 | 0.52 | 1.75 | 1.5 | 1.67 | 2.15 | 4.45 | 1.49 | 1.46 |
| 1971.5 | 0.52 | 1.75 | 1.5 | 1.67 | 2.15 | 4.45 | 1.49 | 1.45 |
| 1972 | 0.52 | 1.75 | 1.5 | 1.67 | 2.15 | 4.44 | 1.49 | 1.45 |
| 1972.5 | 0.52 | 1.75 | 1.49 | 1.67 | 2.14 | 4.44 | 1.49 | 1.45 |
| 1973 | 0.52 | 1.75 | 1.49 | 1.66 | 2.14 | 4.44 | 1.49 | 1.45 |
| 1973.5 | 0.52 | 1.74 | 1.49 | 1.66 | 2.14 | 4.44 | 1.49 | 1.45 |
| 1974 | 0.52 | 1.74 | 1.49 | 1.66 | 2.14 | 4.43 | 1.48 | 1.45 |
| 1974.5 | 0.52 | 1.74 | 1.49 | 1.66 | 2.14 | 4.43 | 1.48 | 1.44 |
| 1975 | 0.52 | 1.74 | 1.49 | 1.66 | 2.13 | 4.43 | 1.48 | 1.44 |
| 1975.5 | 0.52 | 1.74 | 1.48 | 1.66 | 2.13 | 4.42 | 1.48 | 1.44 |
| 1976 | 0.52 | 1.74 | 1.48 | 1.65 | 2.13 | 4.42 | 1.48 | 1.44 |
| 1976.5 | 0.52 | 1.73 | 1.48 | 1.65 | 2.13 | 4.42 | 1.48 | 1.44 |
| 1977 | 0.52 | 1.73 | 1.48 | 1.65 | 2.13 | 4.42 | 1.47 | 1.44 |
| 1977.5 | 0.52 | 1.73 | 1.48 | 1.65 | 2.12 | 4.41 | 1.47 | 1.43 |
| 1978 | 0.52 | 1.73 | 1.48 | 1.65 | 2.12 | 4.41 | 1.47 | 1.43 |
| 1978.5 | 0.52 | 1.73 | 1.47 | 1.65 | 2.12 | 4.41 | 1.47 | 1.43 |
| 1979 | 0.52 | 1.73 | 1.47 | 1.64 | 2.12 | 4.4 | 1.47 | 1.43 |
| 1979.5 | 0.52 | 1.73 | 1.47 | 1.64 | 2.12 | 4.4 | 1.47 | 1.43 |
| 1980 | 0.52 | 1.73 | 1.47 | 1.64 | 2.11 | 4.4 | 1.47 | 1.43 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1980.5 | 0.52 | 1.72 | 1.47 | 1.64 | 2.11 | 4.39 | 1.46 | 1.42 |
| 1981 | 0.52 | 1.72 | 1.47 | 1.64 | 2.11 | 4.39 | 1.46 | 1.42 |
| 1981.5 | 0.52 | 1.72 | 1.47 | 1.64 | 2.11 | 4.39 | 1.46 | 1.42 |
| 1982 | 0.52 | 1.72 | 1.46 | 1.63 | 2.11 | 4.39 | 1.46 | 1.42 |
| 1982.5 | 0.52 | 1.72 | 1.46 | 1.63 | 2.1 | 4.38 | 1.46 | 1.42 |
| 1983 | 0.52 | 1.72 | 1.46 | 1.63 | 2.1 | 4.38 | 1.46 | 1.42 |
| 1983.5 | 0.52 | 1.71 | 1.46 | 1.63 | 2.1 | 4.38 | 1.45 | 1.42 |
| 1984 | 0.52 | 1.71 | 1.46 | 1.63 | 2.1 | 4.38 | 1.45 | 1.41 |
| 1984.5 | 0.52 | 1.71 | 1.46 | 1.63 | 2.1 | 4.37 | 1.45 | 1.41 |
| 1985 | 0.52 | 1.71 | 1.46 | 1.63 | 2.1 | 4.37 | 1.45 | 1.41 |
| 1985.5 | 0.52 | 1.71 | 1.45 | 1.63 | 2.09 | 4.37 | 1.45 | 1.41 |
| 1986 | 0.52 | 1.7 | 1.45 | 1.62 | 2.09 | 4.37 | 1.45 | 1.41 |
| 1986.5 | 0.52 | 1.7 | 1.45 | 1.62 | 2.09 | 4.36 | 1.44 | 1.41 |
| 1987 | 0.52 | 1.7 | 1.45 | 1.62 | 2.09 | 4.36 | 1.44 | 1.41 |
| 1987.5 | 0.52 | 1.7 | 1.45 | 1.62 | 2.09 | 4.36 | 1.44 | 1.4 |
| 1988 | 0.52 | 1.7 | 1.45 | 1.62 | 2.09 | 4.36 | 1.44 | 1.4 |
| 1988.5 | 0.52 | 1.7 | 1.45 | 1.62 | 2.08 | 4.35 | 1.44 | 1.4 |
| 1989 | 0.52 | 1.7 | 1.45 | 1.62 | 2.08 | 4.35 | 1.44 | 1.4 |
| 1989.5 | 0.52 | 1.7 | 1.45 | 1.62 | 2.08 | 4.35 | 1.44 | 1.4 |
| 1990 | 0.52 | 1.7 | 1.45 | 1.61 | 2.08 | 4.35 | 1.44 | 1.4 |
| 1990.5 | 0.52 | 1.69 | 1.44 | 1.61 | 2.08 | 4.35 | 1.43 | 1.4 |
| 1991 | 0.52 | 1.69 | 1.44 | 1.61 | 2.08 | 4.35 | 1.43 | 1.4 |
| 1991.5 | 0.52 | 1.69 | 1.44 | 1.61 | 2.08 | 4.34 | 1.43 | 1.4 |
| 1992 | 0.52 | 1.69 | 1.44 | 1.61 | 2.08 | 4.34 | 1.43 | 1.4 |
| 1992.5 | 0.52 | 1.69 | 1.44 | 1.61 | 2.08 | 4.34 | 1.43 | 1.4 |
| 1993 | 0.52 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1993.5 | 0.52 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1994 | 0.52 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1994.5 | 0.52 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1995 | 0.52 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1995.5 | 0.52 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1996 | 0.52 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1996.5 | 0.53 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1997 | 0.53 | 1.69 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1997.5 | 0.53 | 1.7 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1998 | 0.53 | 1.7 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1998.5 | 0.53 | 1.7 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1999 | 0.53 | 1.7 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 1999.5 | 0.53 | 1.7 | 1.44 | 1.61 | 2.07 | 4.34 | 1.43 | 1.4 |
| 2000 | 0.53 | 1.7 | 1.44 | 1.61 | 2.07 | 4.35 | 1.43 | 1.4 |
| 2000.5 | 0.53 | 1.7 | 1.44 | 1.61 | 2.07 | 4.35 | 1.44 | 1.4 |
| 2001 | 0.53 | 1.7 | 1.44 | 1.62 | 2.08 | 4.35 | 1.44 | 1.4 |
| 2001.5 | 0.53 | 1.7 | 1.45 | 1.62 | 2.08 | 4.35 | 1.44 | 1.41 |
| 2002 | 0.53 | 1.71 | 1.45 | 1.62 | 2.08 | 4.36 | 1.44 | 1.41 |
| 2002.5 | 0.53 | 1.71 | 1.45 | 1.62 | 2.08 | 4.36 | 1.44 | 1.41 |
| 2003 | 0.53 | 1.71 | 1.45 | 1.62 | 2.08 | 4.36 | 1.44 | 1.41 |
| 2003.5 | 0.53 | 1.71 | 1.45 | 1.62 | 2.08 | 4.37 | 1.45 | 1.41 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2004 | 0.53 | 1.71 | 1.46 | 1.63 | 2.09 | 4.37 | 1.45 | 1.42 |
| 2004.5 | 0.53 | 1.72 | 1.46 | 1.63 | 2.09 | 4.37 | 1.45 | 1.42 |
| 2005 | 0.53 | 1.72 | 1.46 | 1.63 | 2.09 | 4.38 | 1.45 | 1.42 |
| 2005.5 | 0.53 | 1.72 | 1.46 | 1.63 | 2.09 | 4.38 | 1.46 | 1.42 |
| 2006 | 0.53 | 1.73 | 1.47 | 1.63 | 2.1 | 4.39 | 1.46 | 1.42 |
| 2006.5 | 0.53 | 1.73 | 1.47 | 1.64 | 2.1 | 4.39 | 1.46 | 1.43 |
| 2007 | 0.53 | 1.73 | 1.47 | 1.64 | 2.1 | 4.4 | 1.47 | 1.43 |
| 2007.5 | 0.53 | 1.74 | 1.48 | 1.64 | 2.1 | 4.4 | 1.47 | 1.43 |
| 2008 | 0.53 | 1.74 | 1.48 | 1.64 | 2.11 | 4.41 | 1.47 | 1.43 |
| 2008.5 | 0.53 | 1.74 | 1.48 | 1.65 | 2.11 | 4.41 | 1.47 | 1.44 |
| 2009 | 0.53 | 1.74 | 1.48 | 1.65 | 2.11 | 4.42 | 1.48 | 1.44 |
| 2009.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.48 | 1.44 |
| 2010 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.48 | 1.44 |
| 2010.5 | 0.53 | 1.75 | 1.49 | 1.66 | 2.12 | 4.43 | 1.48 | 1.45 |
| 2011 | 0.53 | 1.75 | 1.49 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2011.5 | 0.53 | 1.75 | 1.49 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2012 | 0.53 | 1.75 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2012.5 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2013 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2013.5 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2014 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2014.5 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2015 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2015.5 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2016 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2016.5 | 0.53 | 1.76 | 1.5 | 1.66 | 2.12 | 4.43 | 1.49 | 1.45 |
| 2017 | 0.53 | 1.76 | 1.49 | 1.66 | 2.11 | 4.43 | 1.49 | 1.45 |
| 2017.5 | 0.53 | 1.76 | 1.49 | 1.66 | 2.11 | 4.42 | 1.49 | 1.45 |
| 2018 | 0.53 | 1.76 | 1.49 | 1.66 | 2.11 | 4.42 | 1.49 | 1.45 |
| 2018.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.49 | 1.45 |
| 2019 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.49 | 1.45 |
| 2019.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.49 | 1.45 |
| 2020 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.48 | 1.45 |
| 2020.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.48 | 1.45 |
| 2021 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.42 | 1.48 | 1.45 |
| 2021.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.41 | 1.48 | 1.45 |
| 2022 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.41 | 1.48 | 1.45 |
| 2022.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.41 | 1.48 | 1.45 |
| 2023 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.41 | 1.48 | 1.45 |
| 2023.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.41 | 1.48 | 1.45 |
| 2024 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.41 | 1.48 | 1.45 |
| 2024.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.41 | 1.48 | 1.45 |
| 2025 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2025.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2026 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2026.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2027 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2027.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2028 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2028.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2029 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.42 | 1.48 | 1.45 |
| 2029.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.43 | 1.48 | 1.45 |
| 2030 | 0.53 | 1.75 | 1.49 | 1.65 | 2.1 | 4.43 | 1.49 | 1.45 |
| 2030.5 | 0.53 | 1.75 | 1.49 | 1.65 | 2.11 | 4.43 | 1.49 | 1.45 |
| 2031 | 0.53 | 1.76 | 1.49 | 1.65 | 2.11 | 4.43 | 1.49 | 1.46 |
| 2031.5 | 0.53 | 1.76 | 1.5 | 1.65 | 2.11 | 4.44 | 1.49 | 1.46 |
| 2032 | 0.53 | 1.76 | 1.5 | 1.66 | 2.11 | 4.44 | 1.49 | 1.46 |
| 2032.5 | 0.53 | 1.76 | 1.5 | 1.66 | 2.11 | 4.45 | 1.5 | 1.46 |
| 2033 | 0.53 | 1.77 | 1.5 | 1.66 | 2.12 | 4.45 | 1.5 | 1.47 |
| 2033.5 | 0.53 | 1.77 | 1.51 | 1.66 | 2.12 | 4.46 | 1.5 | 1.47 |
| 2034 | 0.53 | 1.77 | 1.51 | 1.67 | 2.12 | 4.46 | 1.51 | 1.47 |
| 2034.5 | 0.53 | 1.78 | 1.51 | 1.67 | 2.13 | 4.47 | 1.51 | 1.48 |
| 2035 | 0.53 | 1.78 | 1.52 | 1.68 | 2.13 | 4.48 | 1.52 | 1.48 |
| 2035.5 | 0.53 | 1.79 | 1.52 | 1.68 | 2.14 | 4.49 | 1.52 | 1.49 |
| 2036 | 0.53 | 1.79 | 1.53 | 1.68 | 2.14 | 4.5 | 1.53 | 1.49 |
| 2036.5 | 0.53 | 1.8 | 1.53 | 1.69 | 2.15 | 4.51 | 1.53 | 1.5 |
| 2037 | 0.53 | 1.8 | 1.54 | 1.7 | 2.15 | 4.52 | 1.54 | 1.51 |
| 2037.5 | 0.53 | 1.81 | 1.55 | 1.7 | 2.16 | 4.53 | 1.55 | 1.51 |
| 2038 | 0.53 | 1.82 | 1.55 | 1.71 | 2.17 | 4.55 | 1.55 | 1.52 |
| 2038.5 | 0.54 | 1.82 | 1.56 | 1.71 | 2.17 | 4.56 | 1.56 | 1.53 |
| 2039 | 0.54 | 1.83 | 1.57 | 1.72 | 2.18 | 4.57 | 1.57 | 1.54 |
| 2039.5 | 0.54 | 1.84 | 1.58 | 1.73 | 2.19 | 4.59 | 1.58 | 1.54 |
| 2040 | 0.54 | 1.85 | 1.58 | 1.74 | 2.2 | 4.6 | 1.59 | 1.55 |
| 2040.5 | 0.54 | 1.86 | 1.59 | 1.75 | 2.21 | 4.62 | 1.59 | 1.56 |
| 2041 | 0.54 | 1.87 | 1.6 | 1.75 | 2.21 | 4.63 | 1.6 | 1.57 |
| 2041.5 | 0.54 | 1.88 | 1.61 | 1.76 | 2.22 | 4.65 | 1.61 | 1.58 |
| 2042 | 0.54 | 1.89 | 1.62 | 1.77 | 2.23 | 4.66 | 1.62 | 1.59 |
| 2042.5 | 0.54 | 1.9 | 1.63 | 1.78 | 2.24 | 4.68 | 1.63 | 1.6 |
| 2043 | 0.54 | 1.91 | 1.64 | 1.79 | 2.25 | 4.7 | 1.64 | 1.61 |
| 2043.5 | 0.54 | 1.92 | 1.65 | 1.8 | 2.26 | 4.71 | 1.65 | 1.62 |
| 2044 | 0.54 | 1.93 | 1.66 | 1.81 | 2.27 | 4.73 | 1.66 | 1.63 |
| 2044.5 | 0.54 | 1.95 | 1.67 | 1.82 | 2.28 | 4.75 | 1.67 | 1.65 |
| 2045 | 0.54 | 1.96 | 1.68 | 1.83 | 2.29 | 4.77 | 1.69 | 1.66 |
| 2045.5 | 0.54 | 1.97 | 1.69 | 1.84 | 2.3 | 4.78 | 1.7 | 1.67 |
| 2046 | 0.54 | 1.98 | 1.7 | 1.85 | 2.31 | 4.8 | 1.71 | 1.68 |
| 2046.5 | 0.54 | 1.99 | 1.71 | 1.86 | 2.32 | 4.82 | 1.72 | 1.69 |
| 2047 | 0.54 | 2 | 1.72 | 1.87 | 2.34 | 4.84 | 1.73 | 1.7 |
| 2047.5 | 0.54 | 2.01 | 1.73 | 1.88 | 2.35 | 4.86 | 1.74 | 1.71 |
| 2048 | 0.54 | 2.03 | 1.74 | 1.89 | 2.36 | 4.87 | 1.75 | 1.72 |
| 2048.5 | 0.54 | 2.04 | 1.75 | 1.9 | 2.36 | 4.89 | 1.76 | 1.73 |
| 2049 | 0.54 | 2.05 | 1.76 | 1.91 | 2.37 | 4.91 | 1.77 | 1.74 |
| 2049.5 | 0.54 | 2.06 | 1.77 | 1.92 | 2.38 | 4.92 | 1.78 | 1.75 |
| 2050 | 0.54 | 2.06 | 1.78 | 1.92 | 2.39 | 4.94 | 1.79 | 1.75 |
| 2050.5 | 0.54 | 2.07 | 1.78 | 1.93 | 2.4 | 4.95 | 1.79 | 1.76 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2051 | 0.54 | 2.08 | 1.79 | 1.94 | 2.4 | 4.96 | 1.8 | 1.77 |
| 2051.5 | 0.54 | 2.08 | 1.8 | 1.94 | 2.41 | 4.97 | 1.8 | 1.77 |
| 2052 | 0.54 | 2.09 | 1.8 | 1.94 | 2.41 | 4.97 | 1.81 | 1.77 |
| 2052.5 | 0.54 | 2.09 | 1.8 | 1.95 | 2.41 | 4.97 | 1.81 | 1.77 |
| 2053 | 0.54 | 2.09 | 1.8 | 1.95 | 2.41 | 4.97 | 1.81 | 1.77 |
| 2053.5 | 0.54 | 2.09 | 1.8 | 1.94 | 2.41 | 4.97 | 1.81 | 1.77 |
| 2054 | 0.54 | 2.08 | 1.8 | 1.94 | 2.4 | 4.96 | 1.8 | 1.77 |
| 2054.5 | 0.54 | 2.08 | 1.79 | 1.94 | 2.4 | 4.95 | 1.79 | 1.76 |
| 2055 | 0.54 | 2.07 | 1.78 | 1.93 | 2.39 | 4.94 | 1.79 | 1.75 |
| 2055.5 | 0.54 | 2.06 | 1.77 | 1.92 | 2.38 | 4.93 | 1.78 | 1.74 |
| 2056 | 0.54 | 2.05 | 1.76 | 1.91 | 2.37 | 4.91 | 1.76 | 1.73 |
| 2056.5 | 0.54 | 2.03 | 1.75 | 1.9 | 2.36 | 4.89 | 1.75 | 1.72 |
| 2057 | 0.54 | 2.02 | 1.74 | 1.89 | 2.34 | 4.86 | 1.74 | 1.7 |
| 2057.5 | 0.54 | 2 | 1.73 | 1.87 | 2.33 | 4.84 | 1.72 | 1.69 |
| 2058 | 0.54 | 1.99 | 1.71 | 1.86 | 2.32 | 4.81 | 1.71 | 1.68 |
| 2058.5 | 0.54 | 1.97 | 1.7 | 1.84 | 2.3 | 4.78 | 1.69 | 1.66 |
| 2059 | 0.54 | 1.95 | 1.68 | 1.83 | 2.28 | 4.76 | 1.68 | 1.64 |
| 2059.5 | 0.54 | 1.94 | 1.66 | 1.81 | 2.27 | 4.73 | 1.66 | 1.63 |
| 2060 | 0.54 | 1.92 | 1.65 | 1.8 | 2.25 | 4.7 | 1.65 | 1.61 |
| 2060.5 | 0.54 | 1.9 | 1.63 | 1.78 | 2.24 | 4.67 | 1.63 | 1.6 |
| 2061 | 0.54 | 1.89 | 1.62 | 1.77 | 2.22 | 4.65 | 1.61 | 1.58 |
| 2061.5 | 0.54 | 1.87 | 1.6 | 1.75 | 2.21 | 4.62 | 1.6 | 1.56 |
| 2062 | 0.54 | 1.86 | 1.59 | 1.74 | 2.19 | 4.59 | 1.58 | 1.55 |
| 2062.5 | 0.54 | 1.84 | 1.57 | 1.73 | 2.18 | 4.57 | 1.57 | 1.53 |
| 2063 | 0.54 | 1.83 | 1.56 | 1.71 | 2.16 | 4.54 | 1.55 | 1.52 |
| 2063.5 | 0.54 | 1.81 | 1.54 | 1.7 | 2.15 | 4.52 | 1.54 | 1.51 |
| 2064 | 0.54 | 1.8 | 1.53 | 1.69 | 2.13 | 4.5 | 1.53 | 1.49 |
| 2064.5 | 0.54 | 1.78 | 1.52 | 1.68 | 2.12 | 4.47 | 1.51 | 1.48 |
| 2065 | 0.54 | 1.77 | 1.51 | 1.66 | 2.11 | 4.45 | 1.5 | 1.47 |
| 2065.5 | 0.54 | 1.76 | 1.49 | 1.65 | 2.1 | 4.43 | 1.49 | 1.46 |
| 2066 | 0.54 | 1.75 | 1.48 | 1.64 | 2.09 | 4.41 | 1.48 | 1.45 |
| 2066.5 | 0.54 | 1.74 | 1.47 | 1.63 | 2.07 | 4.39 | 1.47 | 1.44 |
| 2067 | 0.54 | 1.72 | 1.46 | 1.62 | 2.06 | 4.38 | 1.46 | 1.43 |
| 2067.5 | 0.54 | 1.71 | 1.45 | 1.61 | 2.05 | 4.36 | 1.45 | 1.42 |
| 2068 | 0.54 | 1.7 | 1.44 | 1.6 | 2.05 | 4.35 | 1.44 | 1.41 |
| 2068.5 | 0.54 | 1.7 | 1.44 | 1.6 | 2.04 | 4.33 | 1.43 | 1.4 |
| 2069 | 0.54 | 1.69 | 1.43 | 1.59 | 2.03 | 4.32 | 1.42 | 1.39 |
| 2069.5 | 0.54 | 1.68 | 1.42 | 1.58 | 2.02 | 4.31 | 1.41 | 1.39 |
| 2070 | 0.54 | 1.67 | 1.41 | 1.57 | 2.01 | 4.29 | 1.41 | 1.38 |
| 2070.5 | 0.54 | 1.66 | 1.41 | 1.57 | 2.01 | 4.28 | 1.4 | 1.37 |
| 2071 | 0.54 | 1.66 | 1.4 | 1.56 | 2 | 4.27 | 1.39 | 1.37 |
| 2071.5 | 0.54 | 1.65 | 1.4 | 1.56 | 1.99 | 4.26 | 1.39 | 1.36 |
| 2072 | 0.54 | 1.64 | 1.39 | 1.55 | 1.99 | 4.25 | 1.38 | 1.36 |
| 2072.5 | 0.54 | 1.64 | 1.38 | 1.55 | 1.98 | 4.24 | 1.38 | 1.35 |
| 2073 | 0.54 | 1.63 | 1.38 | 1.54 | 1.98 | 4.24 | 1.37 | 1.35 |
| 2073.5 | 0.54 | 1.63 | 1.38 | 1.54 | 1.97 | 4.23 | 1.37 | 1.34 |
| 2074 | 0.54 | 1.63 | 1.37 | 1.53 | 1.97 | 4.22 | 1.36 | 1.34 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2074.5 | 0.54 | 1.62 | 1.37 | 1.53 | 1.96 | 4.22 | 1.36 | 1.33 |
| 2075 | 0.54 | 1.62 | 1.36 | 1.53 | 1.96 | 4.21 | 1.36 | 1.33 |
| 2075.5 | 0.54 | 1.61 | 1.36 | 1.52 | 1.96 | 4.21 | 1.36 | 1.33 |
| 2076 | 0.54 | 1.61 | 1.36 | 1.52 | 1.95 | 4.2 | 1.35 | 1.33 |
| 2076.5 | 0.54 | 1.61 | 1.36 | 1.52 | 1.95 | 4.2 | 1.35 | 1.32 |
| 2077 | 0.54 | 1.61 | 1.35 | 1.51 | 1.95 | 4.19 | 1.35 | 1.32 |
| 2077.5 | 0.54 | 1.61 | 1.35 | 1.51 | 1.95 | 4.19 | 1.35 | 1.32 |
| 2078 | 0.54 | 1.6 | 1.35 | 1.51 | 1.94 | 4.19 | 1.35 | 1.32 |
| 2078.5 | 0.54 | 1.6 | 1.35 | 1.51 | 1.94 | 4.18 | 1.34 | 1.32 |
| 2079 | 0.54 | 1.6 | 1.35 | 1.51 | 1.94 | 4.18 | 1.34 | 1.32 |
| 2079.5 | 0.54 | 1.6 | 1.35 | 1.51 | 1.94 | 4.18 | 1.34 | 1.32 |
| 2080 | 0.55 | 1.6 | 1.34 | 1.51 | 1.94 | 4.17 | 1.34 | 1.32 |
| 2080.5 | 0.55 | 1.6 | 1.34 | 1.5 | 1.94 | 4.17 | 1.34 | 1.32 |
| 2081 | 0.55 | 1.6 | 1.34 | 1.5 | 1.94 | 4.17 | 1.34 | 1.31 |
| 2081.5 | 0.55 | 1.6 | 1.34 | 1.5 | 1.93 | 4.17 | 1.34 | 1.31 |
| 2082 | 0.55 | 1.6 | 1.34 | 1.5 | 1.93 | 4.16 | 1.34 | 1.31 |
| 2082.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.16 | 1.34 | 1.31 |
| 2083 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.16 | 1.34 | 1.31 |
| 2083.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.16 | 1.34 | 1.31 |
| 2084 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.16 | 1.34 | 1.31 |
| 2084.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.16 | 1.34 | 1.31 |
| 2085 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.34 | 1.31 |
| 2085.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.34 | 1.31 |
| 2086 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.34 | 1.31 |
| 2086.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.34 | 1.31 |
| 2087 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.33 | 1.31 |
| 2087.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.33 | 1.31 |
| 2088 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.33 | 1.31 |
| 2088.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.33 | 1.31 |
| 2089 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.33 | 1.31 |
| 2089.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.93 | 4.15 | 1.33 | 1.31 |
| 2090 | 0.55 | 1.59 | 1.34 | 1.5 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2090.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2091 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2091.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2092 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2092.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2093 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2093.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2094 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2094.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.3 |
| 2095 | 0.55 | 1.59 | 1.33 | 1.49 | 1.92 | 4.15 | 1.33 | 1.3 |
| 2095.5 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.15 | 1.33 | 1.3 |
| 2096 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.15 | 1.33 | 1.3 |
| 2096.5 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.15 | 1.33 | 1.3 |
| 2097 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.14 | 1.33 | 1.3 |
| 2097.5 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.14 | 1.33 | 1.3 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2098 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.14 | 1.33 | 1.3 |
| 2098.5 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.14 | 1.33 | 1.31 |
| 2099 | 0.55 | 1.59 | 1.33 | 1.49 | 1.91 | 4.14 | 1.33 | 1.31 |
| 2099.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.91 | 4.14 | 1.33 | 1.31 |
| 2100 | 0.55 | 1.59 | 1.34 | 1.49 | 1.91 | 4.14 | 1.33 | 1.31 |
| 2100.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.91 | 4.14 | 1.33 | 1.31 |
| 2101 | 0.55 | 1.59 | 1.34 | 1.49 | 1.91 | 4.14 | 1.33 | 1.31 |
| 2101.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.91 | 4.14 | 1.33 | 1.31 |
| 2102 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.14 | 1.33 | 1.31 |
| 2102.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2103 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.33 | 1.31 |
| 2103.5 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.34 | 1.31 |
| 2104 | 0.55 | 1.59 | 1.34 | 1.49 | 1.92 | 4.15 | 1.34 | 1.31 |
| 2104.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.92 | 4.15 | 1.34 | 1.31 |
| 2105 | 0.55 | 1.59 | 1.34 | 1.5 | 1.92 | 4.15 | 1.34 | 1.31 |
| 2105.5 | 0.55 | 1.59 | 1.34 | 1.5 | 1.92 | 4.16 | 1.34 | 1.32 |
| 2106 | 0.55 | 1.6 | 1.34 | 1.5 | 1.92 | 4.16 | 1.34 | 1.32 |
| 2106.5 | 0.55 | 1.6 | 1.34 | 1.5 | 1.92 | 4.16 | 1.34 | 1.32 |
| 2107 | 0.55 | 1.6 | 1.34 | 1.5 | 1.92 | 4.16 | 1.34 | 1.32 |
| 2107.5 | 0.55 | 1.6 | 1.35 | 1.5 | 1.92 | 4.16 | 1.34 | 1.32 |
| 2108 | 0.55 | 1.6 | 1.35 | 1.5 | 1.92 | 4.16 | 1.34 | 1.32 |
| 2108.5 | 0.55 | 1.6 | 1.35 | 1.5 | 1.92 | 4.16 | 1.34 | 1.32 |
| 2109 | 0.55 | 1.6 | 1.35 | 1.5 | 1.92 | 4.17 | 1.34 | 1.32 |
| 2109.5 | 0.55 | 1.6 | 1.35 | 1.5 | 1.92 | 4.17 | 1.34 | 1.32 |
| 2110 | 0.55 | 1.6 | 1.35 | 1.5 | 1.92 | 4.17 | 1.34 | 1.32 |
| 2110.5 | 0.55 | 1.6 | 1.35 | 1.5 | 1.93 | 4.17 | 1.35 | 1.32 |
| 2111 | 0.55 | 1.61 | 1.35 | 1.5 | 1.93 | 4.17 | 1.35 | 1.33 |
| 2111.5 | 0.55 | 1.61 | 1.35 | 1.5 | 1.93 | 4.17 | 1.35 | 1.33 |
| 2112 | 0.55 | 1.61 | 1.35 | 1.5 | 1.93 | 4.17 | 1.35 | 1.33 |
| 2112.5 | 0.55 | 1.61 | 1.36 | 1.51 | 1.93 | 4.17 | 1.35 | 1.33 |
| 2113 | 0.55 | 1.61 | 1.36 | 1.51 | 1.93 | 4.18 | 1.35 | 1.33 |
| 2113.5 | 0.55 | 1.61 | 1.36 | 1.51 | 1.93 | 4.18 | 1.35 | 1.33 |
| 2114 | 0.55 | 1.62 | 1.36 | 1.51 | 1.93 | 4.18 | 1.35 | 1.34 |
| 2114.5 | 0.55 | 1.62 | 1.36 | 1.51 | 1.94 | 4.18 | 1.36 | 1.34 |
| 2115 | 0.55 | 1.62 | 1.36 | 1.51 | 1.94 | 4.19 | 1.36 | 1.34 |
| 2115.5 | 0.55 | 1.62 | 1.36 | 1.51 | 1.94 | 4.19 | 1.36 | 1.34 |
| 2116 | 0.55 | 1.63 | 1.37 | 1.52 | 1.94 | 4.2 | 1.36 | 1.34 |
| 2116.5 | 0.55 | 1.63 | 1.37 | 1.52 | 1.94 | 4.2 | 1.37 | 1.35 |
| 2117 | 0.55 | 1.63 | 1.37 | 1.52 | 1.94 | 4.2 | 1.37 | 1.35 |
| 2117.5 | 0.55 | 1.63 | 1.37 | 1.52 | 1.95 | 4.21 | 1.37 | 1.35 |
| 2118 | 0.55 | 1.64 | 1.38 | 1.53 | 1.95 | 4.21 | 1.37 | 1.35 |
| 2118.5 | 0.55 | 1.64 | 1.38 | 1.53 | 1.95 | 4.22 | 1.38 | 1.36 |
| 2119 | 0.55 | 1.64 | 1.38 | 1.53 | 1.95 | 4.23 | 1.38 | 1.36 |
| 2119.5 | 0.55 | 1.65 | 1.39 | 1.53 | 1.96 | 4.23 | 1.38 | 1.36 |
| 2120 | 0.55 | 1.65 | 1.39 | 1.54 | 1.96 | 4.24 | 1.39 | 1.37 |
| 2120.5 | 0.55 | 1.65 | 1.39 | 1.54 | 1.96 | 4.24 | 1.39 | 1.37 |
| 2121 | 0.55 | 1.66 | 1.4 | 1.54 | 1.96 | 4.25 | 1.39 | 1.37 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2121.5 | 0.55 | 1.66 | 1.4 | 1.55 | 1.97 | 4.26 | 1.4 | 1.37 |
| 2122 | 0.56 | 1.66 | 1.4 | 1.55 | 1.97 | 4.26 | 1.4 | 1.38 |
| 2122.5 | 0.56 | 1.67 | 1.41 | 1.55 | 1.97 | 4.27 | 1.4 | 1.38 |
| 2123 | 0.56 | 1.67 | 1.41 | 1.55 | 1.97 | 4.27 | 1.4 | 1.38 |
| 2123.5 | 0.56 | 1.67 | 1.41 | 1.56 | 1.98 | 4.28 | 1.41 | 1.39 |
| 2124 | 0.56 | 1.68 | 1.42 | 1.56 | 1.98 | 4.28 | 1.41 | 1.39 |
| 2124.5 | 0.56 | 1.68 | 1.42 | 1.56 | 1.98 | 4.29 | 1.41 | 1.39 |
| 2125 | 0.56 | 1.68 | 1.42 | 1.56 | 1.98 | 4.29 | 1.42 | 1.39 |
| 2125.5 | 0.56 | 1.68 | 1.42 | 1.57 | 1.99 | 4.3 | 1.42 | 1.4 |
| 2126 | 0.56 | 1.69 | 1.43 | 1.57 | 1.99 | 4.3 | 1.42 | 1.4 |
| 2126.5 | 0.56 | 1.69 | 1.43 | 1.57 | 1.99 | 4.31 | 1.42 | 1.4 |
| 2127 | 0.56 | 1.69 | 1.43 | 1.57 | 1.99 | 4.31 | 1.43 | 1.4 |
| 2127.5 | 0.56 | 1.69 | 1.43 | 1.57 | 1.99 | 4.31 | 1.43 | 1.4 |
| 2128 | 0.56 | 1.69 | 1.43 | 1.58 | 2 | 4.32 | 1.43 | 1.41 |
| 2128.5 | 0.56 | 1.7 | 1.43 | 1.58 | 2 | 4.32 | 1.43 | 1.41 |
| 2129 | 0.56 | 1.7 | 1.43 | 1.58 | 2 | 4.32 | 1.43 | 1.41 |
| 2129.5 | 0.56 | 1.7 | 1.44 | 1.58 | 2 | 4.32 | 1.44 | 1.41 |
| 2130 | 0.56 | 1.7 | 1.44 | 1.58 | 2 | 4.32 | 1.44 | 1.41 |
| 2130.5 | 0.56 | 1.7 | 1.44 | 1.58 | 2 | 4.33 | 1.44 | 1.41 |
| 2131 | 0.56 | 1.7 | 1.44 | 1.58 | 2 | 4.33 | 1.44 | 1.41 |
| 2131.5 | 0.56 | 1.7 | 1.44 | 1.58 | 2 | 4.33 | 1.44 | 1.41 |
| 2132 | 0.56 | 1.7 | 1.44 | 1.58 | 2 | 4.33 | 1.44 | 1.42 |
| 2132.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2133 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2133.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2134 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2134.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2135 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2135.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2136 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2136.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2137 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2137.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2138 | 0.56 | 1.7 | 1.44 | 1.58 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2138.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2139 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2139.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2140 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2140.5 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2141 | 0.56 | 1.7 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2141.5 | 0.56 | 1.71 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2142 | 0.56 | 1.71 | 1.44 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2142.5 | 0.56 | 1.71 | 1.45 | 1.59 | 2.01 | 4.33 | 1.44 | 1.42 |
| 2143 | 0.56 | 1.71 | 1.45 | 1.59 | 2.01 | 4.33 | 1.45 | 1.42 |
| 2143.5 | 0.56 | 1.71 | 1.45 | 1.59 | 2.01 | 4.33 | 1.45 | 1.42 |
| 2144 | 0.56 | 1.71 | 1.45 | 1.59 | 2.01 | 4.33 | 1.45 | 1.42 |
| 2144.5 | 0.56 | 1.71 | 1.45 | 1.59 | 2.01 | 4.33 | 1.45 | 1.43 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2145 | 0.56 | 1.71 | 1.45 | 1.59 | 2.01 | 4.34 | 1.45 | 1.43 |
| 2145.5 | 0.56 | 1.71 | 1.45 | 1.59 | 2.02 | 4.34 | 1.45 | 1.43 |
| 2146 | 0.56 | 1.71 | 1.45 | 1.6 | 2.02 | 4.34 | 1.45 | 1.43 |
| 2146.5 | 0.56 | 1.71 | 1.45 | 1.6 | 2.02 | 4.34 | 1.45 | 1.43 |
| 2147 | 0.56 | 1.71 | 1.45 | 1.6 | 2.02 | 4.35 | 1.45 | 1.43 |
| 2147.5 | 0.56 | 1.72 | 1.46 | 1.6 | 2.02 | 4.35 | 1.46 | 1.43 |
| 2148 | 0.56 | 1.72 | 1.46 | 1.6 | 2.02 | 4.35 | 1.46 | 1.44 |
| 2148.5 | 0.56 | 1.72 | 1.46 | 1.6 | 2.02 | 4.36 | 1.46 | 1.44 |
| 2149 | 0.56 | 1.72 | 1.46 | 1.6 | 2.02 | 4.36 | 1.46 | 1.44 |
| 2149.5 | 0.56 | 1.72 | 1.46 | 1.61 | 2.02 | 4.36 | 1.46 | 1.44 |
| 2150 | 0.56 | 1.73 | 1.46 | 1.61 | 2.02 | 4.36 | 1.46 | 1.44 |
| 2150.5 | 0.56 | 1.73 | 1.46 | 1.61 | 2.03 | 4.37 | 1.46 | 1.44 |
| 2151 | 0.56 | 1.73 | 1.46 | 1.61 | 2.03 | 4.37 | 1.47 | 1.45 |
| 2151.5 | 0.56 | 1.73 | 1.47 | 1.61 | 2.03 | 4.37 | 1.47 | 1.45 |
| 2152 | 0.56 | 1.73 | 1.47 | 1.61 | 2.03 | 4.38 | 1.47 | 1.45 |
| 2152.5 | 0.56 | 1.74 | 1.47 | 1.62 | 2.03 | 4.38 | 1.47 | 1.45 |
| 2153 | 0.56 | 1.74 | 1.47 | 1.62 | 2.03 | 4.38 | 1.47 | 1.45 |
| 2153.5 | 0.56 | 1.74 | 1.47 | 1.62 | 2.04 | 4.39 | 1.47 | 1.45 |
| 2154 | 0.56 | 1.74 | 1.48 | 1.62 | 2.04 | 4.39 | 1.48 | 1.46 |
| 2154.5 | 0.56 | 1.75 | 1.48 | 1.62 | 2.04 | 4.4 | 1.48 | 1.46 |
| 2155 | 0.56 | 1.75 | 1.48 | 1.63 | 2.04 | 4.4 | 1.48 | 1.46 |
| 2155.5 | 0.56 | 1.75 | 1.48 | 1.63 | 2.05 | 4.4 | 1.48 | 1.46 |
| 2156 | 0.56 | 1.76 | 1.49 | 1.63 | 2.05 | 4.41 | 1.49 | 1.47 |
| 2156.5 | 0.56 | 1.76 | 1.49 | 1.63 | 2.05 | 4.41 | 1.49 | 1.47 |
| 2157 | 0.56 | 1.76 | 1.49 | 1.64 | 2.06 | 4.42 | 1.49 | 1.47 |
| 2157.5 | 0.56 | 1.77 | 1.5 | 1.64 | 2.06 | 4.42 | 1.5 | 1.48 |
| 2158 | 0.56 | 1.77 | 1.5 | 1.64 | 2.06 | 4.43 | 1.5 | 1.48 |
| 2158.5 | 0.56 | 1.77 | 1.5 | 1.65 | 2.07 | 4.43 | 1.5 | 1.48 |
| 2159 | 0.56 | 1.78 | 1.51 | 1.65 | 2.07 | 4.44 | 1.51 | 1.49 |
| 2159.5 | 0.56 | 1.78 | 1.51 | 1.65 | 2.08 | 4.45 | 1.51 | 1.49 |
| 2160 | 0.56 | 1.78 | 1.51 | 1.66 | 2.08 | 4.45 | 1.52 | 1.5 |
| 2160.5 | 0.56 | 1.79 | 1.52 | 1.66 | 2.08 | 4.46 | 1.52 | 1.5 |
| 2161 | 0.56 | 1.79 | 1.52 | 1.67 | 2.09 | 4.47 | 1.52 | 1.5 |
| 2161.5 | 0.56 | 1.8 | 1.52 | 1.67 | 2.09 | 4.48 | 1.53 | 1.51 |
| 2162 | 0.56 | 1.8 | 1.53 | 1.67 | 2.1 | 4.48 | 1.53 | 1.51 |
| 2162.5 | 0.56 | 1.81 | 1.53 | 1.68 | 2.1 | 4.49 | 1.54 | 1.52 |
| 2163 | 0.56 | 1.81 | 1.54 | 1.68 | 2.11 | 4.5 | 1.54 | 1.52 |
| 2163.5 | 0.57 | 1.81 | 1.54 | 1.69 | 2.11 | 4.51 | 1.55 | 1.53 |
| 2164 | 0.57 | 1.82 | 1.54 | 1.69 | 2.12 | 4.51 | 1.55 | 1.53 |
| 2164.5 | 0.57 | 1.82 | 1.55 | 1.7 | 2.12 | 4.52 | 1.55 | 1.54 |
| 2165 | 0.57 | 1.83 | 1.55 | 1.7 | 2.13 | 4.53 | 1.56 | 1.54 |
| 2165.5 | 0.57 | 1.83 | 1.56 | 1.7 | 2.13 | 4.53 | 1.56 | 1.54 |
| 2166 | 0.57 | 1.84 | 1.56 | 1.71 | 2.14 | 4.54 | 1.57 | 1.55 |
| 2166.5 | 0.57 | 1.84 | 1.57 | 1.71 | 2.14 | 4.55 | 1.57 | 1.55 |
| 2167 | 0.57 | 1.85 | 1.57 | 1.72 | 2.15 | 4.56 | 1.58 | 1.56 |
| 2167.5 | 0.57 | 1.86 | 1.58 | 1.72 | 2.15 | 4.56 | 1.58 | 1.56 |
| 2168 | 0.57 | 1.86 | 1.58 | 1.73 | 2.16 | 4.57 | 1.59 | 1.57 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2168.5 | 0.57 | 1.87 | 1.59 | 1.73 | 2.17 | 4.58 | 1.6 | 1.58 |
| 2169 | 0.57 | 1.87 | 1.59 | 1.74 | 2.17 | 4.59 | 1.6 | 1.58 |
| 2169.5 | 0.57 | 1.88 | 1.6 | 1.75 | 2.18 | 4.6 | 1.61 | 1.59 |
| 2170 | 0.57 | 1.89 | 1.61 | 1.75 | 2.19 | 4.61 | 1.61 | 1.59 |
| 2170.5 | 0.57 | 1.89 | 1.61 | 1.76 | 2.19 | 4.62 | 1.62 | 1.6 |
| 2171 | 0.57 | 1.9 | 1.62 | 1.76 | 2.2 | 4.63 | 1.63 | 1.6 |
| 2171.5 | 0.57 | 1.91 | 1.63 | 1.77 | 2.21 | 4.65 | 1.63 | 1.61 |
| 2172 | 0.57 | 1.92 | 1.63 | 1.78 | 2.21 | 4.66 | 1.64 | 1.62 |
| 2172.5 | 0.57 | 1.92 | 1.64 | 1.78 | 2.22 | 4.67 | 1.65 | 1.62 |
| 2173 | 0.57 | 1.93 | 1.65 | 1.79 | 2.23 | 4.68 | 1.65 | 1.63 |
| 2173.5 | 0.57 | 1.94 | 1.65 | 1.79 | 2.23 | 4.7 | 1.66 | 1.64 |
| 2174 | 0.57 | 1.94 | 1.66 | 1.8 | 2.24 | 4.71 | 1.66 | 1.64 |
| 2174.5 | 0.57 | 1.95 | 1.67 | 1.81 | 2.25 | 4.72 | 1.67 | 1.65 |
| 2175 | 0.57 | 1.96 | 1.67 | 1.81 | 2.25 | 4.73 | 1.68 | 1.66 |
| 2175.5 | 0.57 | 1.97 | 1.68 | 1.82 | 2.26 | 4.74 | 1.68 | 1.66 |
| 2176 | 0.57 | 1.97 | 1.69 | 1.83 | 2.27 | 4.75 | 1.69 | 1.67 |
| 2176.5 | 0.57 | 1.98 | 1.69 | 1.83 | 2.27 | 4.76 | 1.7 | 1.68 |
| 2177 | 0.57 | 1.99 | 1.7 | 1.84 | 2.28 | 4.77 | 1.7 | 1.68 |
| 2177.5 | 0.57 | 1.99 | 1.7 | 1.84 | 2.29 | 4.78 | 1.71 | 1.69 |
| 2178 | 0.57 | 2 | 1.71 | 1.85 | 2.29 | 4.79 | 1.71 | 1.69 |
| 2178.5 | 0.57 | 2 | 1.71 | 1.85 | 2.3 | 4.8 | 1.72 | 1.7 |
| 2179 | 0.57 | 2.01 | 1.72 | 1.86 | 2.3 | 4.8 | 1.72 | 1.7 |
| 2179.5 | 0.57 | 2.01 | 1.72 | 1.86 | 2.3 | 4.81 | 1.73 | 1.71 |
| 2180 | 0.57 | 2.01 | 1.72 | 1.86 | 2.31 | 4.82 | 1.73 | 1.71 |
| 2180.5 | 0.57 | 2.02 | 1.73 | 1.87 | 2.31 | 4.82 | 1.73 | 1.71 |
| 2181 | 0.57 | 2.02 | 1.73 | 1.87 | 2.31 | 4.82 | 1.74 | 1.72 |
| 2181.5 | 0.57 | 2.02 | 1.73 | 1.87 | 2.32 | 4.83 | 1.74 | 1.72 |
| 2182 | 0.57 | 2.03 | 1.73 | 1.87 | 2.32 | 4.83 | 1.74 | 1.72 |
| 2182.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.32 | 4.84 | 1.75 | 1.72 |
| 2183 | 0.57 | 2.03 | 1.74 | 1.88 | 2.32 | 4.84 | 1.75 | 1.72 |
| 2183.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.32 | 4.84 | 1.75 | 1.73 |
| 2184 | 0.57 | 2.03 | 1.74 | 1.88 | 2.32 | 4.84 | 1.75 | 1.73 |
| 2184.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.73 |
| 2185 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.73 |
| 2185.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.73 |
| 2186 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.73 |
| 2186.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.73 |
| 2187 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.73 |
| 2187.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.72 |
| 2188 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.72 |
| 2188.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.84 | 1.75 | 1.72 |
| 2189 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.83 | 1.74 | 1.72 |
| 2189.5 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.83 | 1.74 | 1.72 |
| 2190 | 0.57 | 2.03 | 1.74 | 1.88 | 2.33 | 4.83 | 1.74 | 1.72 |
| 2190.5 | 0.57 | 2.03 | 1.73 | 1.88 | 2.32 | 4.82 | 1.74 | 1.72 |
| 2191 | 0.57 | 2.02 | 1.73 | 1.88 | 2.32 | 4.82 | 1.74 | 1.72 |
| 2191.5 | 0.57 | 2.02 | 1.73 | 1.88 | 2.32 | 4.82 | 1.74 | 1.72 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2192 | 0.57 | 2.02 | 1.73 | 1.88 | 2.32 | 4.81 | 1.74 | 1.72 |
| 2192.5 | 0.57 | 2.02 | 1.73 | 1.88 | 2.32 | 4.81 | 1.74 | 1.72 |
| 2193 | 0.57 | 2.02 | 1.73 | 1.88 | 2.32 | 4.81 | 1.73 | 1.72 |
| 2193.5 | 0.57 | 2.02 | 1.73 | 1.88 | 2.32 | 4.81 | 1.73 | 1.72 |
| 2194 | 0.57 | 2.02 | 1.73 | 1.87 | 2.32 | 4.81 | 1.73 | 1.71 |
| 2194.5 | 0.57 | 2.01 | 1.73 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2195 | 0.57 | 2.01 | 1.73 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2195.5 | 0.57 | 2.01 | 1.73 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2196 | 0.57 | 2.01 | 1.73 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2196.5 | 0.57 | 2.01 | 1.73 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2197 | 0.57 | 2.01 | 1.73 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2197.5 | 0.57 | 2.01 | 1.72 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2198 | 0.57 | 2.01 | 1.72 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2198.5 | 0.57 | 2.01 | 1.72 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2199 | 0.57 | 2.01 | 1.72 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2199.5 | 0.57 | 2.01 | 1.72 | 1.87 | 2.31 | 4.8 | 1.73 | 1.71 |
| 2200 | 0.57 | 2.01 | 1.72 | 1.87 | 2.31 | 4.8 | 1.72 | 1.71 |
| 2200.5 | 0.57 | 2.01 | 1.72 | 1.87 | 2.31 | 4.8 | 1.72 | 1.71 |
| 2201 | 0.57 | 2.01 | 1.72 | 1.86 | 2.31 | 4.8 | 1.72 | 1.71 |
| 2201.5 | 0.57 | 2.01 | 1.72 | 1.86 | 2.31 | 4.8 | 1.72 | 1.71 |
| 2202 | 0.57 | 2.01 | 1.72 | 1.86 | 2.31 | 4.8 | 1.72 | 1.71 |
| 2202.5 | 0.57 | 2 | 1.72 | 1.86 | 2.31 | 4.8 | 1.72 | 1.71 |
| 2203 | 0.57 | 2 | 1.72 | 1.86 | 2.31 | 4.79 | 1.72 | 1.71 |
| 2203.5 | 0.57 | 2 | 1.72 | 1.86 | 2.31 | 4.79 | 1.72 | 1.7 |
| 2204 | 0.57 | 2 | 1.72 | 1.86 | 2.31 | 4.79 | 1.72 | 1.7 |
| 2204.5 | 0.57 | 2 | 1.72 | 1.86 | 2.3 | 4.78 | 1.71 | 1.7 |
| 2205 | 0.57 | 2 | 1.71 | 1.86 | 2.3 | 4.78 | 1.71 | 1.7 |
| 2205.5 | 0.58 | 1.99 | 1.71 | 1.85 | 2.3 | 4.78 | 1.71 | 1.7 |
| 2206 | 0.58 | 1.99 | 1.71 | 1.85 | 2.3 | 4.77 | 1.71 | 1.7 |
| 2206.5 | 0.58 | 1.99 | 1.71 | 1.85 | 2.3 | 4.77 | 1.71 | 1.7 |
| 2207 | 0.58 | 1.99 | 1.71 | 1.85 | 2.29 | 4.76 | 1.71 | 1.69 |
| 2207.5 | 0.58 | 1.98 | 1.7 | 1.85 | 2.29 | 4.76 | 1.7 | 1.69 |
| 2208 | 0.58 | 1.98 | 1.7 | 1.84 | 2.29 | 4.75 | 1.7 | 1.69 |
| 2208.5 | 0.58 | 1.98 | 1.7 | 1.84 | 2.28 | 4.75 | 1.7 | 1.69 |
| 2209 | 0.58 | 1.97 | 1.7 | 1.84 | 2.28 | 4.74 | 1.7 | 1.68 |
| 2209.5 | 0.58 | 1.97 | 1.69 | 1.84 | 2.28 | 4.74 | 1.69 | 1.68 |
| 2210 | 0.58 | 1.97 | 1.69 | 1.83 | 2.28 | 4.73 | 1.69 | 1.68 |
| 2210.5 | 0.58 | 1.97 | 1.69 | 1.83 | 2.27 | 4.73 | 1.69 | 1.68 |
| 2211 | 0.58 | 1.96 | 1.69 | 1.83 | 2.27 | 4.72 | 1.69 | 1.67 |
| 2211.5 | 0.58 | 1.96 | 1.68 | 1.83 | 2.27 | 4.72 | 1.68 | 1.67 |
| 2212 | 0.58 | 1.96 | 1.68 | 1.82 | 2.27 | 4.71 | 1.68 | 1.67 |
| 2212.5 | 0.58 | 1.96 | 1.68 | 1.82 | 2.26 | 4.71 | 1.68 | 1.67 |
| 2213 | 0.58 | 1.95 | 1.67 | 1.82 | 2.26 | 4.7 | 1.67 | 1.66 |
| 2213.5 | 0.58 | 1.95 | 1.67 | 1.81 | 2.26 | 4.7 | 1.67 | 1.66 |
| 2214 | 0.58 | 1.95 | 1.67 | 1.81 | 2.25 | 4.69 | 1.67 | 1.66 |
| 2214.5 | 0.58 | 1.94 | 1.67 | 1.81 | 2.25 | 4.69 | 1.66 | 1.65 |
| 2215 | 0.58 | 1.94 | 1.66 | 1.8 | 2.25 | 4.68 | 1.66 | 1.65 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2215.5 | 0.58 | 1.94 | 1.66 | 1.8 | 2.25 | 4.68 | 1.66 | 1.65 |
| 2216 | 0.58 | 1.94 | 1.66 | 1.8 | 2.24 | 4.67 | 1.66 | 1.64 |
| 2216.5 | 0.58 | 1.93 | 1.65 | 1.8 | 2.24 | 4.67 | 1.65 | 1.64 |
| 2217 | 0.58 | 1.93 | 1.65 | 1.79 | 2.24 | 4.67 | 1.65 | 1.64 |
| 2217.5 | 0.58 | 1.93 | 1.65 | 1.79 | 2.24 | 4.66 | 1.65 | 1.63 |
| 2218 | 0.58 | 1.92 | 1.65 | 1.79 | 2.23 | 4.66 | 1.64 | 1.63 |
| 2218.5 | 0.58 | 1.92 | 1.64 | 1.78 | 2.23 | 4.66 | 1.64 | 1.63 |
| 2219 | 0.58 | 1.92 | 1.64 | 1.78 | 2.23 | 4.65 | 1.64 | 1.63 |
| 2219.5 | 0.58 | 1.92 | 1.64 | 1.78 | 2.23 | 4.65 | 1.64 | 1.62 |
| 2220 | 0.58 | 1.91 | 1.64 | 1.78 | 2.22 | 4.64 | 1.63 | 1.62 |
| 2220.5 | 0.58 | 1.91 | 1.63 | 1.77 | 2.22 | 4.64 | 1.63 | 1.62 |
| 2221 | 0.58 | 1.91 | 1.63 | 1.77 | 2.22 | 4.64 | 1.63 | 1.61 |
| 2221.5 | 0.58 | 1.9 | 1.63 | 1.77 | 2.22 | 4.63 | 1.63 | 1.61 |
| 2222 | 0.58 | 1.9 | 1.63 | 1.77 | 2.21 | 4.63 | 1.62 | 1.61 |
| 2222.5 | 0.58 | 1.9 | 1.62 | 1.77 | 2.21 | 4.63 | 1.62 | 1.61 |
| 2223 | 0.58 | 1.9 | 1.62 | 1.76 | 2.21 | 4.62 | 1.62 | 1.61 |
| 2223.5 | 0.58 | 1.9 | 1.62 | 1.76 | 2.2 | 4.62 | 1.62 | 1.61 |
| 2224 | 0.58 | 1.89 | 1.62 | 1.76 | 2.2 | 4.62 | 1.62 | 1.6 |
| 2224.5 | 0.58 | 1.89 | 1.62 | 1.76 | 2.2 | 4.62 | 1.61 | 1.6 |
| 2225 | 0.58 | 1.89 | 1.61 | 1.76 | 2.2 | 4.61 | 1.61 | 1.6 |
| 2225.5 | 0.58 | 1.89 | 1.61 | 1.76 | 2.2 | 4.61 | 1.61 | 1.6 |
| 2226 | 0.58 | 1.89 | 1.61 | 1.75 | 2.19 | 4.61 | 1.61 | 1.6 |
| 2226.5 | 0.58 | 1.89 | 1.61 | 1.75 | 2.19 | 4.61 | 1.61 | 1.6 |
| 2227 | 0.58 | 1.89 | 1.61 | 1.75 | 2.19 | 4.61 | 1.61 | 1.6 |
| 2227.5 | 0.58 | 1.88 | 1.61 | 1.75 | 2.19 | 4.6 | 1.6 | 1.6 |
| 2228 | 0.58 | 1.88 | 1.61 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2228.5 | 0.58 | 1.88 | 1.61 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2229 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2229.5 | 0.58 | 1.88 | 1.6 | 1.75 | 2.18 | 4.6 | 1.6 | 1.59 |
| 2230 | 0.58 | 1.88 | 1.6 | 1.75 | 2.18 | 4.6 | 1.6 | 1.59 |
| 2230.5 | 0.58 | 1.88 | 1.6 | 1.75 | 2.18 | 4.6 | 1.6 | 1.59 |
| 2231 | 0.58 | 1.88 | 1.6 | 1.75 | 2.18 | 4.6 | 1.6 | 1.59 |
| 2231.5 | 0.58 | 1.88 | 1.6 | 1.75 | 2.18 | 4.6 | 1.6 | 1.59 |
| 2232 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2232.5 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2233 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2233.5 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2234 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2234.5 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2235 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2235.5 | 0.58 | 1.88 | 1.6 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2236 | 0.58 | 1.88 | 1.61 | 1.75 | 2.19 | 4.6 | 1.6 | 1.59 |
| 2236.5 | 0.58 | 1.88 | 1.61 | 1.75 | 2.19 | 4.6 | 1.61 | 1.59 |
| 2237 | 0.58 | 1.89 | 1.61 | 1.75 | 2.19 | 4.6 | 1.61 | 1.59 |
| 2237.5 | 0.58 | 1.89 | 1.61 | 1.75 | 2.19 | 4.61 | 1.61 | 1.6 |
| 2238 | 0.58 | 1.89 | 1.61 | 1.76 | 2.2 | 4.61 | 1.61 | 1.6 |
| 2238.5 | 0.58 | 1.89 | 1.61 | 1.76 | 2.2 | 4.61 | 1.61 | 1.6 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2239 | 0.58 | 1.89 | 1.61 | 1.76 | 2.2 | 4.61 | 1.61 | 1.6 |
| 2239.5 | 0.58 | 1.89 | 1.61 | 1.76 | 2.2 | 4.62 | 1.61 | 1.6 |
| 2240 | 0.58 | 1.89 | 1.62 | 1.76 | 2.2 | 4.62 | 1.61 | 1.6 |
| 2240.5 | 0.58 | 1.9 | 1.62 | 1.76 | 2.2 | 4.62 | 1.62 | 1.61 |
| 2241 | 0.58 | 1.9 | 1.62 | 1.76 | 2.2 | 4.62 | 1.62 | 1.61 |
| 2241.5 | 0.58 | 1.9 | 1.62 | 1.76 | 2.21 | 4.63 | 1.62 | 1.61 |
| 2242 | 0.58 | 1.9 | 1.62 | 1.77 | 2.21 | 4.63 | 1.62 | 1.61 |
| 2242.5 | 0.58 | 1.9 | 1.63 | 1.77 | 2.21 | 4.64 | 1.62 | 1.61 |
| 2243 | 0.58 | 1.91 | 1.63 | 1.77 | 2.21 | 4.64 | 1.63 | 1.62 |
| 2243.5 | 0.58 | 1.91 | 1.63 | 1.77 | 2.21 | 4.64 | 1.63 | 1.62 |
| 2244 | 0.58 | 1.91 | 1.63 | 1.78 | 2.21 | 4.65 | 1.63 | 1.62 |
| 2244.5 | 0.58 | 1.91 | 1.63 | 1.78 | 2.22 | 4.65 | 1.64 | 1.62 |
| 2245 | 0.58 | 1.92 | 1.64 | 1.78 | 2.22 | 4.65 | 1.64 | 1.63 |
| 2245.5 | 0.58 | 1.92 | 1.64 | 1.78 | 2.22 | 4.66 | 1.64 | 1.63 |
| 2246 | 0.58 | 1.92 | 1.64 | 1.79 | 2.22 | 4.66 | 1.64 | 1.63 |
| 2246.5 | 0.58 | 1.93 | 1.64 | 1.79 | 2.23 | 4.67 | 1.65 | 1.64 |
| 2247 | 0.59 | 1.93 | 1.65 | 1.79 | 2.23 | 4.67 | 1.65 | 1.64 |
| 2247.5 | 0.59 | 1.93 | 1.65 | 1.8 | 2.23 | 4.68 | 1.65 | 1.64 |
| 2248 | 0.59 | 1.94 | 1.65 | 1.8 | 2.24 | 4.68 | 1.66 | 1.65 |
| 2248.5 | 0.59 | 1.94 | 1.66 | 1.8 | 2.24 | 4.69 | 1.66 | 1.65 |
| 2249 | 0.59 | 1.95 | 1.66 | 1.81 | 2.24 | 4.69 | 1.66 | 1.65 |
| 2249.5 | 0.59 | 1.95 | 1.66 | 1.81 | 2.25 | 4.7 | 1.67 | 1.65 |
| 2250 | 0.59 | 1.95 | 1.67 | 1.81 | 2.25 | 4.71 | 1.67 | 1.66 |
| 2250.5 | 0.59 | 1.96 | 1.67 | 1.82 | 2.26 | 4.71 | 1.67 | 1.66 |
| 2251 | 0.59 | 1.96 | 1.67 | 1.82 | 2.26 | 4.72 | 1.68 | 1.66 |
| 2251.5 | 0.59 | 1.96 | 1.68 | 1.82 | 2.26 | 4.73 | 1.68 | 1.67 |
| 2252 | 0.59 | 1.97 | 1.68 | 1.83 | 2.27 | 4.74 | 1.68 | 1.67 |
| 2252.5 | 0.59 | 1.97 | 1.68 | 1.83 | 2.27 | 4.74 | 1.69 | 1.68 |
| 2253 | 0.59 | 1.97 | 1.69 | 1.83 | 2.28 | 4.75 | 1.69 | 1.68 |
| 2253.5 | 0.59 | 1.98 | 1.69 | 1.84 | 2.28 | 4.76 | 1.7 | 1.68 |
| 2254 | 0.59 | 1.98 | 1.7 | 1.84 | 2.28 | 4.77 | 1.7 | 1.69 |
| 2254.5 | 0.59 | 1.99 | 1.7 | 1.84 | 2.29 | 4.78 | 1.7 | 1.69 |
| 2255 | 0.59 | 1.99 | 1.7 | 1.85 | 2.29 | 4.78 | 1.71 | 1.7 |
| 2255.5 | 0.59 | 2 | 1.71 | 1.85 | 2.29 | 4.79 | 1.71 | 1.7 |
| 2256 | 0.59 | 2 | 1.71 | 1.86 | 2.3 | 4.8 | 1.72 | 1.71 |
| 2256.5 | 0.59 | 2.01 | 1.72 | 1.86 | 2.3 | 4.81 | 1.72 | 1.71 |
| 2257 | 0.59 | 2.01 | 1.72 | 1.86 | 2.31 | 4.82 | 1.73 | 1.72 |
| 2257.5 | 0.59 | 2.02 | 1.73 | 1.87 | 2.31 | 4.83 | 1.73 | 1.72 |
| 2258 | 0.59 | 2.02 | 1.73 | 1.87 | 2.32 | 4.83 | 1.74 | 1.73 |
| 2258.5 | 0.59 | 2.03 | 1.74 | 1.88 | 2.32 | 4.84 | 1.74 | 1.73 |
| 2259 | 0.59 | 2.03 | 1.74 | 1.88 | 2.33 | 4.85 | 1.75 | 1.74 |
| 2259.5 | 0.59 | 2.04 | 1.75 | 1.89 | 2.33 | 4.86 | 1.75 | 1.75 |
| 2260 | 0.59 | 2.05 | 1.75 | 1.89 | 2.34 | 4.87 | 1.76 | 1.75 |
| 2260.5 | 0.59 | 2.05 | 1.76 | 1.9 | 2.34 | 4.88 | 1.77 | 1.76 |
| 2261 | 0.59 | 2.06 | 1.77 | 1.9 | 2.35 | 4.89 | 1.78 | 1.76 |
| 2261.5 | 0.59 | 2.07 | 1.77 | 1.91 | 2.36 | 4.9 | 1.78 | 1.77 |
| 2262 | 0.59 | 2.08 | 1.78 | 1.92 | 2.36 | 4.91 | 1.79 | 1.78 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2262.5 | 0.59 | 2.08 | 1.78 | 1.92 | 2.37 | 4.92 | 1.8 | 1.79 |
| 2263 | 0.59 | 2.09 | 1.79 | 1.93 | 2.38 | 4.93 | 1.8 | 1.79 |
| 2263.5 | 0.59 | 2.1 | 1.8 | 1.94 | 2.38 | 4.95 | 1.81 | 1.8 |
| 2264 | 0.59 | 2.11 | 1.81 | 1.94 | 2.39 | 4.96 | 1.82 | 1.81 |
| 2264.5 | 0.59 | 2.11 | 1.81 | 1.95 | 2.4 | 4.97 | 1.83 | 1.81 |
| 2265 | 0.59 | 2.12 | 1.82 | 1.96 | 2.41 | 4.98 | 1.84 | 1.82 |
| 2265.5 | 0.59 | 2.13 | 1.83 | 1.96 | 2.41 | 5 | 1.84 | 1.83 |
| 2266 | 0.59 | 2.14 | 1.83 | 1.97 | 2.42 | 5.01 | 1.85 | 1.84 |
| 2266.5 | 0.59 | 2.14 | 1.84 | 1.98 | 2.43 | 5.02 | 1.86 | 1.85 |
| 2267 | 0.59 | 2.15 | 1.85 | 1.99 | 2.44 | 5.04 | 1.87 | 1.85 |
| 2267.5 | 0.59 | 2.16 | 1.86 | 1.99 | 2.44 | 5.05 | 1.88 | 1.86 |
| 2268 | 0.59 | 2.17 | 1.87 | 2 | 2.45 | 5.07 | 1.88 | 1.87 |
| 2268.5 | 0.59 | 2.18 | 1.88 | 2.01 | 2.46 | 5.08 | 1.89 | 1.88 |
| 2269 | 0.59 | 2.19 | 1.88 | 2.02 | 2.47 | 5.1 | 1.9 | 1.89 |
| 2269.5 | 0.59 | 2.2 | 1.89 | 2.03 | 2.48 | 5.12 | 1.91 | 1.9 |
| 2270 | 0.59 | 2.21 | 1.9 | 2.04 | 2.49 | 5.13 | 1.92 | 1.91 |
| 2270.5 | 0.59 | 2.22 | 1.91 | 2.05 | 2.5 | 5.15 | 1.93 | 1.92 |
| 2271 | 0.59 | 2.23 | 1.92 | 2.06 | 2.51 | 5.17 | 1.94 | 1.93 |
| 2271.5 | 0.59 | 2.24 | 1.93 | 2.07 | 2.52 | 5.19 | 1.95 | 1.94 |
| 2272 | 0.59 | 2.25 | 1.94 | 2.08 | 2.53 | 5.21 | 1.96 | 1.96 |
| 2272.5 | 0.59 | 2.27 | 1.96 | 2.09 | 2.54 | 5.23 | 1.97 | 1.97 |
| 2273 | 0.59 | 2.28 | 1.97 | 2.1 | 2.56 | 5.25 | 1.99 | 1.98 |
| 2273.5 | 0.59 | 2.3 | 1.98 | 2.11 | 2.57 | 5.27 | 2 | 2 |
| 2274 | 0.59 | 2.31 | 1.99 | 2.13 | 2.59 | 5.3 | 2.02 | 2.01 |
| 2274.5 | 0.59 | 2.33 | 2.01 | 2.14 | 2.6 | 5.32 | 2.03 | 2.03 |
| 2275 | 0.59 | 2.35 | 2.02 | 2.16 | 2.62 | 5.35 | 2.05 | 2.04 |
| 2275.5 | 0.59 | 2.36 | 2.04 | 2.17 | 2.64 | 5.38 | 2.07 | 2.06 |
| 2276 | 0.59 | 2.38 | 2.06 | 2.19 | 2.65 | 5.41 | 2.08 | 2.08 |
| 2276.5 | 0.59 | 2.4 | 2.07 | 2.21 | 2.67 | 5.44 | 2.1 | 2.1 |
| 2277 | 0.59 | 2.42 | 2.09 | 2.23 | 2.69 | 5.47 | 2.12 | 2.11 |
| 2277.5 | 0.59 | 2.45 | 2.11 | 2.25 | 2.72 | 5.51 | 2.15 | 2.14 |
| 2278 | 0.59 | 2.47 | 2.13 | 2.27 | 2.74 | 5.54 | 2.17 | 2.16 |
| 2278.5 | 0.59 | 2.49 | 2.16 | 2.29 | 2.76 | 5.58 | 2.19 | 2.18 |
| 2279 | 0.59 | 2.52 | 2.18 | 2.31 | 2.79 | 5.62 | 2.22 | 2.2 |
| 2279.5 | 0.59 | 2.54 | 2.2 | 2.33 | 2.81 | 5.66 | 2.24 | 2.23 |
| 2280 | 0.59 | 2.57 | 2.23 | 2.36 | 2.84 | 5.71 | 2.27 | 2.25 |
| 2280.5 | 0.59 | 2.6 | 2.25 | 2.38 | 2.86 | 5.75 | 2.29 | 2.28 |
| 2281 | 0.59 | 2.62 | 2.28 | 2.41 | 2.89 | 5.8 | 2.32 | 2.3 |
| 2281.5 | 0.59 | 2.65 | 2.31 | 2.43 | 2.92 | 5.85 | 2.35 | 2.33 |
| 2282 | 0.59 | 2.68 | 2.33 | 2.46 | 2.95 | 5.9 | 2.38 | 2.36 |
| 2282.5 | 0.59 | 2.71 | 2.36 | 2.49 | 2.98 | 5.95 | 2.41 | 2.39 |
| 2283 | 0.59 | 2.74 | 2.39 | 2.51 | 3 | 6 | 2.44 | 2.42 |
| 2283.5 | 0.59 | 2.78 | 2.42 | 2.54 | 3.03 | 6.05 | 2.47 | 2.45 |
| 2284 | 0.59 | 2.81 | 2.45 | 2.57 | 3.06 | 6.1 | 2.5 | 2.48 |
| 2284.5 | 0.59 | 2.84 | 2.48 | 2.59 | 3.09 | 6.15 | 2.53 | 2.51 |
| 2285 | 0.59 | 2.87 | 2.5 | 2.62 | 3.12 | 6.2 | 2.56 | 2.54 |
| 2285.5 | 0.59 | 2.9 | 2.53 | 2.64 | 3.15 | 6.24 | 2.59 | 2.56 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2286 | 0.59 | 2.93 | 2.56 | 2.67 | 3.18 | 6.29 | 2.62 | 2.59 |
| 2286.5 | 0.59 | 2.95 | 2.58 | 2.69 | 3.2 | 6.34 | 2.64 | 2.62 |
| 2287 | 0.59 | 2.98 | 2.61 | 2.72 | 3.23 | 6.38 | 2.67 | 2.64 |
| 2287.5 | 0.59 | 3.01 | 2.63 | 2.74 | 3.25 | 6.42 | 2.7 | 2.67 |
| 2288 | 0.59 | 3.03 | 2.65 | 2.76 | 3.28 | 6.46 | 2.72 | 2.69 |
| 2288.5 | 0.59 | 3.05 | 2.67 | 2.78 | 3.3 | 6.49 | 2.74 | 2.71 |
| 2289 | 0.60 | 3.07 | 2.69 | 2.8 | 3.32 | 6.53 | 2.76 | 2.73 |
| 2289.5 | 0.60 | 3.09 | 2.71 | 2.81 | 3.34 | 6.56 | 2.78 | 2.75 |
| 2290 | 0.60 | 3.1 | 2.72 | 2.83 | 3.35 | 6.58 | 2.8 | 2.77 |
| 2290.5 | 0.60 | 3.12 | 2.73 | 2.84 | 3.36 | 6.61 | 2.81 | 2.78 |
| 2291 | 0.60 | 3.13 | 2.74 | 2.85 | 3.38 | 6.63 | 2.82 | 2.79 |
| 2291.5 | 0.60 | 3.14 | 2.75 | 2.86 | 3.39 | 6.64 | 2.83 | 2.8 |
| 2292 | 0.60 | 3.15 | 2.76 | 2.86 | 3.39 | 6.66 | 2.84 | 2.81 |
| 2292.5 | 0.60 | 3.15 | 2.77 | 2.87 | 3.4 | 6.67 | 2.84 | 2.82 |
| 2293 | 0.60 | 3.16 | 2.77 | 2.87 | 3.4 | 6.68 | 2.85 | 2.82 |
| 2293.5 | 0.60 | 3.16 | 2.77 | 2.87 | 3.4 | 6.69 | 2.85 | 2.82 |
| 2294 | 0.60 | 3.16 | 2.77 | 2.88 | 3.4 | 6.69 | 2.85 | 2.82 |
| 2294.5 | 0.60 | 3.16 | 2.77 | 2.87 | 3.4 | 6.69 | 2.85 | 2.82 |
| 2295 | 0.60 | 3.16 | 2.77 | 2.87 | 3.4 | 6.69 | 2.85 | 2.82 |
| 2295.5 | 0.60 | 3.15 | 2.76 | 2.87 | 3.4 | 6.69 | 2.84 | 2.81 |
| 2296 | 0.60 | 3.15 | 2.76 | 2.86 | 3.39 | 6.68 | 2.84 | 2.81 |
| 2296.5 | 0.60 | 3.14 | 2.75 | 2.86 | 3.38 | 6.68 | 2.83 | 2.8 |
| 2297 | 0.60 | 3.13 | 2.74 | 2.85 | 3.38 | 6.67 | 2.82 | 2.79 |
| 2297.5 | 0.60 | 3.12 | 2.73 | 2.84 | 3.37 | 6.66 | 2.81 | 2.78 |
| 2298 | 0.60 | 3.11 | 2.72 | 2.83 | 3.36 | 6.64 | 2.8 | 2.77 |
| 2298.5 | 0.60 | 3.1 | 2.71 | 2.82 | 3.35 | 6.62 | 2.79 | 2.76 |
| 2299 | 0.60 | 3.09 | 2.7 | 2.81 | 3.33 | 6.6 | 2.78 | 2.75 |
| 2299.5 | 0.60 | 3.07 | 2.68 | 2.8 | 3.32 | 6.58 | 2.76 | 2.73 |
| 2300 | 0.60 | 3.05 | 2.67 | 2.78 | 3.31 | 6.56 | 2.75 | 2.72 |
| 2300.5 | 0.60 | 3.04 | 2.65 | 2.77 | 3.29 | 6.53 | 2.73 | 2.7 |
| 2301 | 0.60 | 3.02 | 2.63 | 2.75 | 3.27 | 6.5 | 2.71 | 2.68 |
| 2301.5 | 0.60 | 3 | 2.62 | 2.73 | 3.25 | 6.47 | 2.69 | 2.67 |
| 2302 | 0.60 | 2.98 | 2.6 | 2.71 | 3.23 | 6.43 | 2.67 | 2.65 |
| 2302.5 | 0.60 | 2.95 | 2.58 | 2.7 | 3.21 | 6.4 | 2.65 | 2.63 |
| 2303 | 0.60 | 2.93 | 2.55 | 2.68 | 3.19 | 6.36 | 2.63 | 2.6 |
| 2303.5 | 0.60 | 2.91 | 2.53 | 2.65 | 3.16 | 6.33 | 2.6 | 2.58 |
| 2304 | 0.60 | 2.88 | 2.51 | 2.63 | 3.14 | 6.29 | 2.58 | 2.56 |
| 2304.5 | 0.60 | 2.86 | 2.49 | 2.61 | 3.12 | 6.25 | 2.56 | 2.54 |
| 2305 | 0.60 | 2.84 | 2.47 | 2.59 | 3.09 | 6.21 | 2.53 | 2.51 |
| 2305.5 | 0.60 | 2.81 | 2.44 | 2.57 | 3.07 | 6.17 | 2.51 | 2.49 |
| 2306 | 0.60 | 2.79 | 2.42 | 2.55 | 3.04 | 6.13 | 2.49 | 2.47 |
| 2306.5 | 0.60 | 2.76 | 2.4 | 2.53 | 3.02 | 6.09 | 2.46 | 2.45 |
| 2307 | 0.60 | 2.74 | 2.38 | 2.51 | 3 | 6.05 | 2.44 | 2.42 |
| 2307.5 | 0.60 | 2.72 | 2.36 | 2.49 | 2.98 | 6.01 | 2.42 | 2.4 |
| 2308 | 0.60 | 2.7 | 2.34 | 2.47 | 2.95 | 5.97 | 2.4 | 2.38 |
| 2308.5 | 0.60 | 2.68 | 2.32 | 2.45 | 2.93 | 5.94 | 2.38 | 2.36 |
| 2309 | 0.60 | 2.66 | 2.3 | 2.43 | 2.91 | 5.9 | 2.36 | 2.34 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2309.5 | 0.60 | 2.64 | 2.28 | 2.41 | 2.9 | 5.87 | 2.34 | 2.32 |
| 2310 | 0.60 | 2.62 | 2.27 | 2.39 | 2.88 | 5.84 | 2.32 | 2.31 |
| 2310.5 | 0.60 | 2.6 | 2.25 | 2.38 | 2.86 | 5.81 | 2.3 | 2.29 |
| 2311 | 0.60 | 2.58 | 2.24 | 2.36 | 2.84 | 5.78 | 2.29 | 2.27 |
| 2311.5 | 0.60 | 2.57 | 2.22 | 2.35 | 2.83 | 5.75 | 2.27 | 2.26 |
| 2312 | 0.60 | 2.55 | 2.21 | 2.33 | 2.81 | 5.72 | 2.26 | 2.24 |
| 2312.5 | 0.60 | 2.54 | 2.2 | 2.32 | 2.8 | 5.7 | 2.24 | 2.23 |
| 2313 | 0.60 | 2.53 | 2.18 | 2.31 | 2.79 | 5.67 | 2.23 | 2.22 |
| 2313.5 | 0.60 | 2.51 | 2.17 | 2.29 | 2.77 | 5.65 | 2.22 | 2.2 |
| 2314 | 0.60 | 2.5 | 2.16 | 2.28 | 2.76 | 5.63 | 2.21 | 2.19 |
| 2314.5 | 0.60 | 2.49 | 2.15 | 2.27 | 2.75 | 5.61 | 2.19 | 2.18 |
| 2315 | 0.60 | 2.48 | 2.14 | 2.26 | 2.74 | 5.59 | 2.18 | 2.17 |
| 2315.5 | 0.60 | 2.47 | 2.13 | 2.25 | 2.73 | 5.57 | 2.17 | 2.16 |
| 2316 | 0.60 | 2.46 | 2.12 | 2.24 | 2.72 | 5.55 | 2.16 | 2.15 |
| 2316.5 | 0.60 | 2.45 | 2.12 | 2.23 | 2.71 | 5.53 | 2.16 | 2.14 |
| 2317 | 0.60 | 2.44 | 2.11 | 2.22 | 2.7 | 5.52 | 2.15 | 2.13 |
| 2317.5 | 0.60 | 2.43 | 2.1 | 2.22 | 2.69 | 5.5 | 2.14 | 2.13 |
| 2318 | 0.60 | 2.42 | 2.09 | 2.21 | 2.68 | 5.49 | 2.13 | 2.12 |
| 2318.5 | 0.60 | 2.41 | 2.09 | 2.2 | 2.68 | 5.48 | 2.12 | 2.11 |
| 2319 | 0.60 | 2.41 | 2.08 | 2.2 | 2.67 | 5.46 | 2.12 | 2.11 |
| 2319.5 | 0.60 | 2.4 | 2.07 | 2.19 | 2.66 | 5.45 | 2.11 | 2.1 |
| 2320 | 0.60 | 2.39 | 2.07 | 2.19 | 2.66 | 5.44 | 2.1 | 2.09 |
| 2320.5 | 0.60 | 2.39 | 2.06 | 2.18 | 2.65 | 5.44 | 2.1 | 2.09 |
| 2321 | 0.60 | 2.38 | 2.06 | 2.18 | 2.65 | 5.43 | 2.09 | 2.08 |
| 2321.5 | 0.60 | 2.38 | 2.05 | 2.17 | 2.64 | 5.42 | 2.09 | 2.08 |
| 2322 | 0.60 | 2.37 | 2.05 | 2.17 | 2.64 | 5.42 | 2.08 | 2.08 |
| 2322.5 | 0.60 | 2.37 | 2.05 | 2.17 | 2.64 | 5.41 | 2.08 | 2.07 |
| 2323 | 0.60 | 2.37 | 2.05 | 2.17 | 2.63 | 5.41 | 2.08 | 2.07 |
| 2323.5 | 0.60 | 2.37 | 2.04 | 2.16 | 2.63 | 5.41 | 2.08 | 2.07 |
| 2324 | 0.60 | 2.36 | 2.04 | 2.16 | 2.63 | 5.4 | 2.07 | 2.06 |
| 2324.5 | 0.60 | 2.36 | 2.04 | 2.16 | 2.63 | 5.4 | 2.07 | 2.06 |
| 2325 | 0.60 | 2.36 | 2.04 | 2.16 | 2.62 | 5.4 | 2.07 | 2.06 |
| 2325.5 | 0.60 | 2.36 | 2.04 | 2.16 | 2.62 | 5.4 | 2.07 | 2.06 |
| 2326 | 0.60 | 2.36 | 2.04 | 2.16 | 2.62 | 5.4 | 2.07 | 2.06 |
| 2326.5 | 0.60 | 2.36 | 2.04 | 2.16 | 2.62 | 5.4 | 2.07 | 2.06 |
| 2327 | 0.60 | 2.36 | 2.04 | 2.16 | 2.62 | 5.4 | 2.07 | 2.06 |
| 2327.5 | 0.60 | 2.36 | 2.04 | 2.16 | 2.62 | 5.4 | 2.07 | 2.06 |
| 2328 | 0.60 | 2.36 | 2.04 | 2.16 | 2.62 | 5.41 | 2.07 | 2.06 |
| 2328.5 | 0.60 | 2.37 | 2.04 | 2.16 | 2.62 | 5.41 | 2.07 | 2.07 |
| 2329 | 0.60 | 2.37 | 2.04 | 2.16 | 2.63 | 5.41 | 2.08 | 2.07 |
| 2329.5 | 0.60 | 2.37 | 2.05 | 2.17 | 2.63 | 5.41 | 2.08 | 2.07 |
| 2330 | 0.60 | 2.37 | 2.05 | 2.17 | 2.63 | 5.42 | 2.08 | 2.07 |
| 2330.5 | 0.61 | 2.38 | 2.05 | 2.17 | 2.63 | 5.43 | 2.09 | 2.08 |
| 2331 | 0.61 | 2.38 | 2.05 | 2.18 | 2.64 | 5.43 | 2.09 | 2.08 |
| 2331.5 | 0.61 | 2.39 | 2.06 | 2.18 | 2.64 | 5.44 | 2.1 | 2.09 |
| 2332 | 0.61 | 2.4 | 2.06 | 2.19 | 2.65 | 5.45 | 2.1 | 2.1 |
| 2332.5 | 0.61 | 2.4 | 2.07 | 2.19 | 2.66 | 5.46 | 2.11 | 2.1 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2333 | 0.61 | 2.41 | 2.07 | 2.2 | 2.66 | 5.47 | 2.12 | 2.11 |
| 2333.5 | 0.61 | 2.42 | 2.08 | 2.21 | 2.67 | 5.49 | 2.12 | 2.12 |
| 2334 | 0.61 | 2.43 | 2.09 | 2.21 | 2.68 | 5.5 | 2.13 | 2.12 |
| 2334.5 | 0.61 | 2.44 | 2.1 | 2.22 | 2.69 | 5.52 | 2.14 | 2.13 |
| 2335 | 0.61 | 2.45 | 2.1 | 2.23 | 2.7 | 5.53 | 2.15 | 2.14 |
| 2335.5 | 0.61 | 2.46 | 2.11 | 2.24 | 2.71 | 5.55 | 2.16 | 2.15 |
| 2336 | 0.61 | 2.47 | 2.12 | 2.25 | 2.72 | 5.57 | 2.17 | 2.16 |
| 2336.5 | 0.61 | 2.48 | 2.13 | 2.26 | 2.73 | 5.59 | 2.18 | 2.18 |
| 2337 | 0.61 | 2.49 | 2.14 | 2.27 | 2.74 | 5.61 | 2.19 | 2.19 |
| 2337.5 | 0.61 | 2.5 | 2.15 | 2.28 | 2.75 | 5.63 | 2.21 | 2.2 |
| 2338 | 0.61 | 2.51 | 2.17 | 2.3 | 2.77 | 5.65 | 2.22 | 2.21 |
| 2338.5 | 0.61 | 2.53 | 2.18 | 2.31 | 2.78 | 5.67 | 2.23 | 2.22 |
| 2339 | 0.61 | 2.54 | 2.19 | 2.32 | 2.79 | 5.69 | 2.24 | 2.24 |
| 2339.5 | 0.61 | 2.55 | 2.2 | 2.33 | 2.8 | 5.7 | 2.25 | 2.25 |
| 2340 | 0.61 | 2.56 | 2.21 | 2.34 | 2.81 | 5.72 | 2.27 | 2.26 |
| 2340.5 | 0.61 | 2.57 | 2.22 | 2.35 | 2.82 | 5.74 | 2.28 | 2.27 |
| 2341 | 0.61 | 2.58 | 2.23 | 2.36 | 2.84 | 5.76 | 2.29 | 2.28 |
| 2341.5 | 0.61 | 2.59 | 2.24 | 2.36 | 2.84 | 5.77 | 2.3 | 2.29 |
| 2342 | 0.61 | 2.6 | 2.25 | 2.37 | 2.85 | 5.79 | 2.31 | 2.3 |
| 2342.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.86 | 5.8 | 2.32 | 2.31 |
| 2343 | 0.61 | 2.62 | 2.26 | 2.39 | 2.87 | 5.81 | 2.32 | 2.32 |
| 2343.5 | 0.61 | 2.62 | 2.27 | 2.39 | 2.87 | 5.82 | 2.33 | 2.32 |
| 2344 | 0.61 | 2.63 | 2.27 | 2.4 | 2.88 | 5.83 | 2.34 | 2.33 |
| 2344.5 | 0.61 | 2.63 | 2.28 | 2.4 | 2.88 | 5.84 | 2.34 | 2.33 |
| 2345 | 0.61 | 2.64 | 2.28 | 2.4 | 2.89 | 5.85 | 2.34 | 2.34 |
| 2345.5 | 0.61 | 2.64 | 2.28 | 2.4 | 2.89 | 5.85 | 2.35 | 2.34 |
| 2346 | 0.61 | 2.64 | 2.28 | 2.4 | 2.89 | 5.86 | 2.35 | 2.34 |
| 2346.5 | 0.61 | 2.64 | 2.28 | 2.4 | 2.89 | 5.86 | 2.35 | 2.34 |
| 2347 | 0.61 | 2.64 | 2.28 | 2.4 | 2.89 | 5.86 | 2.35 | 2.34 |
| 2347.5 | 0.61 | 2.64 | 2.28 | 2.4 | 2.89 | 5.86 | 2.35 | 2.34 |
| 2348 | 0.61 | 2.64 | 2.28 | 2.4 | 2.88 | 5.86 | 2.35 | 2.33 |
| 2348.5 | 0.61 | 2.64 | 2.28 | 2.4 | 2.88 | 5.86 | 2.34 | 2.33 |
| 2349 | 0.61 | 2.64 | 2.27 | 2.4 | 2.88 | 5.86 | 2.34 | 2.33 |
| 2349.5 | 0.61 | 2.63 | 2.27 | 2.39 | 2.88 | 5.85 | 2.34 | 2.33 |
| 2350 | 0.61 | 2.63 | 2.27 | 2.39 | 2.87 | 5.85 | 2.34 | 2.32 |
| 2350.5 | 0.61 | 2.63 | 2.27 | 2.39 | 2.87 | 5.85 | 2.33 | 2.32 |
| 2351 | 0.61 | 2.63 | 2.27 | 2.39 | 2.87 | 5.84 | 2.33 | 2.32 |
| 2351.5 | 0.61 | 2.63 | 2.26 | 2.39 | 2.87 | 5.84 | 2.33 | 2.32 |
| 2352 | 0.61 | 2.62 | 2.26 | 2.38 | 2.86 | 5.84 | 2.33 | 2.31 |
| 2352.5 | 0.61 | 2.62 | 2.26 | 2.38 | 2.86 | 5.83 | 2.33 | 2.31 |
| 2353 | 0.61 | 2.62 | 2.26 | 2.38 | 2.86 | 5.83 | 2.32 | 2.31 |
| 2353.5 | 0.61 | 2.62 | 2.26 | 2.38 | 2.86 | 5.83 | 2.32 | 2.31 |
| 2354 | 0.61 | 2.62 | 2.25 | 2.38 | 2.86 | 5.83 | 2.32 | 2.31 |
| 2354.5 | 0.61 | 2.62 | 2.25 | 2.38 | 2.86 | 5.83 | 2.32 | 2.31 |
| 2355 | 0.61 | 2.62 | 2.25 | 2.38 | 2.86 | 5.83 | 2.32 | 2.3 |
| 2355.5 | 0.61 | 2.62 | 2.25 | 2.38 | 2.86 | 5.83 | 2.32 | 2.3 |
| 2356 | 0.61 | 2.62 | 2.25 | 2.38 | 2.86 | 5.83 | 2.32 | 2.3 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2356.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.86 | 5.83 | 2.32 | 2.3 |
| 2357 | 0.61 | 2.61 | 2.25 | 2.38 | 2.86 | 5.82 | 2.32 | 2.3 |
| 2357.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.86 | 5.82 | 2.32 | 2.3 |
| 2358 | 0.61 | 2.61 | 2.25 | 2.38 | 2.86 | 5.82 | 2.32 | 2.3 |
| 2358.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.86 | 5.82 | 2.32 | 2.3 |
| 2359 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.3 |
| 2359.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.3 |
| 2360 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.3 |
| 2360.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.3 |
| 2361 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.3 |
| 2361.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.3 |
| 2362 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.81 | 2.32 | 2.3 |
| 2362.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.81 | 2.32 | 2.3 |
| 2363 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.81 | 2.32 | 2.3 |
| 2363.5 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.3 |
| 2364 | 0.61 | 2.61 | 2.25 | 2.38 | 2.85 | 5.82 | 2.32 | 2.31 |
| 2364.5 | 0.61 | 2.61 | 2.26 | 2.38 | 2.85 | 5.82 | 2.32 | 2.31 |
| 2365 | 0.61 | 2.61 | 2.26 | 2.38 | 2.85 | 5.82 | 2.32 | 2.31 |
| 2365.5 | 0.61 | 2.62 | 2.26 | 2.38 | 2.85 | 5.83 | 2.32 | 2.31 |
| 2366 | 0.61 | 2.62 | 2.26 | 2.39 | 2.86 | 5.84 | 2.33 | 2.32 |
| 2366.5 | 0.61 | 2.62 | 2.26 | 2.39 | 2.86 | 5.84 | 2.33 | 2.32 |
| 2367 | 0.61 | 2.62 | 2.27 | 2.39 | 2.86 | 5.85 | 2.33 | 2.32 |
| 2367.5 | 0.61 | 2.63 | 2.27 | 2.39 | 2.86 | 5.86 | 2.34 | 2.32 |
| 2368 | 0.61 | 2.63 | 2.27 | 2.4 | 2.87 | 5.86 | 2.34 | 2.33 |
| 2368.5 | 0.61 | 2.63 | 2.28 | 2.4 | 2.87 | 5.87 | 2.34 | 2.33 |
| 2369 | 0.61 | 2.64 | 2.28 | 2.4 | 2.87 | 5.88 | 2.35 | 2.33 |
| 2369.5 | 0.61 | 2.64 | 2.28 | 2.41 | 2.88 | 5.88 | 2.35 | 2.34 |
| 2370 | 0.61 | 2.65 | 2.28 | 2.41 | 2.88 | 5.89 | 2.35 | 2.34 |
| 2370.5 | 0.61 | 2.65 | 2.29 | 2.41 | 2.88 | 5.9 | 2.36 | 2.34 |
| 2371 | 0.61 | 2.65 | 2.29 | 2.41 | 2.89 | 5.9 | 2.36 | 2.34 |
| 2371.5 | 0.61 | 2.65 | 2.29 | 2.42 | 2.89 | 5.91 | 2.36 | 2.35 |
| 2372 | 0.61 | 2.66 | 2.29 | 2.42 | 2.89 | 5.91 | 2.37 | 2.35 |
| 2372.5 | 0.62 | 2.66 | 2.3 | 2.42 | 2.89 | 5.92 | 2.37 | 2.35 |
| 2373 | 0.62 | 2.66 | 2.3 | 2.43 | 2.9 | 5.92 | 2.37 | 2.35 |
| 2373.5 | 0.62 | 2.66 | 2.3 | 2.43 | 2.9 | 5.92 | 2.37 | 2.35 |
| 2374 | 0.62 | 2.66 | 2.3 | 2.43 | 2.9 | 5.93 | 2.38 | 2.35 |
| 2374.5 | 0.62 | 2.67 | 2.3 | 2.43 | 2.9 | 5.93 | 2.38 | 2.35 |
| 2375 | 0.62 | 2.67 | 2.3 | 2.43 | 2.9 | 5.93 | 2.38 | 2.36 |
| 2375.5 | 0.62 | 2.67 | 2.3 | 2.43 | 2.9 | 5.93 | 2.38 | 2.36 |
| 2376 | 0.62 | 2.67 | 2.3 | 2.43 | 2.9 | 5.93 | 2.38 | 2.36 |
| 2376.5 | 0.62 | 2.67 | 2.3 | 2.43 | 2.91 | 5.92 | 2.38 | 2.36 |
| 2377 | 0.62 | 2.66 | 2.3 | 2.43 | 2.91 | 5.92 | 2.38 | 2.36 |
| 2377.5 | 0.62 | 2.66 | 2.3 | 2.43 | 2.91 | 5.92 | 2.38 | 2.36 |
| 2378 | 0.62 | 2.66 | 2.3 | 2.43 | 2.9 | 5.91 | 2.38 | 2.36 |
| 2378.5 | 0.62 | 2.66 | 2.3 | 2.43 | 2.9 | 5.91 | 2.38 | 2.35 |
| 2379 | 0.62 | 2.66 | 2.3 | 2.42 | 2.9 | 5.91 | 2.38 | 2.35 |
| 2379.5 | 0.62 | 2.66 | 2.3 | 2.42 | 2.9 | 5.9 | 2.37 | 2.35 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2380 | 0.62 | 2.66 | 2.29 | 2.42 | 2.9 | 5.9 | 2.37 | 2.35 |
| 2380.5 | 0.62 | 2.65 | 2.29 | 2.42 | 2.9 | 5.89 | 2.37 | 2.35 |
| 2381 | 0.62 | 2.65 | 2.29 | 2.41 | 2.9 | 5.88 | 2.37 | 2.35 |
| 2381.5 | 0.62 | 2.65 | 2.29 | 2.41 | 2.89 | 5.88 | 2.37 | 2.34 |
| 2382 | 0.62 | 2.65 | 2.29 | 2.41 | 2.89 | 5.87 | 2.36 | 2.34 |
| 2382.5 | 0.62 | 2.64 | 2.29 | 2.4 | 2.89 | 5.87 | 2.36 | 2.34 |
| 2383 | 0.62 | 2.64 | 2.28 | 2.4 | 2.89 | 5.86 | 2.36 | 2.34 |
| 2383.5 | 0.62 | 2.64 | 2.28 | 2.4 | 2.88 | 5.85 | 2.35 | 2.33 |
| 2384 | 0.62 | 2.63 | 2.28 | 2.39 | 2.88 | 5.85 | 2.35 | 2.33 |
| 2384.5 | 0.62 | 2.63 | 2.27 | 2.39 | 2.87 | 5.84 | 2.35 | 2.33 |
| 2385 | 0.62 | 2.63 | 2.27 | 2.39 | 2.87 | 5.84 | 2.34 | 2.32 |
| 2385.5 | 0.62 | 2.62 | 2.27 | 2.38 | 2.87 | 5.83 | 2.34 | 2.32 |
| 2386 | 0.62 | 2.62 | 2.26 | 2.38 | 2.86 | 5.82 | 2.34 | 2.32 |
| 2386.5 | 0.62 | 2.62 | 2.26 | 2.37 | 2.86 | 5.82 | 2.33 | 2.31 |
| 2387 | 0.62 | 2.61 | 2.26 | 2.37 | 2.85 | 5.81 | 2.33 | 2.31 |
| 2387.5 | 0.62 | 2.61 | 2.25 | 2.36 | 2.85 | 5.81 | 2.32 | 2.3 |
| 2388 | 0.62 | 2.6 | 2.25 | 2.36 | 2.84 | 5.8 | 2.32 | 2.3 |
| 2388.5 | 0.62 | 2.6 | 2.25 | 2.36 | 2.84 | 5.79 | 2.31 | 2.29 |
| 2389 | 0.62 | 2.59 | 2.24 | 2.35 | 2.83 | 5.79 | 2.31 | 2.29 |
| 2389.5 | 0.62 | 2.59 | 2.24 | 2.35 | 2.83 | 5.78 | 2.3 | 2.28 |
| 2390 | 0.62 | 2.58 | 2.23 | 2.34 | 2.82 | 5.77 | 2.3 | 2.28 |
| 2390.5 | 0.62 | 2.58 | 2.23 | 2.34 | 2.82 | 5.77 | 2.3 | 2.27 |
| 2391 | 0.62 | 2.57 | 2.22 | 2.33 | 2.81 | 5.76 | 2.29 | 2.27 |
| 2391.5 | 0.62 | 2.57 | 2.22 | 2.33 | 2.81 | 5.75 | 2.28 | 2.26 |
| 2392 | 0.62 | 2.56 | 2.21 | 2.32 | 2.8 | 5.75 | 2.28 | 2.26 |
| 2392.5 | 0.62 | 2.56 | 2.21 | 2.32 | 2.79 | 5.74 | 2.27 | 2.25 |
| 2393 | 0.62 | 2.55 | 2.2 | 2.31 | 2.79 | 5.73 | 2.27 | 2.25 |
| 2393.5 | 0.62 | 2.54 | 2.2 | 2.31 | 2.78 | 5.72 | 2.26 | 2.24 |
| 2394 | 0.62 | 2.54 | 2.19 | 2.3 | 2.78 | 5.71 | 2.26 | 2.23 |
| 2394.5 | 0.62 | 2.53 | 2.19 | 2.3 | 2.77 | 5.71 | 2.25 | 2.23 |
| 2395 | 0.62 | 2.53 | 2.18 | 2.29 | 2.76 | 5.7 | 2.24 | 2.22 |
| 2395.5 | 0.62 | 2.52 | 2.17 | 2.29 | 2.76 | 5.69 | 2.23 | 2.21 |
| 2396 | 0.62 | 2.51 | 2.17 | 2.28 | 2.75 | 5.67 | 2.23 | 2.21 |
| 2396.5 | 0.62 | 2.51 | 2.16 | 2.28 | 2.74 | 5.66 | 2.22 | 2.2 |
| 2397 | 0.62 | 2.5 | 2.15 | 2.27 | 2.74 | 5.65 | 2.21 | 2.19 |
| 2397.5 | 0.62 | 2.49 | 2.15 | 2.27 | 2.73 | 5.64 | 2.21 | 2.19 |
| 2398 | 0.62 | 2.49 | 2.14 | 2.26 | 2.72 | 5.63 | 2.2 | 2.18 |
| 2398.5 | 0.62 | 2.48 | 2.13 | 2.25 | 2.72 | 5.61 | 2.19 | 2.17 |
| 2399 | 0.62 | 2.47 | 2.12 | 2.25 | 2.71 | 5.6 | 2.18 | 2.16 |
| 2399.5 | 0.62 | 2.46 | 2.12 | 2.24 | 2.7 | 5.59 | 2.17 | 2.16 |
| 2400 | 0.62 | 2.45 | 2.11 | 2.23 | 2.69 | 5.57 | 2.17 | 2.15 |
| 2400.5 | 0.62 | 2.45 | 2.1 | 2.23 | 2.69 | 5.56 | 2.16 | 2.14 |
| 2401 | 0.62 | 2.44 | 2.1 | 2.22 | 2.68 | 5.54 | 2.15 | 2.14 |
| 2401.5 | 0.62 | 2.43 | 2.09 | 2.21 | 2.67 | 5.53 | 2.14 | 2.13 |
| 2402 | 0.62 | 2.42 | 2.08 | 2.21 | 2.66 | 5.51 | 2.14 | 2.12 |
| 2402.5 | 0.62 | 2.41 | 2.07 | 2.2 | 2.65 | 5.5 | 2.13 | 2.11 |
| 2403 | 0.62 | 2.4 | 2.07 | 2.19 | 2.65 | 5.48 | 2.12 | 2.11 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2403.5 | 0.62 | 2.4 | 2.06 | 2.19 | 2.64 | 5.47 | 2.11 | 2.1 |
| 2404 | 0.62 | 2.39 | 2.05 | 2.18 | 2.63 | 5.45 | 2.11 | 2.09 |
| 2404.5 | 0.62 | 2.38 | 2.04 | 2.17 | 2.62 | 5.44 | 2.1 | 2.08 |
| 2405 | 0.62 | 2.37 | 2.04 | 2.16 | 2.61 | 5.42 | 2.09 | 2.08 |
| 2405.5 | 0.62 | 2.36 | 2.03 | 2.16 | 2.61 | 5.41 | 2.09 | 2.07 |
| 2406 | 0.62 | 2.36 | 2.02 | 2.15 | 2.6 | 5.39 | 2.08 | 2.06 |
| 2406.5 | 0.62 | 2.35 | 2.02 | 2.14 | 2.59 | 5.38 | 2.07 | 2.06 |
| 2407 | 0.62 | 2.34 | 2.01 | 2.14 | 2.58 | 5.37 | 2.06 | 2.05 |
| 2407.5 | 0.62 | 2.33 | 2 | 2.13 | 2.58 | 5.36 | 2.06 | 2.04 |
| 2408 | 0.62 | 2.33 | 2 | 2.12 | 2.57 | 5.34 | 2.05 | 2.04 |
| 2408.5 | 0.62 | 2.32 | 1.99 | 2.12 | 2.56 | 5.33 | 2.04 | 2.03 |
| 2409 | 0.62 | 2.31 | 1.98 | 2.11 | 2.56 | 5.32 | 2.03 | 2.02 |
| 2409.5 | 0.62 | 2.3 | 1.98 | 2.1 | 2.55 | 5.31 | 2.03 | 2.02 |
| 2410 | 0.62 | 2.3 | 1.97 | 2.1 | 2.55 | 5.3 | 2.02 | 2.01 |
| 2410.5 | 0.62 | 2.29 | 1.96 | 2.09 | 2.54 | 5.29 | 2.01 | 2 |
| 2411 | 0.62 | 2.28 | 1.96 | 2.09 | 2.54 | 5.29 | 2.01 | 2 |
| 2411.5 | 0.62 | 2.28 | 1.95 | 2.08 | 2.53 | 5.28 | 2 | 1.99 |
| 2412 | 0.62 | 2.27 | 1.95 | 2.08 | 2.52 | 5.27 | 1.99 | 1.99 |
| 2412.5 | 0.62 | 2.26 | 1.94 | 2.07 | 2.52 | 5.26 | 1.99 | 1.98 |
| 2413 | 0.62 | 2.26 | 1.94 | 2.07 | 2.51 | 5.26 | 1.98 | 1.98 |
| 2413.5 | 0.62 | 2.25 | 1.93 | 2.06 | 2.51 | 5.25 | 1.98 | 1.97 |
| 2414 | 0.63 | 2.25 | 1.93 | 2.06 | 2.5 | 5.24 | 1.97 | 1.97 |
| 2414.5 | 0.63 | 2.24 | 1.92 | 2.06 | 2.5 | 5.23 | 1.97 | 1.96 |
| 2415 | 0.63 | 2.24 | 1.92 | 2.05 | 2.49 | 5.23 | 1.96 | 1.96 |
| 2415.5 | 0.63 | 2.23 | 1.91 | 2.05 | 2.49 | 5.22 | 1.96 | 1.95 |
| 2416 | 0.63 | 2.23 | 1.91 | 2.04 | 2.48 | 5.21 | 1.95 | 1.95 |
| 2416.5 | 0.63 | 2.22 | 1.9 | 2.04 | 2.48 | 5.2 | 1.95 | 1.95 |
| 2417 | 0.63 | 2.22 | 1.9 | 2.04 | 2.48 | 5.19 | 1.94 | 1.94 |
| 2417.5 | 0.63 | 2.22 | 1.9 | 2.03 | 2.47 | 5.19 | 1.94 | 1.94 |
| 2418 | 0.63 | 2.21 | 1.89 | 2.03 | 2.47 | 5.18 | 1.94 | 1.94 |
| 2418.5 | 0.63 | 2.21 | 1.89 | 2.03 | 2.46 | 5.17 | 1.93 | 1.93 |
| 2419 | 0.63 | 2.21 | 1.89 | 2.03 | 2.46 | 5.16 | 1.93 | 1.93 |
| 2419.5 | 0.63 | 2.2 | 1.89 | 2.02 | 2.46 | 5.16 | 1.93 | 1.93 |
| 2420 | 0.63 | 2.2 | 1.88 | 2.02 | 2.45 | 5.15 | 1.93 | 1.93 |
| 2420.5 | 0.63 | 2.2 | 1.88 | 2.02 | 2.45 | 5.14 | 1.92 | 1.92 |
| 2421 | 0.63 | 2.2 | 1.88 | 2.02 | 2.45 | 5.14 | 1.92 | 1.92 |
| 2421.5 | 0.63 | 2.2 | 1.88 | 2.01 | 2.44 | 5.13 | 1.92 | 1.92 |
| 2422 | 0.63 | 2.2 | 1.88 | 2.01 | 2.44 | 5.13 | 1.92 | 1.92 |
| 2422.5 | 0.63 | 2.2 | 1.87 | 2.01 | 2.44 | 5.12 | 1.92 | 1.92 |
| 2423 | 0.63 | 2.19 | 1.87 | 2.01 | 2.44 | 5.12 | 1.92 | 1.91 |
| 2423.5 | 0.63 | 2.19 | 1.87 | 2.01 | 2.44 | 5.12 | 1.91 | 1.91 |
| 2424 | 0.63 | 2.19 | 1.87 | 2.01 | 2.44 | 5.12 | 1.91 | 1.91 |
| 2424.5 | 0.63 | 2.19 | 1.87 | 2.01 | 2.43 | 5.11 | 1.91 | 1.91 |
| 2425 | 0.63 | 2.19 | 1.87 | 2.01 | 2.43 | 5.11 | 1.91 | 1.91 |
| 2425.5 | 0.63 | 2.19 | 1.87 | 2.01 | 2.43 | 5.12 | 1.91 | 1.91 |
| 2426 | 0.63 | 2.19 | 1.87 | 2.01 | 2.43 | 5.12 | 1.91 | 1.91 |
| 2426.5 | 0.63 | 2.19 | 1.87 | 2.01 | 2.43 | 5.12 | 1.91 | 1.91 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2427 | 0.63 | 2.19 | 1.87 | 2.01 | 2.43 | 5.12 | 1.91 | 1.91 |
| 2427.5 | 0.63 | 2.19 | 1.87 | 2.01 | 2.43 | 5.12 | 1.91 | 1.91 |
| 2428 | 0.63 | 2.19 | 1.88 | 2.01 | 2.43 | 5.13 | 1.91 | 1.91 |
| 2428.5 | 0.63 | 2.19 | 1.88 | 2.01 | 2.43 | 5.13 | 1.91 | 1.91 |
| 2429 | 0.63 | 2.19 | 1.88 | 2.01 | 2.44 | 5.13 | 1.91 | 1.92 |
| 2429.5 | 0.63 | 2.2 | 1.88 | 2.01 | 2.44 | 5.14 | 1.91 | 1.92 |
| 2430 | 0.63 | 2.2 | 1.88 | 2.01 | 2.44 | 5.14 | 1.92 | 1.92 |
| 2430.5 | 0.63 | 2.2 | 1.88 | 2.01 | 2.44 | 5.14 | 1.92 | 1.92 |
| 2431 | 0.63 | 2.2 | 1.88 | 2.01 | 2.44 | 5.15 | 1.92 | 1.92 |
| 2431.5 | 0.63 | 2.2 | 1.89 | 2.01 | 2.44 | 5.15 | 1.92 | 1.93 |
| 2432 | 0.63 | 2.2 | 1.89 | 2.01 | 2.45 | 5.15 | 1.92 | 1.93 |
| 2432.5 | 0.63 | 2.2 | 1.89 | 2.02 | 2.45 | 5.16 | 1.93 | 1.93 |
| 2433 | 0.63 | 2.21 | 1.89 | 2.02 | 2.45 | 5.16 | 1.93 | 1.93 |
| 2433.5 | 0.63 | 2.21 | 1.89 | 2.02 | 2.45 | 5.16 | 1.93 | 1.94 |
| 2434 | 0.63 | 2.21 | 1.89 | 2.02 | 2.45 | 5.16 | 1.93 | 1.94 |
| 2434.5 | 0.63 | 2.21 | 1.9 | 2.02 | 2.46 | 5.17 | 1.94 | 1.94 |
| 2435 | 0.63 | 2.22 | 1.9 | 2.03 | 2.46 | 5.17 | 1.94 | 1.94 |
| 2435.5 | 0.63 | 2.22 | 1.9 | 2.03 | 2.46 | 5.17 | 1.94 | 1.95 |
| 2436 | 0.63 | 2.22 | 1.9 | 2.03 | 2.47 | 5.17 | 1.95 | 1.95 |
| 2436.5 | 0.63 | 2.22 | 1.91 | 2.03 | 2.47 | 5.17 | 1.95 | 1.95 |
| 2437 | 0.63 | 2.23 | 1.91 | 2.03 | 2.47 | 5.18 | 1.95 | 1.95 |
| 2437.5 | 0.63 | 2.23 | 1.91 | 2.04 | 2.47 | 5.18 | 1.95 | 1.96 |
| 2438 | 0.63 | 2.23 | 1.91 | 2.04 | 2.48 | 5.18 | 1.96 | 1.96 |
| 2438.5 | 0.63 | 2.23 | 1.91 | 2.04 | 2.48 | 5.19 | 1.96 | 1.96 |
| 2439 | 0.63 | 2.24 | 1.92 | 2.04 | 2.48 | 5.19 | 1.96 | 1.96 |
| 2439.5 | 0.63 | 2.24 | 1.92 | 2.04 | 2.48 | 5.2 | 1.97 | 1.97 |
| 2440 | 0.63 | 2.24 | 1.92 | 2.05 | 2.49 | 5.2 | 1.97 | 1.97 |
| 2440.5 | 0.63 | 2.24 | 1.92 | 2.05 | 2.49 | 5.21 | 1.97 | 1.97 |
| 2441 | 0.63 | 2.25 | 1.93 | 2.05 | 2.49 | 5.21 | 1.97 | 1.97 |
| 2441.5 | 0.63 | 2.25 | 1.93 | 2.05 | 2.49 | 5.22 | 1.98 | 1.97 |
| 2442 | 0.63 | 2.25 | 1.93 | 2.06 | 2.49 | 5.22 | 1.98 | 1.97 |
| 2442.5 | 0.63 | 2.25 | 1.93 | 2.06 | 2.49 | 5.23 | 1.98 | 1.98 |
| 2443 | 0.63 | 2.25 | 1.93 | 2.06 | 2.5 | 5.23 | 1.98 | 1.98 |
| 2443.5 | 0.63 | 2.26 | 1.93 | 2.06 | 2.5 | 5.24 | 1.98 | 1.98 |
| 2444 | 0.63 | 2.26 | 1.93 | 2.06 | 2.5 | 5.24 | 1.99 | 1.98 |
| 2444.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.25 | 1.99 | 1.98 |
| 2445 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.25 | 1.99 | 1.98 |
| 2445.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.26 | 1.99 | 1.98 |
| 2446 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.26 | 1.99 | 1.98 |
| 2446.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.26 | 1.99 | 1.98 |
| 2447 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.27 | 1.99 | 1.98 |
| 2447.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.27 | 1.99 | 1.98 |
| 2448 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.27 | 1.99 | 1.98 |
| 2448.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.27 | 1.99 | 1.98 |
| 2449 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.27 | 1.99 | 1.98 |
| 2449.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.27 | 1.99 | 1.98 |
| 2450 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.98 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2450.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.98 |
| 2451 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.98 |
| 2451.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.99 |
| 2452 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.99 |
| 2452.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.99 |
| 2453 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.99 |
| 2453.5 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.28 | 1.99 | 1.99 |
| 2454 | 0.63 | 2.26 | 1.94 | 2.07 | 2.5 | 5.29 | 2 | 1.99 |
| 2454.5 | 0.63 | 2.26 | 1.95 | 2.07 | 2.5 | 5.29 | 2 | 1.99 |
| 2455 | 0.63 | 2.26 | 1.95 | 2.08 | 2.5 | 5.29 | 2 | 1.99 |
| 2455.5 | 0.63 | 2.27 | 1.95 | 2.08 | 2.5 | 5.29 | 2 | 2 |
| 2456 | 0.64 | 2.27 | 1.95 | 2.08 | 2.5 | 5.29 | 2 | 2 |
| 2456.5 | 0.64 | 2.27 | 1.95 | 2.08 | 2.5 | 5.29 | 2 | 2 |
| 2457 | 0.64 | 2.27 | 1.95 | 2.08 | 2.51 | 5.29 | 2.01 | 2 |
| 2457.5 | 0.64 | 2.27 | 1.96 | 2.08 | 2.51 | 5.29 | 2.01 | 2 |
| 2458 | 0.64 | 2.28 | 1.96 | 2.09 | 2.51 | 5.29 | 2.01 | 2 |
| 2458.5 | 0.64 | 2.28 | 1.96 | 2.09 | 2.51 | 5.29 | 2.01 | 2.01 |
| 2459 | 0.64 | 2.28 | 1.96 | 2.09 | 2.51 | 5.29 | 2.01 | 2.01 |
| 2459.5 | 0.64 | 2.28 | 1.96 | 2.09 | 2.52 | 5.3 | 2.02 | 2.01 |
| 2460 | 0.64 | 2.29 | 1.97 | 2.1 | 2.52 | 5.3 | 2.02 | 2.01 |
| 2460.5 | 0.64 | 2.29 | 1.97 | 2.1 | 2.52 | 5.3 | 2.02 | 2.01 |
| 2461 | 0.64 | 2.29 | 1.97 | 2.1 | 2.53 | 5.3 | 2.02 | 2.01 |
| 2461.5 | 0.64 | 2.29 | 1.97 | 2.1 | 2.53 | 5.31 | 2.03 | 2.02 |
| 2462 | 0.64 | 2.29 | 1.98 | 2.11 | 2.53 | 5.31 | 2.03 | 2.02 |
| 2462.5 | 0.64 | 2.3 | 1.98 | 2.11 | 2.54 | 5.31 | 2.03 | 2.02 |
| 2463 | 0.64 | 2.3 | 1.98 | 2.11 | 2.54 | 5.32 | 2.03 | 2.02 |
| 2463.5 | 0.64 | 2.3 | 1.98 | 2.11 | 2.54 | 5.32 | 2.04 | 2.03 |
| 2464 | 0.64 | 2.3 | 1.98 | 2.11 | 2.55 | 5.33 | 2.04 | 2.03 |
| 2464.5 | 0.64 | 2.3 | 1.99 | 2.11 | 2.55 | 5.33 | 2.04 | 2.03 |
| 2465 | 0.64 | 2.31 | 1.99 | 2.12 | 2.55 | 5.33 | 2.04 | 2.03 |
| 2465.5 | 0.64 | 2.31 | 1.99 | 2.12 | 2.55 | 5.34 | 2.05 | 2.04 |
| 2466 | 0.64 | 2.31 | 1.99 | 2.12 | 2.56 | 5.34 | 2.05 | 2.04 |
| 2466.5 | 0.64 | 2.31 | 2 | 2.12 | 2.56 | 5.35 | 2.05 | 2.04 |
| 2467 | 0.64 | 2.31 | 2 | 2.12 | 2.56 | 5.36 | 2.05 | 2.05 |
| 2467.5 | 0.64 | 2.31 | 2 | 2.12 | 2.56 | 5.36 | 2.06 | 2.05 |
| 2468 | 0.64 | 2.32 | 2 | 2.12 | 2.56 | 5.37 | 2.06 | 2.05 |
| 2468.5 | 0.64 | 2.32 | 2 | 2.12 | 2.57 | 5.37 | 2.06 | 2.05 |
| 2469 | 0.64 | 2.32 | 2.01 | 2.12 | 2.57 | 5.38 | 2.06 | 2.06 |
| 2469.5 | 0.64 | 2.32 | 2.01 | 2.13 | 2.57 | 5.38 | 2.07 | 2.06 |
| 2470 | 0.64 | 2.33 | 2.01 | 2.13 | 2.57 | 5.39 | 2.07 | 2.06 |
| 2470.5 | 0.64 | 2.33 | 2.01 | 2.13 | 2.57 | 5.39 | 2.07 | 2.07 |
| 2471 | 0.64 | 2.33 | 2.02 | 2.13 | 2.57 | 5.4 | 2.07 | 2.07 |
| 2471.5 | 0.64 | 2.33 | 2.02 | 2.13 | 2.58 | 5.4 | 2.07 | 2.07 |
| 2472 | 0.64 | 2.34 | 2.02 | 2.13 | 2.58 | 5.41 | 2.07 | 2.07 |
| 2472.5 | 0.64 | 2.34 | 2.02 | 2.14 | 2.58 | 5.41 | 2.08 | 2.08 |
| 2473 | 0.64 | 2.34 | 2.02 | 2.14 | 2.58 | 5.42 | 2.08 | 2.08 |
| 2473.5 | 0.64 | 2.34 | 2.03 | 2.14 | 2.58 | 5.42 | 2.08 | 2.08 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2474 | 0.64 | 2.35 | 2.03 | 2.14 | 2.59 | 5.43 | 2.08 | 2.08 |
| 2474.5 | 0.64 | 2.35 | 2.03 | 2.15 | 2.59 | 5.43 | 2.08 | 2.09 |
| 2475 | 0.64 | 2.35 | 2.03 | 2.15 | 2.59 | 5.44 | 2.09 | 2.09 |
| 2475.5 | 0.64 | 2.35 | 2.04 | 2.15 | 2.59 | 5.44 | 2.09 | 2.09 |
| 2476 | 0.64 | 2.36 | 2.04 | 2.16 | 2.6 | 5.45 | 2.09 | 2.09 |
| 2476.5 | 0.64 | 2.36 | 2.04 | 2.16 | 2.6 | 5.45 | 2.09 | 2.1 |
| 2477 | 0.64 | 2.36 | 2.04 | 2.16 | 2.6 | 5.46 | 2.1 | 2.1 |
| 2477.5 | 0.64 | 2.37 | 2.04 | 2.17 | 2.6 | 5.46 | 2.1 | 2.1 |
| 2478 | 0.64 | 2.37 | 2.05 | 2.17 | 2.61 | 5.47 | 2.1 | 2.11 |
| 2478.5 | 0.64 | 2.37 | 2.05 | 2.17 | 2.61 | 5.47 | 2.1 | 2.11 |
| 2479 | 0.64 | 2.38 | 2.05 | 2.18 | 2.61 | 5.48 | 2.11 | 2.12 |
| 2479.5 | 0.64 | 2.38 | 2.05 | 2.18 | 2.62 | 5.49 | 2.11 | 2.12 |
| 2480 | 0.64 | 2.38 | 2.05 | 2.18 | 2.62 | 5.49 | 2.12 | 2.12 |
| 2480.5 | 0.64 | 2.39 | 2.06 | 2.19 | 2.62 | 5.5 | 2.12 | 2.13 |
| 2481 | 0.64 | 2.39 | 2.06 | 2.19 | 2.63 | 5.5 | 2.12 | 2.13 |
| 2481.5 | 0.64 | 2.4 | 2.06 | 2.2 | 2.63 | 5.51 | 2.13 | 2.14 |
| 2482 | 0.64 | 2.4 | 2.06 | 2.2 | 2.63 | 5.51 | 2.13 | 2.14 |
| 2482.5 | 0.64 | 2.4 | 2.07 | 2.2 | 2.64 | 5.52 | 2.13 | 2.15 |
| 2483 | 0.64 | 2.41 | 2.07 | 2.21 | 2.64 | 5.52 | 2.14 | 2.15 |
| 2483.5 | 0.64 | 2.41 | 2.07 | 2.21 | 2.64 | 5.53 | 2.14 | 2.15 |
| 2484 | 0.64 | 2.42 | 2.08 | 2.21 | 2.65 | 5.53 | 2.15 | 2.16 |
| 2484.5 | 0.64 | 2.42 | 2.08 | 2.22 | 2.65 | 5.54 | 2.15 | 2.16 |
| 2485 | 0.64 | 2.42 | 2.08 | 2.22 | 2.66 | 5.54 | 2.15 | 2.17 |
| 2485.5 | 0.64 | 2.43 | 2.09 | 2.22 | 2.66 | 5.55 | 2.16 | 2.17 |
| 2486 | 0.64 | 2.43 | 2.09 | 2.22 | 2.66 | 5.55 | 2.16 | 2.17 |
| 2486.5 | 0.64 | 2.44 | 2.09 | 2.23 | 2.67 | 5.56 | 2.16 | 2.18 |
| 2487 | 0.64 | 2.44 | 2.1 | 2.23 | 2.67 | 5.56 | 2.17 | 2.18 |
| 2487.5 | 0.64 | 2.44 | 2.1 | 2.23 | 2.67 | 5.57 | 2.17 | 2.18 |
| 2488 | 0.64 | 2.45 | 2.1 | 2.23 | 2.68 | 5.57 | 2.17 | 2.18 |
| 2488.5 | 0.64 | 2.45 | 2.11 | 2.24 | 2.68 | 5.58 | 2.17 | 2.19 |
| 2489 | 0.64 | 2.45 | 2.11 | 2.24 | 2.69 | 5.58 | 2.18 | 2.19 |
| 2489.5 | 0.64 | 2.46 | 2.12 | 2.24 | 2.69 | 5.58 | 2.18 | 2.19 |
| 2490 | 0.64 | 2.46 | 2.12 | 2.24 | 2.69 | 5.59 | 2.18 | 2.19 |
| 2490.5 | 0.64 | 2.46 | 2.12 | 2.25 | 2.7 | 5.59 | 2.19 | 2.2 |
| 2491 | 0.64 | 2.46 | 2.13 | 2.25 | 2.7 | 5.59 | 2.19 | 2.2 |
| 2491.5 | 0.64 | 2.47 | 2.13 | 2.25 | 2.7 | 5.59 | 2.19 | 2.2 |
| 2492 | 0.64 | 2.47 | 2.13 | 2.25 | 2.7 | 5.59 | 2.2 | 2.2 |
| 2492.5 | 0.64 | 2.47 | 2.14 | 2.25 | 2.71 | 5.59 | 2.2 | 2.2 |
| 2493 | 0.64 | 2.47 | 2.14 | 2.26 | 2.71 | 5.59 | 2.2 | 2.2 |
| 2493.5 | 0.64 | 2.47 | 2.14 | 2.26 | 2.71 | 5.59 | 2.2 | 2.21 |
| 2494 | 0.64 | 2.47 | 2.14 | 2.26 | 2.71 | 5.59 | 2.2 | 2.21 |
| 2494.5 | 0.64 | 2.47 | 2.14 | 2.26 | 2.71 | 5.58 | 2.2 | 2.21 |
| 2495 | 0.64 | 2.47 | 2.14 | 2.26 | 2.7 | 5.58 | 2.21 | 2.21 |
| 2495.5 | 0.64 | 2.47 | 2.14 | 2.26 | 2.7 | 5.57 | 2.21 | 2.2 |
| 2496 | 0.64 | 2.46 | 2.14 | 2.26 | 2.7 | 5.57 | 2.21 | 2.2 |
| 2496.5 | 0.64 | 2.46 | 2.14 | 2.26 | 2.7 | 5.56 | 2.2 | 2.2 |
| 2497 | 0.64 | 2.46 | 2.14 | 2.26 | 2.69 | 5.56 | 2.2 | 2.2 |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2497.5 | 0.65 | 2.45 | 2.13 | 2.25 | 2.69 | 5.55 | 2.2 | 2.19 |
| 2498 | 0.65 | 2.45 | 2.13 | 2.25 | 2.68 | 5.54 | 2.2 | 2.19 |
| 2498.5 | 0.65 | 2.44 | 2.12 | 2.25 | 2.68 | 5.53 | 2.19 | 2.19 |
| 2499 | 0.65 | 2.44 | 2.12 | 2.24 | 2.67 | 5.53 | 2.19 | 2.18 |
| 2499.5 | 0.65 | 2.43 | 2.11 | 2.24 | 2.66 | 5.52 | 2.18 | 2.18 |
| 2500 | 0.65 | 2.43 | 2.11 | 2.23 | 2.66 | 5.51 | 2.18 | 2.17 |